## Slide 1
Christian Cupak, Martina Fellinger, Paul Szabo and Friedrich Aumayr
TU Wien (Fusion@ÖAW)
SDTrimSP related modelling of erosion including morphology, roughness, fuzz
Kickoff Meeting, June 28th, 2021
PWIE SP-D2 Kickoff Meeting Proposed Plans for tasks in 2021
Diploma Thesis
Fusion@ÖAW Vienna, Austria

## Slide 2
  Eurofusion PWIE SP-D.2 (Production of Atomic/Molecular and Surface Data) 2021/01/01 – 2022/12/31
  Our deliverables:
Erosion information of surfaces including morphology, roughness, fuzz (ÖAW)
This presentation:
Overview on our recent BCA code studies
Current developments
Key goals for this SP-D task
Outline
Diploma Thesis
Fusion@ÖAW Vienna, Austria
Outline

## Slide 3
  Key goal: Simulate preferential sputtering of FeW (1.5 at. % W) under 45°, 250eV D bombardment
Outline
Diploma Thesis
Fusion@ÖAW Vienna, Austria
Recent BCA code studies: D on FeW model films
Experiment:
AFM → surface structure of sample
Sputter-XPS → elemental depth information
QCM → in-situ mass removal rate over fluence
TRI3DYN simulation:
Input: AFM image section (200x200µm²), 2x mirrored
Input: target composition from Sputter-XPS
Dynamic mode, same inc. angle and fluence applied
AFM
Sputter-XPS
QCM
  [R. Stadlmayr et al., Phys. Scripta (2020) doi:10.1088/1402-4896/ab438f]

## Slide 4
  Outcome:
Outline
Diploma Thesis
Fusion@ÖAW Vienna, Austria
Recent BCA code studies: D on FeW model films
  [R. Stadlmayr et al., Phys. Scripta (2020) doi:10.1088/1402-4896/ab438f]
Surface patterning
W enrichment due to preferential sputtering
Fluence dependency of mass removal rate

## Slide 5
  Key goal: Simulate dynamic erosion of W-Fuzz under ion bombardment (2keV Ar1+, 60°)
Outline
Diploma Thesis
Fusion@ÖAW Vienna, Austria
Recent BCA code studies: W Fuzz
  [R. Stadlmayr et al., J. Nucl. Mater. (2020) doi:10.1016/j.nme.2019.100722]
SEM image:
Input for TRI3DYN
60°
Ar+
Simulation:
Fluence 1.7E+22m-2
Dynamic
2keV Ar (60°)
  Results:
„Dragonscale“ development found and validated,
pointing towards incoming ion beam direction
Redeposition of sputtered atoms reduces sputter yield
Sputter yield rises with increasing fluence due morphology changes

## Slide 6
  Limitation for 3D BCA codes: surface input limited in size to areas of ≈ 100x100 nm²
  Idea: Use BCA repository data for local ion impact, but raytracing for large scale roughness simulation
  SPRAY = SPuttering simulation via RAYtracing of particles
Outline
Diploma Thesis
Fusion@ÖAW Vienna, Austria
Current developments + key goals for SP-D
δ
Raytracing
BCA
AFM/SEM/CFM images of surface
Primary ions with random impact point
Local ion incidence -> selection of BCA code (i.e., SDTrimSP) data → sputter yields → reflection coefficients → trajectories of emitted particles/ions
Emission of particles / reflected ions + raytracing
Results:
Calculation of effective sputter yields for large-scale images
Emission distribution of sputtered particles / refl. ions

## Slide 7
  Current features of SPRAY:
  Independent on image size, quick calculations on desktop PCs
  Shadowing (C), sputtering via reflected ions (D) & redeposition (E) considered
  Our key goals for this SP-D task:
  a) Further development and benchmarking of SPRAY
    → application for real W surfaces (AFM)
    → implementation of new features (multicomponent targets,…)
    → modelling the dynamics of systematically increasing roughness on erosion
  b) Connection to our SP-B task (lab experiments):
    Det. sputtering, …, of W model systems with var. morphologies and re-dep. W layers (QCM meas.)
    We have the tools to handle both nano- and microscopic roughness
Outline
Diploma Thesis
Fusion@ÖAW Vienna, Austria
Current developments + key goals for SP-D

## Slide 8
  Backup slides
Outline
Diploma Thesis
Fusion@ÖAW Vienna, Austria

## Slide 9
FC cup measurement before and after experiment
Initial Ar cleaning of target
Record QCM resonance frequency during ion induced mass loss
Via ion flux and frequency -> sputter yield
[6]
[6] Sauerbrey G., 1959 (https://doi.org/10.1007/BF01337937)
Beam on
Target QCM
Diploma Thesis
Fusion@ÖAW Vienna, Austria
Detailed QCM procedure

## Slide 10
QCM electronics -> regulation loop to drive quartz in resonance
Resonance frequency changes due to mass loss in experiments
≈ 90 [pg/s] ≈ 3⋅10-4 [W monolayers/s]
Sensitivity:
[G. Hayderer et al., Rev. Sci. Instrum., 70 (1999) 3696-3700.]
[K. Dobes, PhD thesis, TU Wien (2014)]
Diploma Thesis
Fusion@ÖAW Vienna, Austria
Details QCM performance