## Slide 1: SP-X.2: Optimization of laser-based surface analysis diagnostics
Peeter Paris, Indrek Jõgi
University of Tartu

## Slide 2: Tasks and deliverables 2021-2022
Chart: Shot nr.
 | 1290.1826 | 1581.9986 | 1473.7643 | 1354.0281 | 1328.5798 | 1291.4109 | 952.4731 | 758.7541 | 616.4933 | 341.7792 | 318.5441 | 293.4836 | 287.4091 | 215.7554 | 168.2388 | 216.7543 | 157.1228 | 152.4806 | 112.0474 | 91.6364 | 115.3957 | 83.0484 | 52.0466 | 78.9791 | 70.4208 | 40.0323 | 20.8596 | 14.9578 | 25.1241 | 13.3019 | 12.6077 | 0.94413 | -6.6601 | 5.1037 | -20.4527 | -9.324 | -18.3179 | -4.0278 | -17.6963 | -28.0804
 | 378.6629 | 484.2839 | 369.2005 | 575.2548 | 504.6896 | 505.7003 | 526.8686 | 544.3516 | 574.4233 | 521.7215 | 537.2085 | 572.8147 | 542.9433 | 550.753 | 546.9849 | 512.4506 | 560.5164 | 465.0832 | 409.1231 | 345.0192 | 370.7551 | 366.5861 | 286.3157 | 286.9204 | 281.9864 | 306.1968 | 206.113 | 239.7493 | 200.103 | 155.5679 | 290.7182 | 186.9147 | 158.7167 | 97.8048 | 193.9434 | 206.4039 | 146.2376 | 191.9566 | 208.9563 | 87.1634
 | 808.0955 | 904.3133 | 782.8351 | 446.1411 | 535.5946 | 699.1079 | 524.8776 | 780.0949 | 825.4559 | 531.9116 | 792.4096 | 774.9883 | 723.1736 | 728.4378 | 823.8923 | 677.8159 | 727.9562 | 782.7732 | 600.0102 | 639.5936 | 627.7058 | 789.8151 | 516.8213 | 425.6719 | 361.3646 | 638.3387 | 406.4782 | 586.9648 | 387.0362 | 329.4426 | 502.5401 | 185.2383 | 225.0699 | 96.1159 | 252.5781 | 210.5824 | 56.7153 | 199.0572 | 93.6527 | 63.9569
 | 401.9865 | 272.731 | 271.1612 | 168.6305 | 181.9401 | 322.34 | 1378.8484 | 2178.0454 | 2121.2278 | 3476.893 | 3514.7034 | 3712.7122 | 3081.5146 | 3778.7557 | 3504.6138 | 3315.8987 | 3749.9755 | 3561.4532 | 3611.3133 | 3650.7849 | 3618.7764 | 4144.3979 | 4105.5113 | 3484.2478 | 3849.8556 | 3762.4833 | 3602.6618 | 3815.7934 | 3618.0545 | 3925.8701 | 3744.4103 | 3888.7542 | 3722.1104 | 3828.6017 | 3810.3765 | 3850.7156 | 3767.4175 | 3737.5009 | 3812.8502 | 4099.5374
1. Comparison of ps vs. ns LIBS regarding absolute composition and D content in reference and ITER-relevant coatings which can include impurities
Plans: additional studies in different plume region and with laser at 1064 nm
  Studies with W-Ta(5%)-D(5/10%) and W-N(5%)-D(0/5/10%) (by GDOAS)
  Nd:YAG at 532 nm (7ns), LIBS in Ar at 1, 10 and 100 torr, delay time 300 or 1300 ns
  Czerny-Turner spectrometer + iCCD: 410-430 nm and 645-665 nm
Chart: Wavelength (nm)
10 torr, 1300 ns
D
H
Chart: Energy (eV)
| 3.79 | 5.04 | 3.41 | 3.71 | 5.17 | 4.84 | 5.16 | 3.27 | 3.25 | 3.25 | 5.34 | 13.620000000000001 | 13.07 | 12.64
 | -3.6268 | -4.407 | -2.0629 | -4.0586 | -3.8148 | -5.7856 | -5.1044 | -5.8757 | -3.5701 | -3.9648 | -3.7721 | -5.3013 | -13.1952 | -12.6889 | -12.2897
 | -4.527 | -4.9262 | -2.8748 | -4.9797 | -4.0828 | -6.4236 | -5.865 | -6.1645 | -4.162 | -4.6845 | -4.4803 | -6.0032 | -15.1889 | -15.0431 | -14.4869
 | -4.6921 | -5.3031 | -3.109 | -5.3582 | -3.8256 | -6.3646 | -6.1242 | -6.4023 | -4.2642 | -5.0855 | -4.6915 | -6.2172 | -17.8832 | -17.0954 | -16.7394
300 ns
100 torr
1 torr
H isotope detection
Saha-Boltzmann plots
Chart: Pressure (torr)
| 1 | 10 | 100
 | 6644626434990828 | 51730503536183904 | 2.8272e+17
 | 0.73486 | 0.88907 | 1.0485
Electron density and temperature
300 ns
Chart: Pressure (Torr)
| 1 | 10 | 100
 | 1.7 | 1.1 | 1.05
D/W ratio by CF-LIBS
Example with W-Ta(5%)-D(5%) coating
Depth profile
45°
laser
collection of spectra
target

## Slide 3: Tasks and deliverables 2021-2022
2. (CF-) LIBS (ns SP) on samples from different devices
  Studies with 3 WEST samples outside from the regions of strong erosion and deposition
  LIBS in Ar at 1 or 10 torr, delay time 300 or 1300 ns, fluences 10-33 J/cm2
  Czerny-Turner spectrometer + iCCD: 645-665 nm and Andor Mechelle spectrometer
3. (CF-)LIBS on Be containing coatings with different type of fuel content
  New measurements not possible in near future due to the COVID-19 restrictions
Plans: recycling the results of previous experiments?
4. CF-LIBS on produced reference samples before and after He loading
  Experiments with various samples doped or loaded by He
  He detectable during first shot at relatively short delay time (100-200 ns) in Ar at 1-2 Torr
Plans: new samples?
Average ablation rate
≈100 nm/shot
Chart: Wavelength (nm)
Chart: Shot nr.
Plans: compare samples, check CF-LIBS

## Slide 4: Tasks and deliverables 2021-2022
5. Investigate erosion/deposition/fuel retention (including He) by in situ (CF)-LIBS and NRA/RBS in MAGNUM with subjects of interest: outgassing, recycling, and role of impurities (O, N), Tsurface, and implantation energy on retention
  Studies with W-Ta(5%) and W-O samples exposed to D2-N2 or D2-N2-He plasma
  in-situ ns-LIBS with Nd:YAG at 1064 nm (6ns) in Ar at 1, mbar, delay time 1300 ns
Chart: Position (mm)
| -9 | 9 | -6 | 6 | -3 | 3 | 0
360C | 3.1337 | 3.8763 | 1.5345 | 1.4975 | 1.2413 | 1.3345 | 1.0146
200C | 4.0913 | 1.7714 | 1.4669 | 1.1846 | 1.3897 | 1.5571 | 3.4065
410C | 0.9732 | 0.48597 | 0.38753 | 0.43769 | 0.48723 | 0.47783 | 0.70173
Plans: compare with in-situ NRA results and carry out ex-situ LIBS and/or SIMS?
Chart: Shot nr.
Chart: Shot nr.
360°C
-9 mm
0 mm
W-Ta(5%)