## Slide 1: Analysis of Material behavior e.g. (Wf/W) under Plasma and heat loading regarding mechanical properties e.g. cracking, embrittlement, and microstructure. (FZJ)
Jan W. Coenen , A. Litnovsky and Contributors
1: Forschungszentrum Jülich GmbH, Institut für Energie- und Klimaforschung 52425 Jülich, Germany,; 2: Department of Engineering Physics, University of Wisconsin Madison, WI 53706 Madison, USA
Advanced Engineering Materials
Fusion Materials Development at Forschungszentrum Juelich
DOI:10.1002/adem.201901376

## Slide 2: Porous matrix Wf/W by SPS
A controlled amount of fine scale matrix porosity, obviating the need for a fiber coating.
This approach can be viewed as an extension of the porous coating concept wherein crack deflection occurs because of the low fracture toughness of the porous interphase
Compare to conventional Wf/W
No interface needed
  easy to produce
Lower process temperature
  less fiber recrystallization
More homogeneous material
  no weak interface area
Thermal conductivity reduced
Retention?
Wf/W

## Slide 3: Tungsten based Smart ALLOYs
Challenge:
Suppress oxidation when utilizing refractories during ‘Loss of coolant’ and air ingress
Utilize chromium and yttrium to achieve stable oxidation suppression
1000°C, 1 bar,
80 vol.% Ar+20 vol.% O2, 10 hours
Fusion accidents & Oxidizing environments
W-Cr-Y alloys form protective chromium oxide layer
Formation of tungsten-oxides is suppressed
Addition of yttrium (~ 0.6 wt%) is crucial
Nucleation sites, grain-boundary segregation, oxide pegs, impurity binding…
Litnovsky, A.; Klein, F.; Schmitz, J.; Wegener, T.; Linsmeier, C.; Gilbert, M.; Rasinski, M.; Kreter, A.; Tan, X.; Mao, Y.; Coenen, J.W; Bram, M. & Gonzalez-Julian, J. Smart first wall materials for intrinsic safety of a fusion power plant Fusion Engineering and Design, Elsevier BV, 2018

## Slide 4: Wf/W in PSI-2
Y.Mao

## Slide 5: Plasma wall interaction on porous matrix Wf/W
Neon plasma, 98-117 eV, total fluence of 5.4×1025 Ne+ m-2, 100 min, ~200⁰C
Theoretical weight loss due to sputtering is 4.0 mg
With the increasing porosity, the weight loss decreases
The sputtered W were re-caught by the pores/surface roughness
Before Ne erosion
After Ne erosion
-A. Kreter, 2008

## Slide 6: Thermal shock
W
85%
92%
Labs = 0.38 GW/m2, Tbase = RT, n = 1000 pulses
1.6GW/M2 2ms
Laser thermal shock has been performed to simulate the transient heat load
The cracking threshold of porous matrix is between 0.19 GWm-2 and 0.38 GWm-2, which is similar to ITER-grade W
Due to low thermal conductivity, severe melting are observed under loading condition of 1.6 GWm-2 for 2ms.

## Slide 7: PM Wf/W
Porous Matrix Properties
D Plasma Exposure
Bias voltage 78 eV;
Total fluence was 4.99x1025D+ m-2. Temperature was ~202 °C.
D retention was measured by TDS
Porous matrix Wf/W shows similar behavior compared to pure W

## Slide 8: Smart-W

## Slide 9: HHF and plasma tests on SMART alloys
Alloy | Plasma tests | HHF tests | Comments
SMART W-Cr-Y | Finished by now PSI 2 and Magnum PSI | Planned for 2022 | We will see depending on modeling whether new tests are required
SMART W-Cr-Zr | 2021-2022* PSI 2 | not yet in plan | New: oxidation resistance confirmed Tests depend on availability of samples supplied by HFUT (CN)
Nanostructured alloys | 2021-2022* PSI 2 | not yet in plan | Tests depend on availability of samples supplied by SBU (USA)
Status and plans

## Slide 10: Understanding material response to plasma exposure
Modification of the work of P.S. Ho [5] by adding segregation flux
Combined model : erosion, diffusion and segregation
Note: preferential sputtering of
[5] P.S. Ho, Surface Science 72 (1978) 253-263
diffusion with surface recession and segregation
Surface recession velocity
(atomic-) density normalized sputter yields
Coming next: application of the model to experiments
P. Bittner

## Slide 11: Add Ons

## Slide 12: Laser shock by PSI-2
Fiber vertical to the loading surface
Fiber parallel to the loading surface
Loading condition
Labs = 0.38 GW/m2, Tbase = RT, n = 100 pulses
After the loading: crack bridging by the fibers

## Slide 13: Long fiber Wf/W by PM
4-point bending test: flexural strength: ~466 Mpa
Random fiber porous matrix Wf/W with 40% fiber content: ~250 Mpa
Random fiber conventional Wf/W with yttria interface and 30% fiber content: ~230 MPa
Pre-notched 3-point bending tests