## Slide 1: PWIE-SP A.3.T - T001- D002 Performance of advanced materials under high heat loads and their microstructural characterization
J. Riesch*,a, Y. Maob,c, D. Schwalenbergb,e, B. Böswirtha, S. Elgetia, H. Greunera, L. Raumannb, J.W. Coenenb,d, and R. Neua,e
aMax-Planck-Institut für Plasmaphysik, 85748 Garching, Germany
bForschungszentrum Jülich GmbH, Institut für Energie- und Klimaforschung – Plasmaphysik, 52425 Jülich, Germany
cSchool of Mechanical Engineering, Hefei University of Technology, Hefei 230009, China
dDepartment of Engineering Physics, University of Wisconsin - Madison, Madison, WI53706, USA
eTechnische Universität München, 85748 Garching, Germany
Notes: 20 min + 3 min Diskussion

## Slide 2: HHF tests of block-based mock-ups in GLADIS
Aim: Test material until its limit
GLADIS: Homogeneous heating by H neutral beams
  Heat flux: 10/15/20 MW/m²
  Pulse length: 30s (equilibrium after 13s)
  Actively cooled: water inlet 20 °C, 12 m/s
  Procedure
    First step: screening up to maximum heat flux
    Second step: 100 cycles at maximum heat flux
Block based mock-up
  CVD- and PM-Wf/W
  Different sample heights to vary the surface temperature
  5mm x 10mm x 5/10/15/20mm (EU DEMO divertor targets R&D; W armour thickness 5-8 mm) [J.H. You et al. Journal of Nuclear Materials 544 (2021) 152670]
Garching LArge DIvertor Sample test facility [Greuner et al. J NUCL MATER 367-370,(2007) 1444-1448]
soldered Wf/W blocks
W coated CuCrZr
Notes: Lieber Hans,
die H atom fluence ist beim cycling 100 Pulse a 15 s für:
15 MW/m² = 7 e24 H/m²
10 MW/m² = 5,5 e24 H/m²
Beachte aber die abgeschnittenen Blöcke woh Du narürlich die fluence nicht zusammen addieren kannst.
Grüße, henri
Divertor targets R&D
Armour thickness 5-8mm
witdth 23 x 4/12mm
J.H. You, E. Visca, T. Barrett et al.
Journal of Nuclear Materials 544 (2021) 152670

## Slide 3: Status & Results
Status
CVD- and conventional PM-Wf/W: HHF tests completed; microstructural analysis almost done
Porous PM-Wf/W in Gladis: 10 MW/m2 done, microstructural analysis started
GLADIS days in 2021: 3 spent + 2-3 planned
Results
CVD-Wf/W
  Depending on architecture survival up to 20 MW/m2 & crucial role of fibre orientation and manufacturing
PM-Wf/W
  very good performance up to 15 MW/m2 & some degradation at 20 MW/m2 (under evaluation)
100th pulse
400
1600
2800
Tsurf=3293
200 µm
Conventional PM Wf/W after 100 pulses at 15 MW/m2
Porous PM Wf/W after 100 pulses at 10 MW/m2