## Slide 1
Assessment of hydrogen impact on material properties linked to ITER relevant PFUs
M. Richou, G. Kermouche1, M. Lemetais, L. Gallais2 and the WEST team
SPA - Midterm -15th of September 2021
1
2

## Slide 2
1. Studied tungsten
2. Use of WEST to assess hydrogen impact on recrystallization and softening
3. What are the properties we plan to investigate ?
  Loss of mechanical properties -> Hardness measurements
  Modification of the microstructure -> EBSD measurements
4. For what modelization ?
  Impact on recrystallization and softening kinetics.
OUTLINE

## Slide 3: 1. Studied tungsten – implementation in WEST
Incident flux
CuOFHC
CuCrZr
Tungsten and component manufactured by AT&M/ASIPP
ITER-like Geometry:
  6mm W thickness
  Block width from 26.3 mm to 31.8 mm
  AT&M rolled W (ITER W grade material)
A-A
500 mm

## Slide 4: 2. Use of WEST to assess hydrogen impact on recrystallization and softening (1/2)
WEN004 (Position 18)
WEN003 (Position 17)
C4
C5
WEN004 (Position8)
 | Duration max (s) | Cumul (s) | LH max (MW) | W LH total (MJ) | Max heat flux (MW/m²)
C4 – D2 | 55 (USN) | 9678 | 5.4 | 7823 | 6 [J.Gaspar, Nuclear Fusion, 2021]
July-Nov19 |  |  |  |  | 
C4 - He | 30 | 2991 | 4.5 | 4300 | 
Oct-Nov19 |  |  |  |  | 
C5 | 23 | 4630 | 5.4 | 2625 | Under investigation
Nov20-Jan21 |  |  |  |  | 
2 components chosen and available for this study (2021)
Future activities:
Estimates of campaign integrated fluence to be performed, uncertainties to be assessed

## Slide 5: 2. Use of WEST to assess hydrogen impact on recristallisation and softening (2/2)
Chart: 
 | 0.76026 | 0.82507 | 0.88787 | 0.92862 | 0.96799 | 0.99219 | 1 | 0.98934 | 0.96547 | 0.92613 | 0.87428 | 0.81499 | 0.74695 | 0.68119 | 0.61665 | 0.56133 | 0.51516 | 0.48133 | 0.46527 | 0.46375 | 0.48058 | 0.51236 | 0.55874 | 0.61625 | 0.67894 | 0.73743 | 0.80572 | 0.86903 | 0.91278 | 0.9545 | 0.9854 | 0.9994 | 0.99595 | 0.97604 | 0.9409 | 0.89122 | 0.83611 | 0.77107
 | 0.16693 | 0.15685 | 0.14772 | 0.14016 | 0.13455 | 0.13136 | 0.13059 | 0.13246 | 0.13673 | 0.14315 | 0.1514 | 0.16088 | 0.17106 | 0.18068 | 0.19033 | 0.1988 | 0.20557 | 0.21022 | 0.21245 | 0.21213 | 0.2093 | 0.20407 | 0.19679 | 0.19066 | 0.18078 | 0.17039 | 0.16013 | 0.15063 | 0.14246 | 0.1362 | 0.13212 | 0.13059 | 0.13153 | 0.13504 | 0.14081 | 0.14847 | 0.15762 | 0.16763
Maximum of heat flux on PFU surface*
(Normalized to max OSP)
* : depends on plasma scenario (magnetic configuration, in/out asymmetry …)
OSP
ISP
N° PFU
100 %
50 %
5
C4
C5
Future activity:
temperature range reached during plasma operation under assessment (geometry, misalignement..)
Notes: ces composants n’ont pas dépassé 700°C à tout casser sur la top surface (à confirmer par Yann),
Seul endroit où ça a pu chauffer plus localement : bord d’attaque de composants désalignés (je ne sais pas si c’est le cas des 2 que tu as choisi). Ou sinon, pendant les chocs thermiques liés aux disruptions etc, mais sur des temps très courts, dc recrystalisation peu vraisemblable
De yann:
Pour C4 on trouve 110 pulses avec une température FBG > 400°C, et environ 30 chocs avec un TFBG > 600°C, quelques pulses autour de 800°, mesure située à 4mm de la surface donc suffisamment proche pour donner une bonne estimation (en tout cas une borne inférieure) – bien entendu la température vraie de surface est légèrement supérieure, par exemple pour 800°C mesuré on estime avec les calculs de Jonathan une température de surface de 1000°C environ. Donc je dirai que nous avons une petite dizaine de chocs ou Tsurface approche les 1000°C à la fin du choc.

## Slide 6: 3. What are the properties we plan to investigate ? (1/3)
A. Durif, 2019, Fus. Eng and design
Thermal gradient within the component is present during plasma loading
What is the effect of combined loading on tungsten microstructure and softening ?
Objective : Characterize the modification of the microstructure (time and temperature dependent), the softening to propose predictive recrystallization and softening kinetics models

## Slide 7: 3. What are the properties we plan to investigate ? (2/3)
Set up Sketch
First trials on non-loaded components (2021) 
Future objective:
Perform the measurements on the WEST components (formal procedure for PFU return to public domain ongoing)
y
y
1 mm

## Slide 8: 3. What are the properties we plan to investigate ? (3/3)
Nanoindentation : Statistical nanoindentation analysis can help to separate contributions of recovery / recrystallization mechanisms to macroscopic softening
EBSD : Estimation of grain size distribution, quantification of recrystallized-non recrystallized grains
Future objective:
Need to cut the components (authorization pending and cutting scheme under construction)
Nanoindentation
L. Karanja, 2021, Crystals

## Slide 9: 4. For what modelization ?
A. Durif, 2021, Submitted
Mean field model can help to evidence/discriminate recrystallisation-induced softening from recovery-induced softening
Future objective:
According to measurements, propose parameters to be implemented in models

## Slide 11
Metrology C4
5
12
20
30
17 18