## Slide 1: LID hydrogen desorption dynamics
30.3.2020 I Miroslaw Zlobinski, et al.
Spectroscopic Observations

## Slide 2
Spectroscopic setup at TEXTOR
2
920
1140
100
and observation sytem (CLIO)
400
liner (r=550)
coaxial laser injection
14 bit digital VIS camera 100 Hz, 0.3 Mpixel,
synchronized with laser,
with gateable image intensifier (10 ns – 60 s)
LCFS (r=460)
coaxial observation (CO) fibre to hi-resolution spectrometer
(5-15 pm), 2 Hz, range: 363-715 nm synchronized with laser
CaF2 lenses
path in vacuum: 2200 mm
SOL (r>460)
7°
neutral density and spectral filters
(r=470)
toroidal field coil
HFS
LFS
horizontal observation (HO)
integrating spectrometers
polychromator
R = 0
R = 1750
(r=477)
PK16
PK27
PK14
PK21
spatially resolving spectrometer
10b
9
11
7°
vertical observation (VO) IR camera (3 types): 10 – 3500 Hz
300 – 7000 K
8 bit VIS camera
50 Hz, 0.2 Mpixel
with image intensifier
laser fibre optics, 400 µm core diameter, 30 m
monitoring diode
LASAG
Nd:YAG Laser
1064 nm
Emax = 50 J / pulse
1050
200
150
920
f=630
f=560
f=360
f=250
several fast diodes with spectral filters to observe selected wavelength emission

## Slide 3
Spectroscopic observation
3
W surface
without layer
=> for camera observation: integration time of 5 ms was selected
Typically hydrogen desorption shorter than laser pulse.
With increasing layer thickness the desorption duration increases.
Only for very thick layers a fraction of desorption continues after laser pulse. (during spot temperature decay)

## Slide 4
Spectroscopic observation with fast camera
4
[Irrek 2008, hdl.handle.net/2128/3621]
fast camera observation through Ha filter with 2500 Hz, 0.4 ms/frame
5 ms laser pulse duration
desorption from 200 nm a-C:D layer on graphite