## Slide 1: LID rastering mode
30.3.2020 I Miroslaw Zlobinski, et al.
Examples and requirements

## Slide 2
LID spot position scan (rastering mode)
2
10 µm Be/D layer with 1.5 at% D on bulk W substrate (ITER grade)
layer produced in laboratory by magnetron sputtering
Laser pulses every 5 mm => spots not overlapping (3 mm spot diameter)
Pumping:
all pumps off all ionisation gauges off remaining pumping effect probably due to
ionisation in QMS itself
wall effects
[shot1077-1180] FZJ087
mass 4
mass 3
mass 2
QMS signal (MKS)

## Slide 3
LID spot position scan (rastering mode)
3
2 speeds possible:
Slow rastering with intermediate RGA data points => evaluation of each step/pulse individually (extrapolation of pumping effects necessary if pumping time constant ≥ duration between laser pulses)
Fast rastering within one cycle of RGA acquisition => accumulated evaluation (pumping effects can be neglected as they are slower than desorption duration for all laser pulses) requirement: fast movable mirrors