## Slide 1: LID spot temperature measurements and simulations
30.3.2020 I Miroslaw Zlobinski, et al.
Examples and requirements

## Slide 2
LID spot temperature on bulk W
2
W surface
without layer
point pyrometer spot
Laser spot (Ø 3 mm)
ANSYS simulation
For short pulses: agreement of analytic, numeric calculation and measurement within ~100 K (acceptable)

## Slide 3
Effect of surface reflectivity on LID spot temperature (W surfaces)
3
all with W on top surface but still difference in reflectivity up to factor 2 (due to different porosity in CFC and coating coverage)
for comparison: 34 at% C, 25 at% D, 25 at% H, 10 at% W, 5 at% O, 1 at% B

## Slide 4
Effect of surface reflectivity on LID spot temperature (layer effect)
4
Layer growth can lead to reflectivity change of factor 2
a-C:H layer = amorphous hydrocarbon layer

## Slide 5
Effect of layers on LID spot temperature (heat curvature effect)
5
Density * Heat capacity (rc) increase in the layer
leads to different time evolution, but same max. temperature
This effect can be used to deduce information about the layer

## Slide 6
Effect of layers on LID spot temperature (heat offset effect)
6
heat conductivity increases => lower max. temperature in already heated spot
Effect appears esp. if layer material different than substrate
Layer growth => increase in surface temperature (if no adverse reflectivity change) Temperatures could be measured without layer => with layer a lower boundary for the temperature is known => only overheating should appear with layer (neglecting possible reflectivity effects + assuming laser reproducibility)