## Slide 1: Deposition rates
< 5e18 atom D/cm2 deposited over 18.5 hours (divertor plasma ILW3)
Deposition rate 5e18/6.6e4 = 7.5e13 D/cm2/s
Deposition rate per JET pulse (20s) = 15e14 D/cm2
Measurements are based on tiles removed from the vessel (i.e., long term retention)
What are estimates from dynamic retention in-vessel gas balance or long term off gas data?

## Slide 2: ITER-Like Wall Campaigns
Campaign /Period | Plasma time (h) Limiter/x-point | Input energy (GJ)* | Characteristics | Comment
ILW-1 2011-12 79854-83794 | 19 6/13 | 150 | Low power D plasma | C30C 151 # H-mode 83621-83794 15N injection GIM14 83632-83635
ILW-2 2013-14 83795-87944 | 20 5.2/14.2 | 201 | High(er) power D plasma | Finished with 300 # (0.6 h) H 87584-87944
ILW-3 2015-16 88089 - 92504 | 23.4 4.9/18.5 | 245 | D plasma H plasma D plasma (high power) | Finished with 15N2 seeded H-mode (0.25 h) and 18O2 injections 92469-92504
*Energy per tile for ILW1 and ILW2 - Heinola K, et al. 2017 Phys. Scr. T170 14063

## Slide 3: Deposition in the tungsten divertor ILW3 (2015-16)
Determine deposition pattern in JET divertor after ILW-3
Poloidal cross-section of core samples analysed
Decrease of C deposition from ILW-1 to ILW-3
Almost constant retention of D in all three ILW campaigns
Data presented at PFMC 2019 S. Krat et al, Phys. Scr. (submitted)