## Slide 1: IAP activities in 2022: Sample preparation and TDS and GDOES analysis of JET samples- plans and capabilities
C.P. Lungu, C. Porosnicu, B. Butoi, O. G. Pompilian, C. Staicu, V. Zaroschi
E. Grigore, C. Ruset, F. Baiasu
IAP (Institute of Atomic Physics, Bucharest, Romania)

## Slide 2
2022 Sample preparation and cutting – Be tiles
Using beryllium processing facility, we extract components of the Be tiles
Typical sample sizes: 10 mm x 10 mm x 10-12 mm or 10 mm x 10 mm x 2.5 mm
Any other size is possible with some constrains
During cutting the tile temperature did not exceed 58oC
For temperature monitoring in real time a FLIR® E-Series Advanced Thermal Imaging Camera, (+/- 1 oC ; 20-900 oC) was used

## Slide 3
2022 Sample preparation and cutting – Be tiles
Cutting process recording document
Cut samples were packed in special 1” x 1” x 1” plastic boxes and sent to CCFE.
Active surfaces were not touched or exposed to any foreign object

## Slide 4
2022 Sample preparation and cutting - W lamelae
- Special designed diamond milling discs/machine

## Slide 5
2022 TDS capabilities
Sample number | D inventory (atoms)
543 | 4.40E17
551 | 3.35E17
569 | 1.09E18
573 | 7.28E17
580 | 1.41E18
587 | 4.38E17
594 | 4.50E16
Quadrupole mass spectrometer and an oven with a linear heating rate up to a maximum temperature of 1300 K.
Information provided by the TDS system identifies the trapping states of gaseous components in materials and to accurately measure their inventory.
Post mortem analysis of first-wall tiles and divertor components from JET fusion reactor.

## Slide 6
2022 SEM imaging capabilities
Sample / Lamella | 100x | 1000x | 5000x
5/A23 |  |  | 
Sample number | 1000x | 5000x | 10000x
437 |  |  | 

## Slide 7
2022 Nanoindenting capabilities

## Slide 8
2022 Other capabilities – XPS evaluation
Samples (4D14):
339
339 c (Ar etched for 10 min)
355
355c (Ar etched for 10 min)
Be, BeO
Sample | C 1s (%) | O 1s (%) | Be 1s (%) | Ni 2p3 (%) | N 1s (%) | Fe 2p3 (%)
182 | 13.1 | 26.2 | 59.6 | - | 1.1 | -
182_C | 2.8 | 23.2 | 72.4 | 0.1 | 1.5 | 0.1
226 | 37.6 | 12.6 | 47.7 | - | 1.6 | -
226_C | 96.6 | 1.3 | 2.1 | - | - | -
289 | 20.3 | 26 | 51.4 | - | 2.4 | -
289_C | 13.1 | 26.3 | 58.1 | 0.1 | 2.2 | 0.2
290 | 21.2 | 28.1 | 48.6 | - | 2.0 | -
290_C | 13.9 | 25.4 | 58.9 | - | 1.8 | -
339 | 62.7 | 8.5 | 25.5 | - | 1.6 | -
339_C | 58.4 | 7.7 | 31.3 | - | 2.1 | -
355 | 34.8 | 33.6 | 30.5 | - | 1.1 | -
355_C | 17.1 | 37.7 | 43.9 | - | 1.3 | -
367 | 9.9 | 24.2 | 63.9 | 0.2 | 1.5 | 0.2
367_C1 | 2.0 | 24.7 | 71.8 | 0.1 | 1.2 | 0.2
367_C2 | 1.3 | 37.6 | 57.3 | 0.5 | 2.9 | 0.4
368 | 15.7 | 39.7 | 41.3 | 0.7 | 2.1 | 0.5
368_C1 | 9.8 | 41.3 | 45.0 | 0.9 | 2.4 | 0.6
368_C2 | 1.7 | 40.7 | 52.6 | 1.7 | 2.6 | 0.7
369 | 13.1 | 39.4 | 42.6 | 0.9 | 3.5 | 0.7
369_C1 | 3.0 | 44.2 | 48.0 | 1.3 | 2.9 | 0.7
369_C2 | 1.5 | 38.2 | 53.4 | 2.3 | 3.6 | 1.0

## Slide 9
2022 Other capabilities – Surface tritium monitoring
Tritium surface monitor LB 1230UMo with LB 1230 open window gas flow proportional counter detector, Berthold type/ detection area 155 x 15 mm; effective area 22 cm2; detection limits 2.2 Bq, 0.1 Bq/cm2 with window completely open.

## Slide 10
2022 Other capabilities – Surface tritium monitoring
Central tile (211) from 2XR10 IGWL Assembly
36 samples from WPJET3 task were measured

## Slide 11
2022 Other capabilities – Sample tritiation
The glass ampule with W-Mo samples was preliminary vacuumed at room’s temperature (1 h at pressure less than 1 Pa) and degassing at 1000 C (1 h at pressure less than 1.3 10-2 Pa).
The W-Mo samples were put in contact with T2:3He mixture extracted from an old tritium gas source. The samples were kept in the T2:3He atmosphere for 196 hours at 2000 C, followed by slow decrease of the temperature to the room value and maintaining at this temperature for minimum 8 hours.

## Slide 12
2022 Other capabilities – Sample tritiation
The glass ampule with W-Mo samples was preliminary vacuumed at room’s temperature (1 h at pressure less than 1 Pa) and degassing at 1000 C (1 h at pressure less than 1.3 10-2 Pa).
The W-Mo samples were put in contact with T2:3He mixture extracted from an old tritium gas source. The samples were kept in the T2:3He atmosphere for 196 hours at 2000 C, followed by slow decrease of the temperature to the room value and maintaining at this temperature for minimum 8 hours.

## Slide 13
2022 Other capabilities – ICPOES
Sample | B2 | D1 | 31 | C1 | C2 | 11 | 26
Be Wt ratio | 0.766 | 0.626 | 0.592 | 0.422 | 0.248 | 0.399 | 0.854
Cr Wt ratio | 0.032 | 0.023 | 0.030 | 0.048 | 0.112 | 0.003 | 0.000
Cu Wt ratio | 0.003 | 0.024 | 0.022 | 0.043 | 0.058 | 0.010 | 0.002
Fe Wt ratio | 0.152 | 0.105 | 0.110 | 0.338 | 0.379 | 0.304 | 0.085
Mo Wt ratio | 0.004 | 0.045 | 0.004 | 0.008 | 0.030 | 0.003 | 0.015
Ni Wt ratio | 0.025 | 0.127 | 0.131 | 0.030 | 0.059 | 0.057 | 0.011
W Wt ratio | 0.018 | 0.051 | 0.111 | 0.112 | 0.113 | 0.223 | 0.032
B2 - swab pot 27
D1 - divertor dust 2014-11
31 - HFGC Divertor tile (2014)
C1 - 15BNG6D – Dust 2010-2014
C2 – 14BWG6B – Dust 2010-2014
11 - SEM stubs
26 - SEM stubs

## Slide 14
Conclusions
Sectioning of Be tiles
Sectioning of selected lamella ILW-2 and ILW-3
SEM imaging of samples
Nano-indentation of Be tiles and W lamellae
TDS and full high temperature outgassing of samples from sectioned tiles.
Other capabilities
Surface tritium monitoring
Ar sputtered XPS measurements are available
Manufacture tritiated samples for calibration of T measurements and determine T content
Perform TDS with implanted calibration samples, with D, T, He, etc.
Analysis of dust composition by ICP-OES

## Slide 15: Analysis capabilities:
Glow Discharge Optical Emission Spectrometer (GDOES) able to perform depth profile analysis (29 elements +1). It is provided with a monochromator that can be set on a specific emission line (D, He, etc)
GDOES depth profile for a sample cored from marker tile exposed to WEST plasma (C3- 34il )
GDOES equipment
Illustration of GDOES profiles
SEM image of a cross section for Mo/W marker on FGG

## Slide 16: GDOES measurements:
GDOES depth profles for the samples cored from Tile 3 at s = 470 (a) and at s = 554 (b) after plasma exposure in ILW-3 campaign
GDOES depth profles for (witness sample) Tile 3 before plasma exposure in ILW1 campaign
SEM image of a cross section for Mo/W marker on CFC

## Slide 17: GDOES measurements:
GDOES sample measurement device (a) and cored FGG sample used for GDOES measurement (b)
GDOES sample cut
Requirements: samples = 7mm and h=10mm

## Slide 18: XRD measurements
XRD of a Be cut sample
X-ray diffraction (XRD) equipment. Used for :
- Phase analysis measurements
- Crystallite size measurements
- Quantitative phase analysis