## Slide 1: University of Latvia activities in 2022: Tritium and composition analysis of JET samples – plans and capabilities
WP PWIE SP E: Kick-off meeting
2nd March, 2022
E. Pajuste et al

## Slide 2: OUTLINE
Tritium analysis methods
  Dissolution/etching
  TDS
  Full combustion
Materials that can be analyzed
Additional analysis

## Slide 3: Different concepts of tritium measurements in plasma facing materials (available at UL)
Releasing tritium from the material
Getting tritium to the detector
Detecting tritium
Information obtained
Thermal
Non-thermal
TPD
Dissolution
Purge gas
Liquid
Proportional counter
(beta radiation)
Liquid scintillation
(beta radiation)
Total tritium content
Depth profile
Desorption spectra
Combustion

## Slide 4: Dissolution/etching method
Materials to be applied for: bulk metals, metallic coatings
Based on controlled dissolution/etching of metallic matrix and measurement of tritium being released
Plasma facing surface
Me+
T+,
HT, DT, T2
DTO, HTO
T0 interstitial
T+ chemically bonded to impurities
HT, DT or T2 in pores
Me
Me
Dissolution/etching
Purge gas
Tritium measurment in gasous phase (proportional gas flow detector)
Tritum measurement by the means of liquid scintillation
Tritium measurements based on its radioactivity
If dissolution/ etching rate is controlled - depth profile can be assessed of tritium released in the gas phase

## Slide 5: Thermal desorption
Plasma facing surface
T0 interstitial
T+ chemically bonded to impurities
HT, DT or T2 in pores
Me, CFC,
mixed
Materials to be applied for: all
Based on controlled thermal treatment and measurement of tritium being released as a result of diffusion
HTO,DTO,
HT, DT, T2
Heating
Rate ~5 K·min-1
Tmax ~1300K
Purge gas
Tritium measurement in gaseous phase (proportional gas flow detector)
Me, CFC,
mixed
Before monitor the zinc bed at ~400oC converts HTO/DTO to HT, DT, and traces of T2

## Slide 6: Full combustion
Materials to be applied for: all combustible
Based on full oxidation of material (destruction of the matrix) itself and and measurement of tritium being released
HTO,DTO,
HT, DT, T2
Heating in moistened air
~1100K
All tritium species are oxidized to water form
Plasma facing surface
T0 interstitial
T+ chemically bonded to impurities
HT, DT or T2 in pores
Me, CFC,
mixed
MeO , CO2,
Example of Be specimen
Measured by the means of liquid scintillation

## Slide 7: Combination of methods
Chemical dissolution
Electrochemical dissolution
Be
Inconel
First beryllium coating is dissolved and tritium measured (both in gas phase in a liquid). Process is followed by electrochemical etching - measurement of tritium in Inconel substrate.
Chemical dissolution
Electrochemical dissolution
Electrochemical dissolution
Full combustion
W
CFC
First tungsten coating is electrochemically etched and tritium measured (both in gas phase in a liquid). Process is followed by full combustion- measurement of tritium in CFC substrate.

## Slide 8: Comparison of methods
Characteristics | Chemical or electrochemcal etching | TDS | Full combustion
Information obtained | tritium total amount depth profile chemical state (To, TH, TD, T2 in gas phase, T+ - in liquid phase | Tritium total amount Desorption spectra | Tritium total amount
Tritium release method | Dissolution in 1M H2SO4 solution or electrochemical etching with simultaneous hydrogen measurement (by different aproaches) | Heating in a furnace, ~5oC/min up to 1030oC and held 1h at this temperature | Heating in a furnace in a moistened air, up to 1223K and held for 4-6 h at this temperature, HT and T2 oxidized in CuO furnace
Carrier gas | Argon, can be varied | Helium + 0,1% H2(must be dicussed) | Moistened air
Tritium measurement | Proportional counter – gas phase Liquid scintillation – liquid phase | Proportional counter | Liquid scintillation

## Slide 9: Materials to be analysed
Chemical/electrochemical etching - Be, W, Inconel + can be devloped for other metals
Combustion - all the materials that are combustible (carbon based, metals)
TDS - all solid materials
Combination of the methods - coatings, mixed materials

## Slide 10: Additional analysis to be performed
SEM, FT – IT, TG/TDA
Data analysis for evaluation of the factors influencing tritium retention in plasma facing materials using mathematical methods
Tritium behavior in non-exposed materials - sorption-desorption, permeation (both HT and HTO available)

## Slide 11: Thank you for your attention!
Asoc. prof. Dr. Elina Pajuste
Institute of Chemical Physics
University of Latvia
Jelgavas 1, Riga, Latvia
elina.pajuste@lu.lv

## Slide 12: Supplementary slides

## Slide 13: COMPARISON OF METHODS
Dissolution/etching
TDS
Full combustion
ADTVANTAGES
DISADTVANTAGES
Information on
  total tritium amount
  depth profile
  chemical state (can be adapted)
In layered materials information on tritium in each layer can be assessed
Fast
No elevated temperatures used (safe)
Information on
  total tritium amount
  Desorption spectra
Tritium trapping energies can be assessed
Applicable to all kinds of material
High sensitivity
Information on
  total tritium amount
Can be assumed that all tritium is measured since the «hosting matrix» is fully destroid.
Not all tritium might be measured if not sufficient layer thickness is etched (remains in bulk)
Some data might be lost if tritiated water vapor condensates before reaching the Zn bed
Time consuming
Limited information on tritium initial state in the material

## Slide 14: Dissolution method - beryllium
Be0 + 2H+ → Be 2+ + 2H0
H0 + H0 → H2 (gas ph.)
H0+T0 (solid phase) → HT (gas ph.)
T2 (solid ph.) → T2 (gas ph.)
T+(solid ph.) → T+ (liquid ph.)
Successive layers of Be are removed using 1 mol/L sulphuric acid and amount of evolved hydrogen (depicted as ‘H’) and released tritium (depicted as ‘T’) measured. Argon is used as a purge gas (~8 L/h).
T0(solid phase)- tritium atoms as interstitials in the bulk beryllium;
T2(solid phase)- molecular tritium trapped in the bulk beryllium;
T+(solid phase)- tritium chemically bonded with the impurities in the bulk beryllium;
T2(gas phase)- molecular tritium released in the flow of the purge gas;
T+(liquid phase)-tritium remaining in the acid solution as a part of the HTO+ ion;
Tritium in purge gas is measured by tritium monitor TEM 2100 with a proportional gas flow detector DDH 32 (counting gas - mixture of Ar and 10% methane)
Solution containing tritium is distilled and 5 or 1 mL (+4 mL deionized water) aliquot mixed with 15 mL of Ultima Gold scintillation cocktail and analysed for total tritium with a TRi-Carb 2910TR counter (PerkinElmer, Inc).

## Slide 15: Dissolution method - beryllium
Simultaneous etching of the metal surface and measurements of the released tritium in purge gas (proportional counter) and solution (liquid scintillation)

## Slide 16: Electrochemical dissolution method - tungsten, inconel
H0 + H0 → H2 (gas ph.)
H0+T0 (solid phase) → HT (gas ph.)
T2 (solid ph.) → T2 (gas ph.)
T+(solid ph.) +OH-→ HTO (liquid ph.)
H0 + H0 → H2 (gas ph.)
H0+T0 (solid phase) → HT (gas ph.)
T2 (solid ph.) → T2 (gas ph.)
T+(solid ph.) +OH-→ HTO (liquid ph.)
Successive layers of W are removed using electrochemically in 35% KOH solution where both electrods are tungsten, amount of evolved hydrogen (depicted as ‘H’) and released tritium (depicted as ‘T’) measured. Applied voltage ~3V. Argon is used as a purge gas (~8 L/h).
T0(solid phase)- tritium atoms as interstitials in the bulk tungsten;
T2(solid phase)- molecular tritium trapped in the bulk tungsten;
T+(solid phase)- tritium chemically bonded with the impurities in the bulk tungsten;
T2(gas phase)- molecular tritium released in the flow of the purge gas;
T+(liquid phase)-tritium remaining in the KOH solution as a part of the OT- or HTO molecule ion;
Tritium in purge gas is measured by tritium monitor TEM 2100 with a proportional gas flow detector DDH 32 (counting gas - mixture of Ar and 10% methane)
Solution containing tritium is distilled and 5 or 1 mL (+4 mL deionized water) aliquot mixed with 15 mL of Ultima Gold scintillation cocktail and analysed for total tritium with a TRi-Carb 2910TR counter (PerkinElmer, Inc).

## Slide 17: Dissolution method - tungsten
Simultaneous etching of the metal surface and measurements of the released tritium in purge gas (proportional counter) and solution (liquid scintillation)

## Slide 18: Experimental Setup
Beryllium – chemical etching
Tungsten, inconel – electrochemical etching

## Slide 19: Full combustion
Method is based on a full combustion of the sample in the moistened air.
Combustion conditions:
  Temperature: 850-870 °C,
  Flow rate of moistened air: 15-20 mL/min,
  Time of a complete combustion, 4-6 h.

## Slide 20: Thermal desorption
Purge gas He + 0.1% H2 at 14-15 L/h.
The quartz tube in the setup had two compartments – one for the sample in a quartz boat and one for a bed of granulated zinc.
The quartz cap had a thermocouple channel – an inner quartz tube sealed towards the sample.
The zinc bed at ~400oC converts tritiated water to molecular gaseous tritium (HT, DT, and traces of T2).
Heating rate 4.8 oC/min to 1030oC and then kept at that temperature for 1 h.
Temperatures of the sample, the zinc bed and the cold trap were continuously measured. The tritium activity in the purge gas was continuously monitored using a proportional counter with an operating volume of 300 cm3 and a tritium monitor TEM 2102A.
The total released tritium activity was calculated by integrating the release rate over the time where a release was measurable.

## Slide 21: Thermal desorption - experimental setup