## Slide 1
Plasma Wall Interaction and Exhaust
WP PWIE SP B: Meeting on results from WEST C3 marker PFUs
Broad-beam PIXE/NRA/RBS results - correspondence to MPG results (IST)
Rodrigo Mateus
Norberto Catarino
Rui Silva
Eduardo Alves 4 March 2022

## Slide 2: Laboratory layout
JET chamber - EBS, RBS, NRA, PIXE, from small samples to full tiles
RBS/C, ERD chamber - EBS, RBS, NRA, Be-based, W-based,
small samples, good adhesion
JET

## Slide 3: Experimental Setup
Experimental chamber
Detector geometry
JET line

## Slide 4: Experimental IBA conditions
Measurement positions in the samples
  4 points per core every 3.0-4.0 mm
  (deviated 2 mm from SIMS analysis at VTT).
  Spot size area ~ 1 mm2
IBA experimental conditions
  PIXE: 2300 keV proton beam detector at 150°
  EBS: 2300 keV proton beam detector at 150°
  NRA: 1000 keV and 2300 keV 3He beams detector at 135°
Available information
  D contents along depth ranges down to 3-4 mm in W-based coatings by NRA
  Contents of B and C co-deposits by NRA (2300 keV), if they are significant
  W contents above the Mo interlayer by EBS
  Amounts of minor contaminants by PIXE
  Evaluate the presence of other elements like O from elemental depth profiles by EBS

## Slide 5: Tiles for SEM and IBA analyses
6
Standard initially cooled W-coated graphite tiles
16 erosion marker tiles installed in WEST phase 1
2 retrieved after campaign C3
(D exposure only)
2 erosion marker tiles
and 1 standard tile after C4
(He phase at end of campaign)
M. Balden, WEST task force meeting
Inner tiles
baffles
EM: Erosion marker tiles
C1+C2+C3
C1+C2+C3+C4
q//
q//
ISP
OSP
Outer tiles
LFS
HFS
Photo after C3
s
0
0
s
04.03.2021
Tiles configuration at WEST
standard tile erosion marker tile
~100 nm Mo
~2-4 µm W
15 µm W
3 µm Mo
C
C
3 µm Mo
15 µm W

## Slide 6: Analysis of C3 marker tiles of WEST
C3-34iB
C3-34iK
C3-34iM
C3-22oE
C3-22oJ
Analysed points:
x - IBA / IST ; 0 - SIMS / VTT
As-prepared
Marker Tiles
C3-34i marker tile of WEST
x
x
x
thin deposition erosion strong erosion some deposition
x
x
C3-22o marker tile of WEST
thin deposition some deposition erosion

## Slide 7: Analysis of WEST samples by IBA
R. Mateus, E. Alves | WP PFC SP5 Kick-off meeting | 1 February 2019 | Page 7
C3-22oE
C3-34iK

## Slide 8: Analysis of WEST samples by IBA
Identification of particle yields in NRA spectra:
example of NRA spectra of point 8 (sample C3-32iK)
Used yields for elemental quantification (cross sections from IBANDL data base)
2H(3He,p0)4He [ W.Moller, F.Besenbacher, NIM 168 (1980) 11 ]
10B(3He,p1)12C [ J.R. Patterson et al., Proc. of the Physical Society 88 (1966) 641 ]
12C(3He,p0)14N [ G. Provatas et al., NIMB 500-501 (2021) 57 ]

## Slide 9: Analysis of WEST samples by IBA
co-deposition of O ?
11B(p,1)8Be  c.s.  60 mb/sr at 150º (IBANDL)
8Be  4He + 4He (complex analysis: use of standards or standard analysis ?)
agreement (IPP)
agreement (IPP)
slightly lower
W contents (IPP)
Mo layer partly on
the surface (IPP)

## Slide 10: Analysis of WEST samples by IBA

## Slide 11: Summary
Samples of the exposed C3-22o and C3-34i Marker Tiles of WEST
were analysed by IBA at IST (C3-22oJ, C3-22oE ,C3-34iB, C3-34iK, C3-34iM).
Low D contents behind the depth range achieved by NRA analysis (3 mm)
B quantification difficult by the low cross-sections of the 10B(3He,p)12C reaction
C co-deposited in superficial layers in C3-22oJ, C3-22oE, C3-34iB, C3-34iM
Thick co-deposition of B and C in C3-34iK
Mo quantification is hindered by the first W layer (roughness effect ?)
Cr and Fe were identified by PIXE as minor contaminants in all the samples
The experimental setup at IST enables the analysis of WEST samples by IBA