## Slide 1: WPSA – General meeting WPDIV JT60SA 04/05/22 M. Richou (marianne.richou@cea.fr)

## Slide 2: JT60SA - Operation phases
document BA SC 27-7.4 issue 07/21
Scope
Carbon
Tungsten

## Slide 3: WPDIV-JT60SA (Main objectives)
F4E has the responsibility to procure C actively cooled divertor target PFCs (C-ACD), to be operated around 2029 (-> Full divertor delivery in 2025)
For the C-ACD, the objective of WPDIVJT-60SA subproject consists in providing support to F4E to run the C-ACD series manufacturing (thermo-mechanical analysis, Electromagnetic loads analysis, mechanical testing, high heat flux tests)
A transition to a full metallic device is foreseen after 2033 for the “Integrated Research Phase II”. With this new phase, actively cooled tungsten (W) divertor target PFCs will have to be installed (W-ACD) (-> Full divertor delivery in 2031)
For the W-ACD, WPDIVJT-60SA subproject has the responsibility to design and develop the W-ACD by full scale prototype manufacturing and high-heat-flux testing.

## Slide 4
Source
40°C, 20 bar (inlet) 0.8 kg/s
Graphite
TZM
The JT60SA divertor (Integrated Phase 1)
For JT60SA, the divertor is composed of : cassette + plasma facing components

## Slide 5: Achievements 2021
Highlights for activities related to C-ACD:
  Under nominal heat flux of 10MW/m² some stress peaks have been identified, but further verification (w.r.t. brazing pre-stress + up to date material properties) shall be carried out
  Electromagnetic loads are not the limiting load cases
Graphite
TZM
(Tmax=800°C)
340 mm
Chart: 
| -1.4751999999999999E-2 | -1.2111E-2 | -9.4520000000000003E-3 | -6.7749999999999998E-3 | -4.0790000000000002E-3 | -1.3630000000000001E-3 | 1.928E-3 | 5.8079999999999998E-3 | 9.7409999999999997E-3 | 1.3742000000000001E-2 | 1.7824E-2 | 2.2002000000000001E-2 | 2.6294000000000001E-2 | 3.0714999999999999E-2 | 3.5284000000000003E-2 | 4.0018999999999999E-2 | 4.4941000000000002E-2 | 5.0071999999999998E-2 | 5.5435999999999999E-2 | 6.1057E-2 | 6.6964999999999997E-2 | 7.3190000000000005E-2 | 7.9765000000000003E-2 | 8.6730000000000002E-2 | 9.4128000000000003E-2 | 0.10202 | 0.11074000000000001 | 0.12064999999999999 | 0.13189000000000001 | 0.14463000000000001 | 0.15912999999999999 | 0.17574000000000001 | 0.19497 | 0.21768999999999999 | 0.24554000000000001
 | 247000 | 417000 | 529000 | 722000 | 911000 | 1280000 | 1840000 | 2890000 | 4800000 | 7010000 | 8980000 | 9730000 | 9280000 | 8440000 | 7360000 | 6340000 | 5420000 | 4600000 | 3930000 | 3340000 | 2890000 | 2510000 | 2190000 | 1910000 | 1640000 | 1370000 | 1160000 | 967000 | 816000 | 698000 | 574000 | 456000 | 344000 | 284000 | 227000
Heat FLux
10 MW/m²
Target length / m
1500°C

## Slide 6: Prospects 2022
With regard to the JT-60SA C-ACD, the objectives are to :
  Provide the data (mechanical, thermo-physical) on raw materials (materials delivered by F4E)
  Finalize the thermal design analysis (updated mechanical properties, thermo-mechanical history induced by the manufacturing process)
  Assess the performance by high heat flux tests of small-scale/prototypes (prototypes provided by F4E)
  Participate to dicussions for the design of C-ACD Langmuir Probes (WPSA collab.)
Graphite
TZM
Small-scale (4 tiles)
Graphite
TZM
Prototype full scale (12 tiles)
~100 mm

## Slide 7: W target ( Integrated Reasearch Phase II) - Technology
W monoblock
W Flat tile
12 mm
WEST curent configuration
CuCrZr

## Slide 8: W target - Time line
2023 | 2024 | 2025 | 2026 | 2027 | 2028 | 2029 | 2030 | 2031 | 2032 | 2033
End
of manufacturing
Plasma
Operation
2022 | 2023 | 2024 | 2025 | 2026 | 2027
Start of the manufacturing
FP9 2021-2025
Already proven technology
Thermal performance
Choice of concept and material

## Slide 9: W target - Time line and needs
FP9 2021-2025
Needed data from the modeling (WPSA):
Pumping efficiency (W vs Carbon) (2023) -> Needed for the definition of the target geometry
Assessment of the neutron activation (2023) -> Needed for the definition of the structural material
What is the surface shaping needed (2024) -> Needed for the choice of the armor material (machining tolerances) and for the final drawing
Steady state metallic plasma operation (WEST)
Feedback from W monoblock concept and surface shaping dimensions (WEST)
JT60SA:
First feedback from heat flux deposition, pumping (2025)
First feedback from long pulse operation in JT60SA (2026)
Start of the manufacturing

## Slide 10
WPDIV and WPDIV-JT60SA
WPDIV
W7X
JT60SA
IDTT
Eu-DEMO
R. Neu
M. Richou
R. Neu
M. Richou
J-H. You
Courtesy G.Federici, 2020
Fusion Science
Program manager

## Slide 11: Conclusions
For the C-ACD, the objective of WPDIVJT-60SA subproject consists in providing support to F4E to run the C-ACD series manufacturing (thermo-mechanical analysis, Electromagnetic loads analysis, mechanical testing, high heat flux tests)
For the W-ACD, WPDIVJT-60SA subproject has the responsibility to design and develop the W-ACD by full scale prototype manufacturing and high-heat-flux testing. For this, the first assumption, in order to save cost and R&D time, is to keep the same interfaces and boundary conditions as the ones taken for the design of C-ACD (heat flux, cooling capability, interfaces…), while developing PFC solution(s) compatible with an industrial fabrication
Close collaboration with WPSA to define our inputs

## Slide 13: W HHFT - Enhanced technology: W flat tile on CuCrZr heat sink
Standard cooling channel
Hypervapotron
Synergies with W7-X:
  Use of additive manufacturing for CuCrZr heat sink, especially for hypervapotron
  Suitability of W3.5Ni1.5Cu for divertor application (better manufacturability)
13