## Slide 1: VR contribution to PWIE SP-X
Per Petersson, Laura Dittrich, Sunwoo Moon, Marek Rubel, Daniel Primetzhofer

## Slide 2
ECWC, ICWC, and GDC plasma characterization / Pre- and post-characterization of samples used for cleaning and isotope exchange
Task Specification
Eurofusion PWIE SP-X

## Slide 3: Sample exposure 2022
New set of samples produced and pre-characterized by NRA and ToF-ERDA
Samples exposed in TOMAS 9-20 May
Investigation of effects of bias on the sample:

## Slide 4
Plasma characterization
Neutral particle analyser

## Slide 5: 2021-11 Exp. ToF-NPA
Total flux (1014 n0/cm2 s) | IC 0.25 kW | IC 0.5 kW | IC 1 kW | IC 1.5 kW
EC(2 kW) + IC | 5.44 | 9.38 | 23.33 | 38.29
IC only | 0.38 | 1.52 | 8.11 | 18.15
Neutral Particles Flux from Hydrogen EC+IC
Differential flux (n0 cm-2 s-1)
Neutral Particles Flux from Hydrogen IC
Differential flux (n0 cm-2 s-1)
Energy (eV)
Energy (eV)
Increase of power generates more neutral particle flux
The energy of neutral particles could be estimated by Maxwell-Boltzmann distribution fitting
  EC+IC is fitted to 50% of 15 eV and 50% of 35 eV
  IC only is fitted to 50% of 15 eV and 50% of 40 eV

## Slide 6: Summary
Starting to have a good set of data from both exposed samples and NPA
Should aim for putting it together
Also looking at other improvements and how it can impact, measurements
  Vacuum in NPA
  Different types of samples
  Methods of biasing the samples (pulsed DC)
Proposal with Tom Wauters for similar investigations in EAST

## Slide 7
Thank you!