## Slide 1: SP-X.2: Optimization of laser-based surface analysis diagnostics
Peeter Paris, Indrek Jõgi
University of Tartu

## Slide 2: Tasks and deliverables 2021-2022
1. Comparison of ps vs. ns LIBS regarding absolute composition and D content in reference and ITER-relevant coatings which can include impurities
2. (CF-) LIBS (ns SP) on samples from different devices
  Studies with 3 WEST C3 samples outside from the regions of strong erosion and deposition
Chart: LIBS shot nr.
Chart: LIBS shot nr.
Chart: LIBS shot nr.
Chart: LIBS shot nr.
C3-22oL
C3-34iP
C3-34iA
Chart: LIBS shot nr.
Chart: LIBS shot nr.
  2022: depends on the plans of other groups (comparison of results)

## Slide 3: Tasks and deliverables 2021-2022
3. (CF-)LIBS on Be containing coatings with different type of fuel content (+He)
Chart: Shot nr.
 | 911.9544 | 146.0153 | 127.62 | 117.392 | 131.1274 | 143.6433 | 101.4322 | 112.952 | 106.928 | 130.5633 | 138.0753 | 124.2671 | 157.9434 | 148.6904 | 133.4478 | 127.3145 | 146.2193 | 141.4439 | 101.5981 | 113.8181 | 160.5152 | 89.0468 | 117.2903 | 121.4009 | 76.7963 | 84.969 | 86.4045 | 73.2638 | 83.4344 | 86.9667 | 72.5799 | 62.9142 | 43.1794 | 42.3177 | 50.6462 | 42.6357 | 42.5461 | 54.4441 | 48.0694 | 53.0828 | 43.1072 | 45.3919 | 42.8472 | 46.37 | 26.8453 | 34.902 | 27.3205 | 49.861 | 31.4569 | 41.4018 | 36.0821 | 17.9084 | 34.9931 | 18.6391 | 30.6126 | 30.94 | 32.5727 | 21.3651 | 14.7403 | 17.5006
ne=7.1·1015 cm-3
Te=0.98 eV
Be-5%He-5%D
Chart: Wavelength (nm)
Chart: Wavelength (nm)
Chart: LIBS shot nr.
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10
B | 11634.5981 | 5288.7584 | 3262.4121 | 2394.7516 | 1806.9841 | 2518.8657 | 2137.0617 | 1396.6955 | 1301.0482 | 1492.8492
O | 12630.0687 | 1643.1744 | 903.3371 | 1233.0094 | 1001.8411 | 983.1484 | 885.5804 | 879.3862 | 735.2719 | 410.8668
D | 550.1805 | 182.5458 | 136.9193 | 79.4486 | 79.7642 | 78.4947 | 65.4307 | 74.5482 | 72.0796 | 51.2041
Chart: LIBS shot nr.
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10
B | 21699.7825 | 6523.7804 | 3173.1701 | 2872.9616 | 1905.6746 | 1927.1471 | 1540.0249 | 2653.5385 | 2245.6269 | 529.3425
O | 21287.4703 | 1165.0569 | 1110.6805 | 649.8591 | 1007.5124 | 921.6098 | 274.9938 | 536.689 | 666.9949 | 639.1857
D | 3918.1972 | 142.3562 | 17.3455 | 26.1468 | 57.6546 | 35.8804 | 1.6928 | 36.2983 | 67.0505 | 41.0874
Chart: LIBS shot nr.
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10
B | 7696.2477 | 2425.5596 | 899.5589 | 1311.9974 | 745.1609 | 981.4727 | 1092.5539 | 487.0649 | 1096.4695 | 80.9621
O | 9406.5389 | 1031.0605 | 883.2196 | 531.9695 | 1234.3484 | 710.7392 | 984.9901 | 948.4966 | 742.2389 | 1114.0288
D | 531.088 | 101.7749 | 98.8533 | 74.4769 | 60.3615 | 48.5136 | 30.9108 | 39.7377 | 64.6913 | 28.3727
C3-22oL
C3-34iP
C3-34iA
2. (CF-) LIBS (ns SP) on samples from different devices
  2022: similar measurements with WEST samples after C4 and publication
  2022: Data analysis and publication (JET, BeO etc.)

## Slide 4: Tasks and deliverables 2021-2022
4. CF-LIBS on produced reference samples before and after He loading
  He detectable near the target surface at relatively short delay time (100-200 ns) in Ar at 1-2 Torr
He signal strongest at 1-2 Torr Ar pressure
He signal stronger near the target
Chart: Shot nr.
 | 410.3578 | 2739.722 | 3636.9068 | 1893.9462 | 3080.9402 | 2393.1649 | 1713.4843 | 1760.1645 | 3281.9544 | 2291.2709 | 1208.447 | 2600.667 | 2371.3971 | 2460.5115 | 1307.1635 | 2041.6775 | 1353.2352 | 2234.581 | 588.8825 | 1855.6519 | 2247.8011 | 1926.8354 | 348.5471 | 1347.8284 | 1155.8604 | 762.8231 | -216.5843 | 1513.5907 | 1410.2433 | 636.9633 | -341.2171 | 903.4615 | -410.3846 | -298.9335 | 393.3744 | -89.0119 | -1455.4414 | -31.8331 | 19.1047 | 318.7989
 | 8662.7161 | 2685.8088 | 296.578 | 1234.0274 | 1860.397 | 316.2253 | 317.3324 | 815.1021 | 138.348 | 1684.2708 | 358.9947 | 750.0325 | -135.7107 | 1551.4173 | 1737.4918 | 1969.9751 | 1061.2077 | 2187.1829 | 2370.6341 | 1716.3889 | 2275.074 | 4420.1337 | 3676.8912 | 5112.7028 | 5848.3177 | 6895.4911 | 6880.6762 | 5766.1446 | 6145.386 | 6223.6431 | 5947.3724 | 7394.8955 | 6662.6136 | 4632.71 | 4721.149 | 5183.5743 | 5587.8863 | 7394.6182 | 4432.1185 | 5923.9886
 | 693.6024 | 11241.4072 | 9795.2586 | 8951.63 | 10489.082 | 11870.4897 | 10824.4341 | 9018.2178 | 9693.8904 | 9272.706 | 10168.5218 | 6756.2037 | 10288.0888 | 7236.2758 | 8263.3062 | 8106.7494 | 8392.684 | 6544.7206 | 7990.8317 | 8523.181 | 7994.0755 | 7612.6531 | 6723.5759 | 6885.4014 | 9452.2867 | 6981.4617 | 8008.7319 | 5423.3014 | 4598.192 | 6501.997 | 5830.0541 | 4289.5435 | 6146.8664 | 4753.2462 | 7322.4765 | 6289.0343 | 4921.5342 | 4480.8726 | 5074.2297 | 3843.0275
Chart: Pressure (Torr)
| 0.5 | 1 | 2 | 12 | 30
 | 4369.2952 | 8045.7357 | 14887.2013 | 3794.6283 | 1339.2755
ns-LIBS in Argon:
7 ns, 60 mJ
delay time 200ns
Chart: Distance from target (mm)
| 0 | 1 | 2 | 3 | 4.5
 | 15088.5102 | 20527.1227 | 11936.6778 | 5245.4689 | 1446.7807
Spectrum around He 587.56 nm
Depth profile of He, W and Mo
laser
target
Chart: Wavelength (nm)
He signal missing in undoped W coating
signal recorded perpendicularly to laser beam
IU-555
6 µm W (5% He) coating on Mo
  2022: Data analysis (also Be samples) and publication

## Slide 5: Tasks and deliverables 2021-2022
5. Investigate erosion/deposition/fuel retention (including He) by in situ (CF)-LIBS and NRA/RBS in MAGNUM with subjects of interest: outgassing, recycling, and role of impurities (O, N), Tsurface, and implantation energy on retention
  Raman spectra for W-O detection
0
3
6
9 mm
-3
-6
Chart: Position (mm)
| 0 | 3 | 6 | 9 | -6 | -9
LIBS | 5.0593 | 6.9639 | 2.8086 | 6.5587 | 4.5546 | 4.0874
NRA | 0.8 | 1.1 | 1.5 | 3 | 2.5 | 2.5
Comparison of LIBS and NRA
Chart: Wavenumber (cm-1)
W=O
  p-W-O exposed to D2-7%N2 at 380°C
Chart: Shot nr.
 | 92.8039 | 48.224 | 35.5763 | 128.2916 | 91.2858 | 35.9382 | 8.138 | 10.174 | -3.3613 | 5.7251 | -2.0101 | 11.7261 | -2.2238 | -11.6279 | 5.6601 | 0.32759 | -11.3801 | -7.8827 | -1.6109 | -0.61004 | -23.0207 | 4.4336 | -6.9011 | 6.2157 | 0.19252 | -1.9662 | -13.3593 | -11.8612 | -5.5747 | -4.5164 | -12.1752 | -11.9637 | -5.1881 | -16.8629 | -9.6762 | -7.7345 | -11.734 | -13.2402 | -7.6761 | -3.752
 | 52.6638 | -65.217 | -51.5432 | 69.7093 | 107.3947 | 101.5581 | 177.1456 | 239.3187 | 209.0969 | 247.7864 | 205.6631 | 240.8542 | 233.559 | 216.0493 | 248.1121 | 234.9847 | 246.7573 | 240.267 | 216.4315 | 222.2165 | 270.9856 | 243.6954 | 236.8801 | 232.9127 | 232.7501 | 218.4667 | 257.1415 | 256.839 | 220.7915 | 261.7774 | 236.3813 | 196.8642 | 260.1041 | 201.3347 | 258.2468 | 213.9438 | 245.5013 | 261.8854 | 216.1193 | 218.0271
 | 251.5692 | 110.6727 | 83.6578 | 45.0698 | 38.5992 | -17.069 | 38.511 | -4.4363 | 86.7807 | 40.1018 | 67.2325 | 120.1356 | 105.2166 | 64.4002 | 109.9649 | 94.7571 | 106.6625 | 99.9699 | 108.931 | 108.6467 | 119.1586 | 92.2966 | 103.8644 | 86.2327 | 123.5056 | 124.1806 | 98.8023 | 112.8809 | 118.8957 | 168.9317 | 130.9048 | 71.435 | 164.3244 | 99.1139 | 91.7813 | 100.6677 | 107.1872 | 118.3012 | 110.4435 | 98.4537
Chart: Depth in TFU (1015 at/cm2)
| 0 | 1200 | 1200 | 5600 | 5600
 | 1.5 | 1.5 | 0.3 | 0.3 | 0
 | 0 | 0 | 0 | 0 | 0 | 0 | 100 | 100
 | 55.3 | 55.3 | 47.3 | 47.3 | 100 | 100 | 0
 | 43.2 | 43.2 | 52.4 | 52.4 | 0 | 0
LIBS Depth profile
  2022: Data analysis and publication