## Slide 1: WP PWIE SP X2 Kick-off meeting May 25 2022
G. Sergienko, E. Wüst, R. Yi
FZJ

## Slide 2: FZJ tasks for 2022
Investigate erosion/deposition/fuel retention (including He) by in situ (CF)-LIBS and NRA/RBS in MAGNUM, LIBS, LAMIS, and LIA-QMS/EDX in PSI-2 with subjects of interest: outgassing, recycling, and role of impurities (O, N), Tsurface, and implantation energy on retention (DIFFER, FZJ, UT), LAMIS qualification for W7-X application (FZJ)
Comparison ps vs. ns LIBS regarding absolute composition and D content in reference and ITER-relevant coatings which can include impurities (FZJ, CU, UT, ISSPUL, CEA)
Comparison Single Pulse vs. Double Pulse LIBS (or alternative LIBS signal enhancement methods) regarding absolute material composition and D content in ITER- and DEMO-relevant W including self-damage W and reference coatings. (FZJ, ENEA, CEA)
(CF-) LIBS (ps, ns SP or DP) on samples (if available) from different devices (tokamaks or W-7X) (collab. SP B) (ISSP UL, CU, UT, VTT, FZJ, ENEA)
CF-LIBS on produced reference samples before and after He loading (FZJ, CU, UT, ENEA)

## Slide 3: Outgoing activity
ns-laser (Innolas) has been repaired and reinstall on PSI-2 laser lab but need modification of solenoid control valve for cooling water.
New vacuum chamber for LIBS is under installation in the PSI-2 laser lab.
Optical setup for ns-LIBS in air was installed in the beam line of PSI-2 LIBS system.
New high repetition ps-laser YLPP-25-3-50-R (1030nm, 50kHz-2MHz, pulse duration 2 ps, pulse energy < 35J) from IPG photonics was installed in LIBS lab. First measurements were performed.
2D-scanner for IPG laser is under installation and will be ready at June for LIBS measurements in air
Double-Pulse Laser ablation molecular isotopic spectroscopy (LAMIS) of W-7X divertor fingers

## Slide 4: Preparation of ns-LIBS on PSI-2
near field
far field
Laser was repaired and re-adjusted but has problem with a solenoid control valve (it make very loud noise due to hydraulic shocks).The problem is under investigation.
SpitLight2000 laser
Focusing lens
Observation mirror optics
Sample XY holder
c
ns-LIBS in air
Vacuum chamber
The camera will be combined with McPherson 225 / McPherson 235 spectrometers and will utilize Innolas SpitLight2000 Nd:YAG laser
a
b

## Slide 5: Preparation of high repetition ps-LIBS in LIBS lab
High repetition ps-laser YLPP-25-3-50-R
Beam expander x10
2-Axis Galvo Scan Head INNOSCAN2-20D-1064
F-Theta lens f=500mm D20mm SH-1064-360-500-20-FS
E1803D All-In-One Scanner Controller (HALaser Systems)
2-Axis Galvo Scan Head
INNOSCAN2-20D-1064
F-Theta lens f=500mm D20mm
SH-1064-360-500-20-FS
ps-laser model YLPP-25-3-50-R
=1030nm
=2ps
f=50kHz-2MHz
E=25-35J
Innotech Laser GmbH
IPG photonics

## Slide 6: Initial test of fast scanning ps-LIBS
exposure time 200ms (104 laser pulses)
Fe
Al
W
Compact spectrometer measurement
Mechelle5000
Fe
Cu
Scan 1
100 μm
32.3 m
45.1 m
Scan 10
Ablation crater’s diameter ~ 30 - 50 μm
Ablation rate ~ 11.25 nm/pulse
Spectrometer
ps-laser
Beam expander
XYZ stage
F=80 mm
Laser energy：31 μJ Laser frequency：50k Hz
Scanning system

## Slide 7: Double-Pulse Laser ablation molecular isotopic spectroscopy (LAMIS)
Double-Pulse Laser ablation molecular isotopic spectroscopy (LAMIS) was set up (ps-laser)
TDU from end of OP1.2b are being analysed for carbon 13 distribution after injection of isotopically marked gas into plasma
First results from divertor finger near injection show same qualitative characteristics as results from nuclear reaction analysis (NRA) of same finger
Further divertor fingers are being analysed; including the one right next to the injection
Simulation of gas injection with ERO2.0 will be compared with these measurements
C2 molecule Swan bands with ∆v=1. Relative intensities give 84% fraction of 13C
12C2
13C12C
13C2
LAMIS results of near injection (d~223 mm) vs. NRA results of same divertor finger. LAMIS data set shows 13C fraction in topmost 400 nm