## Slide 1: Powder metallurgy produced tungsten fiber reinforced Tungsten (Wf/W)
2022.08.11 I Yiran Mao, Jan Coenen, Alexis Terra, Rui Shu, Xiaoyue Tan, Chao Liu, Johann Riesch, Yucheng Wu, Christoph Broeckmann and Christian Linsmeier

## Slide 2
Crack formation for tungsten armor
Intrinsic brittleness of tungsten material
Thermal heat load at the divertor: thermal stress and thermal fatigue
G. Pintsuk et al. / Fusion Engineering and Design 88 (2013) 1858– 1861 1861
Neutron embrittlement
A damage resilient material is required
H Bolt, et al; Journal of Nuclear Materials, Volumes 307–311, Part 1, 2002, Pages 43-52
Accumulated equivalent plastic strain field in the tungsten armor block after the 5th HHF load cycle at 20 MW/m2.
-M.Li 2015.

## Slide 3: Solution: Tungsten fiber reinforced tungsten composites
Pseudo ductile behavior
Tungsten fiber-reinforced tungsten (Wf/W)

## Slide 4: Porous matrix composites
It is the same principle like weak interface composite
Examples:
SiC/SiC
CFC
“a controlled amount of fine scale matrix porosity, obviating the need for a fiber coating.
This approach can be viewed as an extension of the porous coating concept wherein crack deflection occurs because of the low fracture toughness of the porous interphase.”
Matrix Cracking
Crack Front Debonding
Interface debonding
Fiber pull-out
a

## Slide 5: Production upscaling
Sample with a dimension of 105 mm x 30(25) mm has been produced
Large scale FAST/SPS facility in HFUT, sample geometry up to 300 mm in diameter
Large Scale PM Wf/W

## Slide 6: Application projects
Wf/W Application in foundry industry
Melt guiding part
Mechanical tests with different size up to 84 mm x 20mm x 10 mm
Component design, Wf/W joint with steel via V
20 mm to 105 mm in diameter
Wf/W joint with Copper
Cu infiltration into the porous matrix
Wf/W monoblocks, 28x12x23 mm
Flat tiles design with Wf/W
Up to 23x28x8 mm

## Slide 7: Long fiber Wf/W
Production
Tungsten Weaves laser cutting and coating
Alternate placement of W weaves and W powders in the graphite tool of SPS
Spark Plasma Sintering (SPS)
Wf/W with long aligned fibers

## Slide 8: Long fiber Wf/W
Microstructure
200 µm
50 µm
Interface impacted by SPS process but remain intact
Fiber arrangement may need to be improved

## Slide 9: Long fiber Wf/W
Mechanical properties
Long fiber Wf/W show more promising mechanical properties compared to short fiber Wf/W
Samples | Fracture energy density (kJ/m2) | Fracture toughness, Kq(MPa m0.5) | Flexural strength (MPa)
Pure tungsten | 0.1±0.0 | 5.5±0.0 | 381±46
Wf/W | 1.9±0,7 | 25.5±7.8 | 221±17
Porous matrix Wf/W | 3.3±1.0 | 21±7.1 | 235±10
Long fiber Wf/W | 11.6±3.1 | 67.6±15.0 | 495±78

## Slide 10: Long fiber Wf/W
Thermal shock
Fiber vertical to the loading surface
Fiber parallel to the loading surface
Loading condition
Labs = 0.38 GW/m2, Tbase = RT, n = 100 pulses
After the loading: crack bridging by the fibers

## Slide 11: Development outlook
-From several kilograms to hundred kilograms
105 mm x 30 mm, 4.5 kg
Typical samples
105 mm x 10-30 mm, 1.5-4.5 kg
Typical samples
1-3mm
105 mm
3mm
105 mm

## Slide 12: Wf/W
For Flat Tile Applications incl. Joining
Vanadium as stress relieving interlayer
Wf/W- 5 mm
V - 0.3 mm
316L - 5 mm
parameters | 
Temperature | 850°C
Pressure | 30MPa
Holding time | 15min
Heating rate | 25 K/min
Cooling rate | 5 K/min
Test of Residual stresses and stress during quenching – utilize steel to maximze stresse
Heated to 1000°C
Quenched at 4°C

## Slide 13: Mock Ups for Gladis Testing
Material produced and Cut – joining underway
Joining at FZJ
Joining at ENEA

## Slide 14: Operational Window
Crack resistance at low temperatures
High strength at elevated temperatures and high heatfluxes
Of Wf/W
Tokamak Energie Ltd: Cyclic testing at minimum 10 MWm-2 up to 1000 cycles, 60s on/off.
Based on: Zinkle, S. J. & Busby, J. T. Structural materials for fission amp; fusion energy Materials Today , 2009, 12, 12-19

## Slide 15: Finding an Application of the Material
For a Composite Material a dedicated wayof solving problems or adding operational space can be found
E.g allow operating Wf/W above 1500 ºC
Stable properties during irradiation
No need for monoblock – joining Wf/W & Wf/Cu
Tungsten Flat-Tile
W
RAFM
CuCrZr or
novel Cu alloy
W/Cu FGM or WfCu
Cooling water: 150 ℃, 16m/s, 5 MPa
20 MW/m2 Tmax：1060℃
G.N.Luo ( ICFRM 2019)

## Slide 16: Advanced Concepts
What goes beyond what exists
Wf/W
CVI produced Wf/W with infiltrated copper Coolant (missing proof of principle)
Wf/W
Complet Wf/W based component CVI / PM
With 3D weaves – needs development
Wf/W
Utilizing µ-structure tungsten as armour
Wf/W pure W

## Slide 17: Thermal conductivity