## Slide 1: PWIE-SP A.3.T – plans for 2022 Performance of advanced materials under high heat loads and their microstructural characterization & Effect of hydrogen on the strength of W wire
J. Riesch*,a, Y. Maob,c, A. Laub, A. Feichmayera,e B. Böswirtha, S. Elgetia, H. Greunera, T. Höschena, J.W. Coenenb,d, and R. Neua,e
aMax-Planck-Institut für Plasmaphysik, 85748 Garching, Germany
bForschungszentrum Jülich GmbH, Institut für Energie- und Klimaforschung – Plasmaphysik, 52425 Jülich, Germany
cSchool of Mechanical Engineering, Hefei University of Technology, Hefei 230009, China
dDepartment of Engineering Physics, University of Wisconsin - Madison, Madison, WI53706, USA
eTechnische Universität München, 85748 Garching, Germany
Notes: 20 min + 3 min Diskussion

## Slide 2: PWIE-SP A.3.T – plans for 2022
Performance of advanced materials under high heat loads and their microstructural characterization
  Use high heat flux facility GLADIS at IPP, Garching
  Test advanced W composite based mock-ups until its limits
  Microstructural evaluation by light and electron microscopy
Effect of hydrogen on the strength of W wire
  Use in-situ testing device GIRAFFE at IPP, Garching
  Use keV H/D beam to load very thin W wire
  Evaluate change of stress state due to uptake of H/D
Garching LArge DIvertor Sample test facility [Greuner et al. J NUCL MATER 367-370,(2007) 1444-1448]
Rotary stage
Load cell
Sample
Rotary stage
Linear actuator
Heating / Cooling
General-purpose irradiated fiber and foil experiment

## Slide 3: High heat flux tests – new mock-ups
Mono-Block concept according to WPDIV
  Manufacturing within WPMAT in collaboration with ENEA
  Aim: direct comparison to conventionsl W materials
  Status: blocks cut, manufacturing of mock-up on- going
Large scale flat-tile mock-ups
  Aim: investigate the effect of size on the performance of Wf/W composite mock-ups  does the composite concept allow for larger flat tile sizes?
  Status: tiles cut and soldered, final machining of mock-ups on-going, pre-characterization planned in September, first tests planned in October

## Slide 4: Effect of hydrogen on strength
Plasma source installed at GIRAFFE and tested
  ECR ion gun (Tectra Gen II)
    energy range of 25 eV – 5 KeV, total beam current of 1mA (at 5 kV)
    e.g. 1x1018 D ions / m2s at 300 eV
  Hardware adoptions in progress
    guiding pipe, beam sensors, …
First tests planned for October
  Stress relaxation by D
    load sample to dedicated load and hold it there
    load sample with D beam and monitor load
  Midterm: investigate synergies between D effect and irradiation damage
Rotary stage
Load cell
Sample
Rotary stage
Linear actuator
Heating / Cooling
Giraffe (General-purpose irradiated fiber and foil experiment)