## Slide 1: PWIE-SP A.A4.T-T002 – D001 Assessment of hydrogen impact on material properties linked to ITER relevant PFUs
M. Richou
29th of August 2022 – WPPWIE SPA meeting

## Slide 2
Assessment of hydrogen impact on material properties linked to ITER relevant PFUs
M. Richou1, M. Lemetais2, Q. Tichit1, Y. Corre1, G. Kermouche2 and the WEST team
SPA - Midterm -29th August 2022
2
1

## Slide 3
Use of WEST to assess and model tokamak plasma impact on recrystallization and softening
Assess: what are the properties we plan to investigate ?
  Loss of mechanical properties -> Hardness measurements
  Modification of the microstructure -> EBSD measurements
For what modelization ?
  Impact on recrystallization and softening kinetics.
Global strategy
In this presentation :
1. Studied tungsten – implementation in WEST
2. WEST campaigns (Heat flux and cumulative pulse duration, misalignment)
First measurements on one WEST PFU
3. Samples with well-known plasma (D, He) loading (used for the input needed for the modeling)

## Slide 4: 1. Studied tungsten – implementation in WEST
Incident flux
CuOFHC
CuCrZr
Tungsten and component manufactured by AT&M/ASIPP
ITER-like Geometry:
  6mm W thickness
  Block width from 26.3 mm to 31.8 mm
  AT&M rolled W (ITER W grade material)
A-A
500 mm

## Slide 5: 2. WEST campaigns
 | Duration max (s) | Cumul (s) | LH max (MW) | W LH total (MJ) | Max heat flux - Qn (MW/m²)
C4 – D2 | 55 (USN) | 9678 | 5.4 | 7823 | <6 [J.Gaspar, Nuclear Fusion, 2021]
July-Nov19 |  |  |  |  | 
C4 - He | 30 | 2991 | 4.5 | 4300 | 
Oct-Nov19 |  |  |  |  | 
C5 | 23 | 4630 | 5.4 | 2625 | 6 [J. Bucalossi, Nuclear Fusion, 2022]
Nov20-Jan21 |  |  |  |  | 
5
C4 : 14 ITER like PFU
C5 : 2 full sectors

## Slide 6: 2.1 Misalignement in WEST
C5
α (3.1°)
A misalignement (or exposed edges) leads to expose the leading edge with huge heat flux
(If Qn = 5.2 MW/m² - > Qs ~ 100 MW/m² !!!)
 In WEST, some PFUs are misaligned on purpose (during C4: up to 0.5 mm)
δ
δ
14 PFUs
δ = 0.5 mm
δ = 0.4 mm
C4
WEAN004, post C5

## Slide 7: 2.2 High surface loading in WEST (2/2)
Qn
T=1500°C (Sharp, δ =0.3 mm)
T=1500°C (Sharp, δ =0.6 mm)
From embedded measurments
δ
Qn = 6 MW/m²
Sharp
ANSYS simulations
J.Bucalossi et al., nuclear fusion, 2022
Temperature Max. / °C

## Slide 8
2.3 Combinaison of heat flux and misalignement
The PFU 8 is of interest (δ ~ 0.4 mm ) (may have reached 1500°C during the C4 campaign)
But…is it recristallised (it is a question of time…) ?
OSP
ISP
-> Focus on the OSP LE region
100 %
50 %
OSP
Highest heat flux zone
8
PFUs
Normalised heat flux
Notes: NB PFU 13^peut être un candidat (WECN001)

## Slide 9: 2.4 Loading time
Y. Corre, submitted
M. Richou, Nuclear Materials, 2020
For a leading edge surface temperature of 1500°C, annealed during 300s, hardness is decreased by a half (Alfonso etal.).
Future steps : Check the annealed time and Qn on PFU 8, monoblocks 23-27
Monoblock 24
26

## Slide 10: 2.5 Visual observation of the relevant PFU
M. Diez, 2021, Nuclear Fusion
δ = 0.4 mm
Presence of cracks, deposits on the zone dedicated to the hardness measurment
Hardness measurments are not relevant on the full not polished PFU
Future step : polish, use of sample rather than a complete PFU
Plasma loaded surface
Notes: Discrimner transient et SS WERI002 Mono 20 TE

## Slide 11: 3. Reference samples to check the potential mean field model on well known loaded samples (Collab Rasinsky)
Sample 0: Reference sample without any RXX or plasma loading
Sample 1 : Only D plasma (7-8 1021 D/m².s)
Sample 2.1 to 2.3 : D plasma annealing (7-8 1021 D/m².s) inducing recrystallisation
Exposed at 1350 °C for 1h, 2h and 5h respectivelly
Sample 3 : Only He plasma (8-9 1021 He.m².s) Exposed at 1100°C for 1h (recrystallisation not reached).

## Slide 12: Conclusions and prospects
Experimental (mainly hardness measurements):
  Perform the hardness measurements on the WEST PFUs
  Perform the nanoindentation/EBSD measurements on WEST PFU samples (samples provided by SP.B3)
Model:
  Define the influence of microstructure (due to manufacturing processes) on recrystallization/restoration using mean field model
  According to hardness measurements, propose parameters to be implemented in mean field model to take into account plasma loading
Link with the WEST plasma operation (needed for correlation of experimental and modelisation):
  Assess the temperature and fluence reached during plasma operation (C4 and C5 WEST campaigns) for the analyzed PFUs
From January meeting (Jan presentation)

Under progress
Identification of the most relevant PFU first
 (poster at SOFT)
Some characterizations are planned first (2023)
Not relevant