## Slide 1: Update on PIM studies
14th October 2022 I M. Wirtz et al.
Forschungszentrum Jülich GmbH, Institut für Energie- und Klimaforschung, 52425 Jülich, Germany

## Slide 2: Environmental conditions
plasma exposure
neutrons
very high thermal loads
Steady state heat loads:
up to 20 MWm-2 in ITER (lower loads in DEMO)
recrystallization
failure of joints
Transient thermal loads:
up to 60 MJm-2
(disrupt., ELMs, VDEs)
crackings
melting
dust formation
Plasma loads:
sputtering
hydrogen
helium
Neutrons:
up to 14 MeV
defects
transmutation

## Slide 3: Reference material
Plansee pure tungsten according to ITER specifications (‟IGP-W”)
Top view, ~10 µm
Side view, 5 × 25 µm²
50 µm
12 × 12 × 5 mm³
longitudinal
transversal
recrystallized
1600 °C, 1 hour

## Slide 4: Sample material
Powder injection molding
Time & cost effective near-net-shape forming process with shape complexity and high final density
Courtesy of S. Antusch, KIT
Mass production of near-net-shape parts
Create new materials/investigation of properties
Brittle to ductile transition for pure PIM W at 200 °C (low strain rates)
No porosities or cracks, high density (better than 99 % t.d.)
No recrystallization – possible grain growth at very high temperatures only
Fully isotropic material properties

## Slide 5: Sample material
Powder injection molding
Time & cost effective near-net-shape forming process with shape complexity and high final density
  Based on low and high pulse number pure heat load tests performed in WPMAT-HHFM the following PIM alloys were chosen for synergistic tests:
          W-1TiC
          W-2Y2O3
          W-3Re1TiC
          W-3Re2Y2O3
          W-1HfC
          W-2Y2O31TiC
A: 10 mm; B: 2 mm; C: 3 mm; D: 1 mm

## Slide 6: Linear plasma device PSI-2
Target Positions
Plasma Source
Target Exchange &
Analysis Chamber
Linear Manipulator
Nd:YAG Laser
Steady-state
D, He, Ar plasma
plasma column diameter 60 mm
ion flux ≤ 1023 m-2s-1
incident ion energy (bias) 10 – 300 eV
ELM-like heat pulse
Nd:YAG laser wavelength 1064 nm
laser energy 32 J

## Slide 7: PSI-2 conditions for all experiments
absorbed power density 0.41 GW/m²
base temperature of approximately 1000 °C
pulse duration 0.5 ms; repetition rate 10 Hz; 105 pulses
Deuterium / Helium (6 %) plasma
particle energy 35 eV
flux ~ 4 x 1021 m-2s-1; fluence ~ 4 x 1025 m-2

## Slide 8: IGP-WT, High pulse number tests
transversal
SEM images
Metalographic cross section
FIB cut

## Slide 9: PIM samples, High pulse number tests
W-1TiC
W-2Y2O3
W-3Re1TiC
W-3Re2Y2O3
W-1HfC
W-2Y2O31TiC
IGP-WT
SEM images

## Slide 10: PIM samples, post mortem analysis
FIB cuts and bubble formation
Roughening
Bubble size and density is comparable/very similar for all tested materials. Exemplarily shown for W-1TiC and IGP-WT.
reference for IGP-W ~ 19 µm
IGP-WT
W-1TiC
W-2Y2O3 and W-3Re1TiC show a factor of 4 to 5 higher surface roughness than the other three PIM alloys. However, all samples have a much lower surface roughness than the IGP-W reference material.

## Slide 11: Next steps, summary and conclusions
Preparation of metallographic cross sections in order to investigate the crack propagation into the material
PIM-W alloys show comparable or better fatigue performance to the as-received pure tungsten grade in terms of damage category and crack formation
more detailed investigations of the induced damages indicate that especially surface modifications like roughening due to plastic deformation and the particle induced nanostructures are less severe/pronounced
PIM-W alloys represent a very promising alternative material to commercially available pure tungsten grades. The fatigue performance could be even further improved by an optimization of the microstructure via the manufacturing process parameters, i.e. used powders and thermal treatments.