## Slide 1
Assessment of hydrogen impact on material properties linked to ITER relevant PFUs
M. Richou1, M. Lemetais2, Q. Tichit1, Y. Corre1, L. Gallais3, G. Kermouche2 and the WEST team
WPPWIE - SPA – Review meeting – 14th of October 2022

## Slide 2: The strategy
WEST: Thermal field+D+He (Combined effect)
Testing
Modelisation
H
He
Characterization
(EBSD,indentation, nano-indentation)
  For T < 1350°C : conventional set-ups
  For T > 1350°C : conventional set-ups are limited (ampoules operational temperature, low heating speed 5°C/min [1]
PSI2 [2]…
West plasma conditions
Thermal field (WPMAT)
Isothermal, anisothermal
[1] M. Minissale et al., 2020
[2] A. Pospieszczyk et al. 2013
  5 mm
WPPWIE

## Slide 3: Recovery and recrystallization
ta: Annealing time
X=0
X=1 (fully recrystallized)
Tungsten maintained at Ta (annealing temperature)
Temperature and time dependent process
Hardness  (Xh= 1 fully softened)
Dislocation
Grain boundary
Sub grain boundary
New grain
Notes: During primary recrystallization, the new grains grow at the expanse of the strain hardened microstructure (removal of dislocations), the driving force being the stored energy associated to dislocations and sub-grain boundaries.
Recovery summarizes all thermally activated mechanisms by which dislocations annihilate and rearrange themselves into more stable configurations. Dislocation density
Recrystallization is a thermally activated process by which strain-free regions (nuclei) are generated and grow into it.

## Slide 4: MODELIZATION
What modelization ? Assess the Impact of recrystallization and softening
[3] A. Durif et al., 20202
[4] M. Lemetais et al., 2022 (to be submitted)

## Slide 5
Studied tungsten in WEST
WEST campaigns
Visual observation of relevant PFUs

## Slide 6: 1. Studied tungsten – implementation in WEST
CuOFHC
CuCrZr
Tungsten and component manufactured by AT&M/ASIPP
ITER-like Geometry:
  6mm W thickness
  Block width from 26.3 mm to 31.8 mm
  AT&M rolled W (ITER W grade material)
A-A
500 mm
Chamfer

## Slide 7: 2. WEST campaigns
 | Duration max (s) | Cumul (s) | LH max (MW) | W LH total (MJ) | Max heat flux - Qn (MW/m²)
C4 – D2 | 55 (USN) | 9678 | 5.4 | 7823 | <6*
July-Nov19 |  |  |  |  | 
C4 - He | 30 | 2991 | 4.5 | 4300 | 
Oct-Nov19 |  |  |  |  | 
C5 | 23 | 4630 | 5.4 | 2625 | 6*
Nov20-Jan21 |  |  |  |  | 
C4 : 14 ITER like PFU
C5 : 2 full sectors
*[J. Bucalossi, Nuclear Fusion, 2022]

## Slide 8: 2.1 Misalignment in WEST
C5
α (3.1°)
A misalignement (or exposed edges) leads to expose the leading edge with huge heat flux
(If Qn = 5.2 MW/m² - > Qs ~ 100 MW/m² *!!!)
 In WEST, some PFUs are misaligned on purpose (during C4: up to 0.5 mm)
δ
δ
14 PFUs
δ = 0.5 mm
δ = 0.4 mm
C4
WEAN004, post C5
2.3 mm
(δ+groove on purpose)
* [Y Corre et al 2021 Phys. Scr. 96 124057]
Notes: Y Corre et al 2021 Phys. Scr. 96 124057.
Dans un deuxième temps nous avons amélioré les analyses et les simulations, tu peux indiquer que si on prend les processus d’émission thermoionique et un flux plus piqué (lq=3mm), on trouve 150.MW.m2, S. Ratynskaia et al. PSI2022, submitted. A savoir que pour cette expérience nous avons un écart entre mesures standard et mesure avec caméra IR VHR, on trouve des flux plus piqué avec la caméra VHR donc plus d’intensité, c’est juste pour info

## Slide 9: 2.2 High surface loading in WEST (2/2)
Qn
T=1500°C (Sharp, δ =0.3 mm)
T=1500°C (Sharp, δ =0.6 mm)
From embedded measurments
J.Bucalossi et al., nuclear fusion, 2022

## Slide 10
2.3 Combinaison of heat flux and misalignement
The PFU 8 is of interest (δ ~ 0.4 mm ) (may have reached 1500°C during the C4 campaign)
But…is it recristallised (it is a question of time…) ?
 Focus on the OSP LE region
OSP
Highest heat flux zone
8
PFUs
19
OSP
ISP
100 %
50 %
Normalised heat flux
1
38
δ
Notes: NB PFU 13^peut être un candidat (WECN001)

## Slide 11: 2.4 Loading time
M. Richou, Nuclear Materials, 2020
Future steps : Check the annealed time and Qn on PFU 8 and 19, monoblocks 23-27
 At 1500°C, > 300 s are needed to reach a decrease by a half of hardness

## Slide 12: 3. Visual observations of the relevant PFU
[M. Diez, 2021, Nuclear Fusion]
δ = 0.4 mm
 Presence of cracks, deposits on the zone dedicated to the hardness measurment
 Hardness measurments are not relevant on the full not polished PFU
 Future step : polish, use of sample rather than a complete PFU
Plasma loaded surface
Notes: Discrimner transient et SS WERI002 Mono 20 TE

## Slide 13: Conclusions and prospects
 | WEST | Thermal field (isothermal) | Thermal field (anisothermal) WPMAT | H | He
Testing |  |  |  |  | 
Testing condition assessment | 2023 |  |  |  | 
Characterization | 2023 |  |  Analysis 2023 |  Dislocation density beg. 2023 | 
Modelisation |  |  Upgrade may be needed |  |  |