## Slide 1
Christian Cupak, Paul Szabo, Martina Fellinger, Johannes Brötzner, Alexander Redl, Friedrich Aumayr
cupak@iap.tuwien.ac.at
WP PWIE 2022 Review Meeting
+ 2023 Planning Meeting
Sputtering of rough and nanostructured W samples
Diploma Thesis
Fusion@ÖAW Vienna, Austria
This work has been carried out within the framework of the EUROfusion Consortium, funded by the European Union via the Euratom Research and Training Programme (Grant Agreement No 101052200 — EUROfusion). Views and opinions expressed are however those of the author(s) only and do not necessarily reflect those of the European Union or the European Commission. Neither the European Union nor the European Commission can be held responsible for them.
Notes: Thank you very much for the warm introduction!
First of all I‘d like to thank the organisers of this conference to give me the opportunity to present the results of my research, focusing on the effect of surface roughness on sputtering, here at the ICACS conference.

## Slide 2
Outline
Diploma Thesis
Fusion@ÖAW Vienna, Austria
Acknowledgements
Special thanks to colleagues and research partners!
H. Biber, P.S. Szabo, M. Fellinger, J. Brötzner, A. Redl, F. Aumayr
E. Pitthan, M.V. Moro, D. Primetzhofer
A. Lopez-Cazalilla, F. Granberg, K. Nordlund
R. González-Arrabal
Notes: In addition, I would like to thank my colleages at TU Wien, and also our international research partners,
from Germany to Sweden
to Spain, and also to Finland.
We appreciate your support and look forward to our future collaborations.

## Slide 3
Sputter theory, simulations → for flat surfaces
Real surfaces not flat → surface roughness
Relevant for nuclear fusion, space weathering, coating techniques,…
Outline
Diploma Thesis
Fusion@ÖAW Vienna, Austria
Introduction
Notes: In my talk, I will focus in detail on the contribution of surface roughness on the sputtering of materials under ion bombardment.
Generally, sputtering theory and many numerical simulation codes show good agreement to experiments with perfectly flat surfaces, and this is established since years.
However, real surfaces are rarely flat, but have a certain surface roughness which can change sputtering yields severely.
This is an ongoing topic of investigation, especially in the field of Plasma Wall interaction for nuclear fusion reactors, which is my background.
In addition, this is also of relevance in example for space weathering, where the rough surface of celestial bodies is exposed to solar wind ions
Furthermore, this is also relevant for industrial coating techniques like physical vapour deposition, where a crucible may develop a surface roughness.
Therefore, our desire was to find a robust roughness parameter, which enables to predict the effects on the sputter yields.

## Slide 4
Local incident angles
Redeposition
Shadowing
Secondary sputtering
Outline
Diploma Thesis
Fusion@ÖAW Vienna, Austria
Roughness effects on Sputtering
most experiments modify surface
3D BCA codes often limited by topography input size
M. Küstner et al., Nucl. Inst. Meth. Sec. B, 145, 1998, https://doi.org/10.1016/S0168-583X(98)00399-1
Notes: At first, I would like to talk a little more about the individual roughness effects that can occur during ion bombardment.
In example, the local inclination of a surface feature can affect the actual ion incidence angle, which alters the local sputter yield and reflection coefficients.
Also, redeposition of sputtered atoms on neighbouring surface features can severely reduce the total sputter yield
Shadowing of certain surface areas can also occur, especially under grazing ion incidence.
Finally, secondary sputtering may also contribute to the total erosion, if reflected ions hit the surface again.
These individual effects are hard to investigate, especially since most ion beam experiments would modify the surface dynamically.

## Slide 5
Experimental method QCM (SP-B)
SPRAY simulation code (synergy with SP-D)
Sputtering of classic rough surfaces
Sputtering of oriented rough surfaces
Outline
Diploma Thesis
Fusion@ÖAW Vienna, Austria
Outline
Notes: These conditions motivated us to investigate this field more, both experimentally and numerically, which can be seen here in the outline:
One the one hand, we used a so-called QCM to experimenteally investigate the connection between surface roughness and the total sputter yield, with a special focus on static sputter yields, or in other words: when the surface is not yet altered due to the ion beam.
Furthermore, we developed a new raytracing simulation code which allows any larger surface sections as input, enabling to study the roughness effect for a liberal choice of topographies.
With both approaches, we then worked on the key goal, which is to identify a good roughness parameter, allowing to characterise rough surfaces to even enable predictions of total sputter yields.

## Slide 6
At TU WIEN:
QCM = Quartz Crystal Microbalance
Specialised electronics + SC-cut quartz [1]
≈ 90 pg/cm²/s (3 ⋅ 10-4 W monolayers/s)
Low ion fluxes for minimal surface alteration
Classic Target QCM: ions cause mass reduction
Catcher QCM: deposited atoms cause mass increase
[1] G. Hayderer et al., Rev. Sci. Instrum. 70 (1999), https://doi.org/10.1063/1.1149979
Outline
Diploma Thesis
Fusion@ÖAW Vienna, Austria
Experimental Approach: QCM
A = ion beam
B = sputtered atoms C = reflected ions
D = QCM
Notes: At our institute, measuring with a QCM has a long history. Specialised electronics and resonators allow very high sensitivity for our QCM. In example, it is possible to achieve a mass change sensitivity of 10 to the power of -4 tungsten monolayers per second.
Due to this high sensitivity, we were able to use very small ion fluxes for our experiments on the rough surfaces, which therefore allowed to neglect surface alteration. This is very important, since dynamic changes of the rough surface would limit conclusions in the context of this project.
The classic QCM configuration can be seen here: The quartz is directly bombarded by ions which cause a mass loss.
In addition, we developed a cacher QCM configuration, where the quartz is used to probe the angular distribution around the target.
If you are more interested in this method, stay tuned for Friedrich Aumayr‘s talk on Thursday.

## Slide 7
  Our in-house developed code SPRAY
Outline
Diploma Thesis
Fusion@ÖAW Vienna, Austria
Simulation of rough surface sputtering
SPRAY = SPuttering simulation via RAYtracing of particles
Flat surface repository data from BCA codes
(sputter yields, emission vectors)
2) Topography input (limitless) e.g., by AFM
3) Raytracing loop
4) No cluster necessary
Raytracing
BCA
Roughness effects
  Cupak et al., Appl. Surf. Sci. 570, 2021, https://doi.org/10.1016/j.apsusc.2021.151204
Notes: At next, I introduce you to our numerical method used: The raytracing code SPRAY.
SPRAY stands for SPuttering simulation via RAYtracing of particles.
Here, a repository data set from earlier conducted BCA code simulations is used (for instance from SDTRimSP). The repository is obtained for a perfectly flat surface of given composition.
Afterwards, a topography input of liberal size, like from AFM, is loaded to the code
Then, the raytracing algorithm projects the repository data to the neighbourhood around each individual ion impact.
The code is parallelised, runs under Python 3 and can be executed on desktop PCs without need for cluster infrastructure.
Also, all former mentioned surface roughness effects like Changes of local ion incidence angle, shadowing, redeposition or secondary sputtering are included.

## Slide 8
Recap: Which roughness parameter for predicting sputter yields of rough surfaces?
RMS
RMS:
No consistent trend
RMS not reliable
Outline
Diploma Thesis
Fusion@ÖAW Vienna, Austria
Characterisation of roughness for sputtering
SPRAY sweep: many surface inputs with rising roughness
(2keV Ar+ on W, 0° and 60°)
Characterise roughness by root mean square (RMS) → common in science and technology
  Cupak et al., Appl. Surf. Sci. 570, 2021, https://doi.org/10.1016/j.apsusc.2021.151204
Notes: The large stack of images was first characterised by RMS and then piped into the SPRAY code for a sweep. Here you can see results again for 2keV Ar irradiation, under 0 and 60 deg incidence angle. The roughness of the surfaces was characterised first by the root mean square roughness, which is commonly used in science and technology
As you can see, no consistent trend was found. The individual data stacks did show independend behaviour. Furthermore, the same RMS value can lead to completely different sputter yields. Therefore, we found the RMS parameter not to be reliable.

## Slide 9
Which one is the mountain landscape, which one the AFM image?
Outline
Diploma Thesis
Fusion@ÖAW Vienna, Austria
Characterisation of roughness for sputtering
Notes: With this in mind, I would like to discuss this also from an alternative point of view.
When I was hiking in the mountains, I often observed the similarities which you can see from AFM images of rough surfaces and alpine views. Therefore I would like you to ask the question, which sketch resembles a mountain image, and which one the AFM image…?
I give you some seconds to make a personal judgement before I solve this small riddle…

## Slide 10
AFM image rough W surface RMS = 420 nm
Dachstein, Austria, 31.12.2021 RMS = several 100 m
x 109
scale-independent parameter desired
Outline
Diploma Thesis
Fusion@ÖAW Vienna, Austria
Characterisation of roughness for sputtering
Notes: So, here is the answer!
The left side shows an AFM image of a rough tungsten surface with about 420nm root mean square roughness.
The right hand side shows many mountains around the Dachstein in Austria– I guess the RMS would be in the range of some 100 meters.
There is a scale difference of 10 to the power of 9, while the appearance is very similar.
But why do I tell you this. I think this also motivates a scale-independent parameter to describe sputtering of rough surfaces, since sputtering is a very small scale atomistic process. I think, it can be assumed that as long as the collision cascade in the target material is substantially smaller than the expansion of the mountains on a rough surface, the actual scale becomes unimportant, limiting therefore parameters like root mean square roughness.

## Slide 11
Scale-independent parameter:
Mean inclination angle δm
Calculation:
Quantitative surface data (AFM,...)
Calculate local surface normal vectors
→ surface triangulation
Project towards global surface normal
Histogram → mean value
Rule-of-thumb values:
smooth δm < 10°
moderately rough 10° < δm < 35°
very rough 35° < δm
Outline
Diploma Thesis
Fusion@ÖAW Vienna, Austria
Characterisation of roughness for sputtering
  Cupak et al., Appl. Surf. Sci. 570, 2021, https://doi.org/10.1016/j.apsusc.2021.151204
Notes: Therefore, I‘d like to introduce you to an alternative metric, the mean inclination angle delta m.
This can be interpreted as a mean tilt of all surface features, therefore a scale independent representative.
It can be calculated relatively simple:
At first, quantitative data like from AFM is needed,
Then, all local surface normal vectors are needed. Our option to achieve this was to create a mesh from the AFM data, and perform a triangulation of the data.
All surface vectors from the triangles can then be projected towards the global surface normal, which enables to plot the angles as a histogram.
Finally, just the mean angle is required, which can characterise the surface roughness.
Just as a rule of thumb: delta values below 10 are still representing very smooth surfaces.
Up to 35°, I‘d interpret them as moderately rough, while beyond, the surfaces start to appear more spiky.

## Slide 12
Recap: Which roughness parameter is good to predict sputter yields of conventional rough surfaces?
RMS
δm
RMS:
No consistent trend
RMS not reliable
δm
Common trends found
0°: δm acts like increase of ion incidence angle
60°: linear fit found
Outline
Diploma Thesis
Fusion@ÖAW Vienna, Austria
Characterisation of roughness for sputtering
[1] Cupak et al., Appl. Surf. Sci. 570, 2021, https://doi.org/10.1016/j.apsusc.2021.151204
[2] Szabo et al., Surf. Interfaces 30, 2022, https://doi.org/10.1016/j.surfin.2022.101924
Analytical Model (2022)
Notes: We then used this delta parameter to characterise the large stack of surfaces used for SPRAY simulations, and suddenly, we obtained much better trends!
For instance under 60° degree incidence, we see a common linear decrease for all images.
Under normal incidence, we even see a slight increase of the sputtering yield up to moderate roughness of about 20°.
This is explained by the dependence of the yield on incidence angle, as known for flat surfaces, while redeposition is not yet strong enough to be effective.
This changes for rougher surfaces dramatically.
Generally, we concluded that indeed the delta m parameter is a good metric for rough surface sputtering.

## Slide 13
How about sputtering of oriented structures?
Outline
Diploma Thesis
Fusion@ÖAW Vienna, Austria

## Slide 14
Comparative study with SPRAY and QCM: Nano-columnar W (NCW)
Outline
Diploma Thesis
Fusion@ÖAW Vienna, Austria
Nano-columnar W surface sputtering
SEM original
AFM
SEM imitation
NCW on QCM -> sputtering measurements
50 nm diameter, 500 nm high NCs, areal density 58%
AFM: quantitiative input to SPRAY, limited by tip size
Artificial topography created for SPRAY (SEM imitation)
PVD on QCM resonator by R. González-Arrabal (UPM)
A. Lopez-Cazalilla & C. Cupak et al., Phys. Rev. Mater. 6, 2022, https://doi.org/10.1103/PhysRevMaterials.6.075402

## Slide 15
Selected results:
1keV Ar + under various incidence angles
Outline
Diploma Thesis
Fusion@ÖAW Vienna, Austria
Nano-columnar W surface sputtering
Sputter yield in very good agreement between QCM and SPRAY (for SEM imitating input)
AFM tip convolution led to underestimation of redeposition in channels
Sputter yield generally reduced by NCW
Almost no dependence on incidence angle
Favourable for a first wall material
A. Lopez-Cazalilla & C. Cupak et al., Phys. Rev. Mater. 6, 2022, https://doi.org/10.1103/PhysRevMaterials.6.075402

## Slide 16
Outline
Diploma Thesis
Fusion@ÖAW Vienna, Austria
Nano-columnar W surface sputtering
Sputter yield generally reduced by NCW
Almost no dependence on incidence angle
Comparative study between QCM experiments, SPRAY and MD simulations (Univ. Helsinki, A. Lopez-Cazalilla)
Very good agreement, despite different scales in geometry for MD
Publication in Phys. Rev. Mater. (2022)
A. Lopez-Cazalilla & C. Cupak et al., Phys. Rev. Mater. 6, 2022, https://doi.org/10.1103/PhysRevMaterials.6.075402
1keV Ar +
2keV Ar +
50x downscaled NCW for MD
Original scale for SPRAY

## Slide 17
Outline
Diploma Thesis
Fusion@ÖAW Vienna, Austria
Nano-columnar W surface sputtering
Same NCW under D irradiation
Eventually transmission effects?
Sputter yield again reduced
Good agreement SPRAY and SDTrimSP-3D
No transmission of D expected
Experiments: different trend at 10-8 mbar
At 10-9 mbar: good agreement (adsorbates)
MD simulations soon (Univ. Helsinki)
1keV D+ under various incidence angles

## Slide 18
Outline
Diploma Thesis
Fusion@ÖAW Vienna, Austria
Summary
[1] Szabo et al., Surf. Interfaces 30, 2022, https://doi.org/10.1016/j.surfin.2022.101924
[2] A. Lopez-Cazalilla & C. Cupak et al., Phys. Rev. Mater. 6, 2022, https://doi.org/10.1103/PhysRevMaterials.6.075402
δm
RMS
Analytical model: Sputtering of rough W [1]
Sputtering of nano-columnar W [2]

## Slide 19
Outline
Diploma Thesis
Fusion@ÖAW Vienna, Austria
Outlook for future studies in SP-B (& SP-D)
Nano-columnar tungsten (NCW):
  Optimise shape of NCs to minimise sputter yields (height, areal density,…) with SPRAY
  Deploy optimised NCW as a real sample on QCM
  QCM experiments + simulations (static behaviour)
  Study dynamic erosion of NCW both experimentally and numerically
Pyramidal W samples (see A. Uccello‘s talk):
  Cooperation ongoing
  Continue experimental investigations with QCM methods (Catcher-QCM etc…)
  Support with numerical simulations
Of course, we are open for your suggestions!

## Slide 20: Backup slides

## Slide 21
Outline
Diploma Thesis
Fusion@ÖAW Vienna, Austria
Sputtering of redeposited W
2keV Ar+ irradiation
2keV D2+ irradiation
original W sample:
redeposited W sample:

## Slide 22
angular distribution of sputtered particles from pure W and redeposited W:
original W sample:
redeposited W sample:
Outline
Diploma Thesis
Fusion@ÖAW Vienna, Austria
Sputtering of redeposited W

## Slide 23
2keV Ar+ irradiation
2keV D2+ irradiation
original W sample:
redeposited W sample:
Outline
Diploma Thesis
Fusion@ÖAW Vienna, Austria
Sputtering of redeposited W

## Slide 24
Outline
Diploma Thesis
Fusion@ÖAW Vienna, Austria
Simulation of rough surface sputtering
SPRAY simulation raytracing workflow
Ion randomly hits surface → local impact angle → BCA repository
Sputtered atoms emitted → redeposition
Reflected ions emitted → secondary impacts
Secondary sputtering
Output:
Effective sputter yields
Emission distribution of sputtered particles / refl. ions
Quick simulations, sweep studies possible (multiple images)
  Cupak et al., Appl. Surf. Sci. 570, 2021
Notes: To give a better overview, you can see here the principal workflow of the code. At first, an ion hits the surface on randomly selected impact points.
The local impact angle determines the BCA repository data (on sputter yields or emission vectors) for the further nested loops.
Next, trajectories of sputtered atoms are launched from the primary impact site, while the raytracing algorithm evaluates if an atom leaves the surface (and is therefore sputtered) or otherwise hits the surface again, and therefore is redeposited.
Similar is done for the reflected ions, while the focus is here mostly on the identification of secondary impact sites.
These are then relevant for considering secondary sputtering effects in the last nested loop.
This is done for a large number of ions to gain sufficient statistics of a surface, which then results in effective sputtering yields for large – scale images,
Also the emission distribution for sputtered atoms or reflected ions can be exported.
In contrast to other established codes, SPRAY has also the big advantage to allow quick simulations. It even allows sweep studies, like for instance for continuously rising incidence angles, or alternatively, for sequentially simulating sputtering of a stack of different images.
It must be mentioned that the code so far only includes static operation.

## Slide 25
QCM experiments vs. SPRAY Microscopy images of rough W samples:
4 AFM images
QCM sample
Outline
Diploma Thesis
Fusion@ÖAW Vienna, Austria
Benchmark with rough W samples
smooth
  Cupak et al., Appl. Surf. Sci. 570, 2021
QCM sample
medium rough
5 CFM images
5 CFM images
not QCM sample
very rough
Notes: The QCM was then used to make a benchmark study for the code.
In the experiments, tungsten was selected as target material, since it is a prominent material used in nuclear fusion devices. Both tungsten coated quartz crystal samples and bulk tungsten targets with variable roughness were used.
Both AFM and confocal microscopy was used to investigate these samples, while the latter technique was used especially for the rougher ones.
Here, i shortly want to show you some selected images of the sample surfaces.
Sample 1 was the smoothest one and had RMS roughness values on the nm scale. This sample was only investigated with AFM, since CFM could not resolve the mirror-like surface.
Sample 2 could be probed with both microscopes. At first, the AFM image is shown. The RMS roughness was about 34 nm. It has to be mentioned, that in total 15 AFM images were used to determine these parameters for better statistics.
The CFM image of the same sample 2 interestingly had a much higher RMS value of 187nm. It can be assumed that the much larger lateral size of these image included also surface peaks, which were not captured before by AFM. However, a clear lack of resolution was observed.
Finally, the roughest sample 3 is shown here, which had RMS on the micrometer scale.

## Slide 26
Benchmark of SPRAY with Samples S1, S2, S3; 2keV Ar+ under φ = 60°
1) Angular emission distribution: Catcher QCM vs. SPRAY
Outline
Diploma Thesis
Fusion@ÖAW Vienna, Austria
Benchmark with rough W samples
  Cupak et al., Appl. Surf. Sci. 570, 2021
Single knock-on peak
smooth
S1
Roughness reduces emission
Microscopy resolution important
med. rough
S2
High roughness → collimation effect
S3
very rough
2) Target sputter yields
S1, S2 direct sputter yields (QCM crystals)
S3 estimated sputter yields
High resolution of microscope important
Good agreement QCM / SPRAY
smooth
med. rough
very rough
Notes: The results of the benchmark can be seen here
First, the angular distribution under 2keV Ar bombardement with 60° incidence is inspected. The smoothest sample 1 shows good agreement of catcher QCM measured data with the simulated emission distribution.
The medium rough sample 2 shows a reduced emission, both for simulated and experimental data. It is important to mention, that we found better agreement for the AFM simulated cases, which is expected, since the confocal microscopy images did show a lack of resolution, causing an overestimated emission.
The third sample consistently showed the most reduced emission, and a collimation effect towards the surface normal.
In addition, also the target sputtering yields are compared. Since the roughest sample 3 was not a quartz crystal, we used the emission profile to estimate the target sputter yield here, while the other samples allowed a direct evaluation. In this table, you can see the good agreement between SPRAY and QCM for all surfaces, while image resolution remained important.

## Slide 27
Benchmark of SPRAY with Samples S1, S2
Angular sweep of target sputter yield
Even nm-scale roughness (S1) changes yield
QCM results well reproduced by SPRAY
SPRAY good basis for large numerical study:
1) nm- to µm roughness
2) Artificially smoothed/roughened images (S2-s, S3-s)
Sputter yield vs. ion incidence angle φ
scaling s
s = 0.2
s = 1 (original)
Outline
Diploma Thesis
Fusion@ÖAW Vienna, Austria
Benchmark with rough W samples
  Cupak et al., Appl. Surf. Sci. 570, 2021
Notes: We then used the samples to conduct a parameter sweep study by changing the global ion incidence angle for a final benchmark.
As you can see, the data are in good agreement as well. Interestingly, we could identify that even the nanometre scale roughness of sample 1 had an effect under grazing ion incidence, compared to a purely flat plane surface.
Based on the benchmark, we then prepared for a larger numerical study. We aimed to sweep roughness from nanometre to microns regime, by applying a scaling factor to microscopy images which I’ve shown you before.
Also, a completely artificial surface was chosen, obtained from a gaussian height values generator
For example, when the scaling factor is 1, we receive the original surface, but if it higher or as here, lower, the surface is smoothed.

## Slide 28
  Which roughness parameter is good to predict effective sputter yields? -> mean inclination angle δm
Double sweep: roughness + ion incidence angle
δm : global fit function → prediction
Outline
Diploma Thesis
Fusion@ÖAW Vienna, Austria
Characterisation of roughness for sputtering
  Cupak et al., Appl. Surf. Sci. 570, 2021
δm
RMS
Notes: We then extended this study also towards another dimension.
To fully investigate the trends, we included variable ion incidence angles to the sweep and the results show, overall, a much more consistent trend with the delta m parameter.
This even allowed to deduce an empiric fit formula, which enables to predict sputter yields of a rough surface with a given roughness parameter delta m.
It has to be mentioned, that this primarily holds for conventional, isotropically rough surfaces
For those of you who are more interested, I suggest to take a look on our recent paper in applied surface science.
I also want to draw attention that our empirical experiences were recently supported by an analytical concept established by my colleague Paul Szabo.
He linked the delta m parameter to the ratio of root mean square roughness over autocorrelation length.
With this, I come to the end of my talk. If any questions arised, I‘d be happy to answer them now. Thank you for your attention!

## Slide 29
[1] Cupak et al., Appl. Surf. Sci. 570, 2021, https://doi.org/10.1016/j.apsusc.2021.151204
[2] Szabo et al., Surf. Interfaces 30, 2022, https://doi.org/10.1016/j.surfin.2022.101924
QCM + SPRAY → roughness effects on sputtering
δm better parameter than RMS
Isotropic, conventionally rough surfaces
Empirical study (QCM + SPRAY) → Applied Surface Science [1]
Analytical concept (Szabo et al.) → Surfaces and Interfaces [2]
Outline
Diploma Thesis
Fusion@ÖAW Vienna, Austria
Summary
SPRAY
QCM
Sputter yield vs. δm
Notes: We then extended this study also towards another dimension.
To fully investigate the trends, we included variable ion incidence angles to the sweep and the results show, overall, a much more consistent trend with the delta m parameter.
This even allowed to deduce an empiric fit formula, which enables to predict sputter yields of a rough surface with a given roughness parameter delta m.
It has to be mentioned, that this primarily holds for conventional, isotropically rough surfaces
Also, this is only the static picture. Dynamic erosion of rough surfaces is a different topic.
For those of you who are more interested, I suggest to take a look on our recent paper in applied surface science.
I also want to draw attention that our empirical experiences were recently supported by an analytical concept established by my colleague Paul Szabo.
He linked the delta m parameter to the ratio of root mean square roughness over autocorrelation length.
With this, I come to the end of my talk. If any questions arised, I‘d be happy to answer them now. Thank you for your attention!

## Slide 30
QCM = Quartz Crystal Microbalance
Sauerbrey equation [1]
Thin layer on top (e.g., W) -> ion beam experiments
SiO2
Au
Au
e.g., W
[1] G. Sauerbrey, Z. Physik 155 (1959), 206-222
Outline
Diploma Thesis
Fusion@ÖAW Vienna, Austria
Experimental Approach: QCM
Notes: In this context, I will shortly present our experimental approach: The QCM. QCM stands for quartz crystal microbalance. The fundamental basis of this technique is a thin quartz crystal with 2 gold electrodes on each side, forming a piezoelectric resonator.
When this quartz is provided with an alternating current with corresponding eigen-frequency, the quartz performs shear vibrations due to the piezoelectric effect.
With the sauerbrey equation, a direct connection between this resonance frequency and the mass of the quartz can be drawn. In other words, small mass changes can be determined by recording the change of this resonance frequency.
It is very useful for us, that this method is still working if a thin layer of different material, like Tungsten, is applied on the quartz, which is, in our experiments, exposed to an ion beam for erosion studies.
At our institute, measuring with a QCM has a long history. Specialised electronics and resonators allow very high sensitivity for our QCM. In example, it is possible to achieve a mass change sensitivity of 10 to the power of -4 tungsten monolayers per second.
Due to this high sensitivity, we were able to use very small ion fluxes for our experiments on the rough surfaces, which therefore allowed to neglect surface alteration. This is very important, since dynamic changes of the rough surface would limit conclusions in the context of this project.
The classic QCM configuration can be seen here: The quartz is directly bombarded by ions which cause a mass loss.
In addition, we developed a cacher QCM configuration, where the quartz is used to probe the angular distribution around the target.
My mentor Friedrich Aumayr will provide a more detailed overview to the QCM in his talk on Thursday.

## Slide 31
QCM electronics -> regulation loop to drive quartz in resonance
Resonance frequency changes due to mass loss in experiments
≈ 90 [pg/s] ≈ 3⋅10-4 [W monolayers/s]
Sensitivity:
[G. Hayderer et al., Rev. Sci. Instrum., 70 (1999) 3696-3700.]
[K. Dobes, PhD thesis, TU Wien (2014)]
Motivation
Diploma Thesis
QCM electronics

## Slide 32
Beam on
FC cup measurement before and after experiment
Initial Ar cleaning of target + catcher, pre-coating procedure
For ref Q: both target and catcher frequency signal
For other targets: only catcher frequency
Via ion current and frequency -> sputter / catcher yield
[6]
[6] Sauerbrey G., 1959 (https://doi.org/10.1007/BF01337937)
Target QCM
Catcher QCM (always)
Off-sputtered W atoms per incoming ion
adsorbed W atoms on catcher per incoming ion on the target
Motivation
Diploma Thesis
Catcher-QCM procedure

## Slide 33
[1] U. v. Toussaint et al., Phys. Scr. T170 (2017), 014056
[2] W. Möller, Nucl. Instrum. Methods Phys. Res. B. 322 (2014), 23-33
[3] R. Stadlmayr et al., J. Nucl. Mater. 532 (2020), 152019
Outline
Diploma Thesis
Fusion@ÖAW Vienna, Austria
Roughness effects on Sputtering
Established 3D BCA codes: SDTrimSP-3D [1] or TRI3DYN [2] simulate 3D structures like W-fuzz [3]
limited lateral size of surface (but becomes better)
computational cluster needed
60°
Ar+
Notes: In contrast, established 3D BCA codes like SDtrimSP-3D or TRI3DYN are great tools to simulate even complex 3D structures like Tungsten-fuzz.
However, these codes are rather limited to relatively small lateral surface sections and usually require a cluster infrastructure, still demanding long computational time.

## Slide 34
3D BCA Monte Carlo Code
BCA = Binary collision approximation -> collision cascades do not overlap
Static or dynamic
Input: 3D surface from AFM (limited to 200x200x200 voxel), target composition
Output: target sputter yields, list files with trajectories of sputtered atoms/reflected ions etc…
[7]
[7] Möller W., 2014 (http://dx.doi.org/10.1016/j.nimb.2013.12.027)
Output
Motivation
Diploma Thesis
TRI3DYN
AFM
Input

## Slide 35
Raytracing Code
Static simulations, multicomponent targets possible, liberal surface structures
Input: 3D surface from AFM or CFM (no limit), target composition, sputter yields for BCA codes for flat surface
Output: target sputter yields, list files with trajectories of sputtered atoms/reflected ions etc…
Output
Motivation
Diploma Thesis
SPRAY
AFM
Input
Sputter yields

## Slide 36
Target + Catcher QCM: Investigate rough samples, sputter yield, angular distribution
AFM+CFM: probe surface topography, input for SPRAY
SPRAY: simulate sputter yields, angular distributions of atoms
Motivation
Diploma Thesis
Benchmark SPRAY

## Slide 37
QCM experiments vs. SPRAY Microscopy images of rough W samples:
Outline
Diploma Thesis
Fusion@ÖAW Vienna, Austria
Benchmark with rough W samples
  Cupak et al., Appl. Surf. Sci. 570, 2021
Notes: The QCM was then used to make a benchmark study for the code.
In the experiments, tungsten was selected as target material, since it is a prominent material used in nuclear fusion devices. Both tungsten coated quartz crystal samples and bulk tungsten targets with variable roughness were used.
Both AFM and confocal microscopy was used to investigate these samples, while the latter technique was used especially for the rougher ones.
Here, i shortly want to show you some selected images of the sample surfaces.
Sample 1 was the smoothest one and had RMS roughness values on the nm scale. This sample was only investigated with AFM, since CFM could not resolve the mirror-like surface.
Sample 2 could be probed with both microscopes. At first, the AFM image is shown. The RMS roughness was about 34 nm. It has to be mentioned, that in total 15 AFM images were used to determine these parameters for better statistics.
The CFM image of the same sample 2 interestingly had a much higher RMS value of 187nm. It can be assumed that the much larger lateral size of these image included also surface peaks, which were not captured before by AFM. However, a clear lack of resolution was observed.
Finally, the roughest sample 3 is shown here, which had RMS on the micrometer scale.

## Slide 38
QCM experiments vs. SPRAY Microscopy images of rough W samples:
4 AFM images
QCM sample
Outline
Diploma Thesis
Fusion@ÖAW Vienna, Austria
Benchmark with rough W samples
smooth
  Cupak et al., Appl. Surf. Sci. 570, 2021
Notes: The QCM was then used to make a benchmark study for the code.
In the experiments, tungsten was selected as target material, since it is a prominent material used in nuclear fusion devices. Both tungsten coated quartz crystal samples and bulk tungsten targets with variable roughness were used.
Both AFM and confocal microscopy was used to investigate these samples, while the latter technique was used especially for the rougher ones.
Here, i shortly want to show you some selected images of the sample surfaces.
Sample 1 was the smoothest one and had RMS roughness values on the nm scale. This sample was only investigated with AFM, since CFM could not resolve the mirror-like surface.
Sample 2 could be probed with both microscopes. At first, the AFM image is shown. The RMS roughness was about 34 nm. It has to be mentioned, that in total 15 AFM images were used to determine these parameters for better statistics.
The CFM image of the same sample 2 interestingly had a much higher RMS value of 187nm. It can be assumed that the much larger lateral size of these image included also surface peaks, which were not captured before by AFM. However, a clear lack of resolution was observed.
Finally, the roughest sample 3 is shown here, which had RMS on the micrometer scale.

## Slide 39
QCM experiments vs. SPRAY Microscopy images of rough W samples:
4 AFM images
QCM sample
Outline
Diploma Thesis
Fusion@ÖAW Vienna, Austria
Benchmark with rough W samples
smooth
  Cupak et al., Appl. Surf. Sci. 570, 2021
Notes: The QCM was then used to make a benchmark study for the code.
In the experiments, tungsten was selected as target material, since it is a prominent material used in nuclear fusion devices. Both tungsten coated quartz crystal samples and bulk tungsten targets with variable roughness were used.
Both AFM and confocal microscopy was used to investigate these samples, while the latter technique was used especially for the rougher ones.
Here, i shortly want to show you some selected images of the sample surfaces.
Sample 1 was the smoothest one and had RMS roughness values on the nm scale. This sample was only investigated with AFM, since CFM could not resolve the mirror-like surface.
Sample 2 could be probed with both microscopes. At first, the AFM image is shown. The RMS roughness was about 34 nm. It has to be mentioned, that in total 15 AFM images were used to determine these parameters for better statistics.
The CFM image of the same sample 2 interestingly had a much higher RMS value of 187nm. It can be assumed that the much larger lateral size of these image included also surface peaks, which were not captured before by AFM. However, a clear lack of resolution was observed.
Finally, the roughest sample 3 is shown here, which had RMS on the micrometer scale.

## Slide 40
QCM experiments vs. SPRAY Microscopy images of rough W samples:
4 AFM images
QCM sample
Outline
Diploma Thesis
Fusion@ÖAW Vienna, Austria
Benchmark with rough W samples
smooth
  Cupak et al., Appl. Surf. Sci. 570, 2021
15 AFM images
QCM sample
medium rough
Notes: The QCM was then used to make a benchmark study for the code.
In the experiments, tungsten was selected as target material, since it is a prominent material used in nuclear fusion devices. Both tungsten coated quartz crystal samples and bulk tungsten targets with variable roughness were used.
Both AFM and confocal microscopy was used to investigate these samples, while the latter technique was used especially for the rougher ones.
Here, i shortly want to show you some selected images of the sample surfaces.
Sample 1 was the smoothest one and had RMS roughness values on the nm scale. This sample was only investigated with AFM, since CFM could not resolve the mirror-like surface.
Sample 2 could be probed with both microscopes. At first, the AFM image is shown. The RMS roughness was about 34 nm. It has to be mentioned, that in total 15 AFM images were used to determine these parameters for better statistics.
The CFM image of the same sample 2 interestingly had a much higher RMS value of 187nm. It can be assumed that the much larger lateral size of these image included also surface peaks, which were not captured before by AFM. However, a clear lack of resolution was observed.
Finally, the roughest sample 3 is shown here, which had RMS on the micrometer scale.

## Slide 41
QCM experiments vs. SPRAY Microscopy images of rough W samples:
4 AFM images
QCM sample
Outline
Diploma Thesis
Fusion@ÖAW Vienna, Austria
Benchmark with rough W samples
smooth
  Cupak et al., Appl. Surf. Sci. 570, 2021
15 AFM images
QCM sample
medium rough
Notes: The QCM was then used to make a benchmark study for the code.
In the experiments, tungsten was selected as target material, since it is a prominent material used in nuclear fusion devices. Both tungsten coated quartz crystal samples and bulk tungsten targets with variable roughness were used.
Both AFM and confocal microscopy was used to investigate these samples, while the latter technique was used especially for the rougher ones.
Here, i shortly want to show you some selected images of the sample surfaces.
Sample 1 was the smoothest one and had RMS roughness values on the nm scale. This sample was only investigated with AFM, since CFM could not resolve the mirror-like surface.
Sample 2 could be probed with both microscopes. At first, the AFM image is shown. The RMS roughness was about 34 nm. It has to be mentioned, that in total 15 AFM images were used to determine these parameters for better statistics.
The CFM image of the same sample 2 interestingly had a much higher RMS value of 187nm. It can be assumed that the much larger lateral size of these image included also surface peaks, which were not captured before by AFM. However, a clear lack of resolution was observed.
Finally, the roughest sample 3 is shown here, which had RMS on the micrometer scale.

## Slide 42
QCM experiments vs. SPRAY Microscopy images of rough W samples:
4 AFM images
QCM sample
Outline
Diploma Thesis
Fusion@ÖAW Vienna, Austria
Benchmark with rough W samples
smooth
  Cupak et al., Appl. Surf. Sci. 570, 2021
15 AFM images
QCM sample
medium rough
5 CFM images
Notes: The QCM was then used to make a benchmark study for the code.
In the experiments, tungsten was selected as target material, since it is a prominent material used in nuclear fusion devices. Both tungsten coated quartz crystal samples and bulk tungsten targets with variable roughness were used.
Both AFM and confocal microscopy was used to investigate these samples, while the latter technique was used especially for the rougher ones.
Here, i shortly want to show you some selected images of the sample surfaces.
Sample 1 was the smoothest one and had RMS roughness values on the nm scale. This sample was only investigated with AFM, since CFM could not resolve the mirror-like surface.
Sample 2 could be probed with both microscopes. At first, the AFM image is shown. The RMS roughness was about 34 nm. It has to be mentioned, that in total 15 AFM images were used to determine these parameters for better statistics.
The CFM image of the same sample 2 interestingly had a much higher RMS value of 187nm. It can be assumed that the much larger lateral size of these image included also surface peaks, which were not captured before by AFM. However, a clear lack of resolution was observed.
Finally, the roughest sample 3 is shown here, which had RMS on the micrometer scale.

## Slide 43
QCM experiments vs. SPRAY Microscopy images of rough W samples:
4 AFM images
QCM sample
Outline
Diploma Thesis
Fusion@ÖAW Vienna, Austria
Benchmark with rough W samples
smooth
  Cupak et al., Appl. Surf. Sci. 570, 2021
QCM sample
medium rough
5 CFM images
Notes: The QCM was then used to make a benchmark study for the code.
In the experiments, tungsten was selected as target material, since it is a prominent material used in nuclear fusion devices. Both tungsten coated quartz crystal samples and bulk tungsten targets with variable roughness were used.
Both AFM and confocal microscopy was used to investigate these samples, while the latter technique was used especially for the rougher ones.
Here, i shortly want to show you some selected images of the sample surfaces.
Sample 1 was the smoothest one and had RMS roughness values on the nm scale. This sample was only investigated with AFM, since CFM could not resolve the mirror-like surface.
Sample 2 could be probed with both microscopes. At first, the AFM image is shown. The RMS roughness was about 34 nm. It has to be mentioned, that in total 15 AFM images were used to determine these parameters for better statistics.
The CFM image of the same sample 2 interestingly had a much higher RMS value of 187nm. It can be assumed that the much larger lateral size of these image included also surface peaks, which were not captured before by AFM. However, a clear lack of resolution was observed.
Finally, the roughest sample 3 is shown here, which had RMS on the micrometer scale.

## Slide 44
QCM experiments vs. SPRAY Microscopy images of rough W samples:
4 AFM images
QCM sample
Outline
Diploma Thesis
Fusion@ÖAW Vienna, Austria
Benchmark with rough W samples
smooth
  Cupak et al., Appl. Surf. Sci. 570, 2021
QCM sample
medium rough
5 CFM images
5 CFM images
not QCM sample
very rough
Notes: The QCM was then used to make a benchmark study for the code.
In the experiments, tungsten was selected as target material, since it is a prominent material used in nuclear fusion devices. Both tungsten coated quartz crystal samples and bulk tungsten targets with variable roughness were used.
Both AFM and confocal microscopy was used to investigate these samples, while the latter technique was used especially for the rougher ones.
Here, i shortly want to show you some selected images of the sample surfaces.
Sample 1 was the smoothest one and had RMS roughness values on the nm scale. This sample was only investigated with AFM, since CFM could not resolve the mirror-like surface.
Sample 2 could be probed with both microscopes. At first, the AFM image is shown. The RMS roughness was about 34 nm. It has to be mentioned, that in total 15 AFM images were used to determine these parameters for better statistics.
The CFM image of the same sample 2 interestingly had a much higher RMS value of 187nm. It can be assumed that the much larger lateral size of these image included also surface peaks, which were not captured before by AFM. However, a clear lack of resolution was observed.
Finally, the roughest sample 3 is shown here, which had RMS on the micrometer scale.