## Slide 1: Langmuir probes from the JET tungsten divertor: Surface composition from hydrogen to tungsten by IBA
Per Petersson

## Slide 2: Background
Front
Right side
Left side
From section 14 IW

## Slide 3: ToF ERDA analysis
H D BeC N O Fe Ni Crc
W

## Slide 4: ToF ERDA analysis

## Slide 5: Right hand side
Chart: Distance from bottom (mm)
| 26 | 21 | 11 | 1
1H | 36.141 | 26.463 | 30.486 | 32.949
2H | 26.947 | 16.164 | 19.0995 | 33.376
Chart: Distance from bottom (mm)
| 26 | 21 | 11
1H | 18.0975 | 11.169 | 14.277
2H | 11.364 | 2.04 | 1.404
Chart: Distance from bottom (mm)
| 27 | 22 | 12
1H | 21.9045 | 19.0215 | 19.419
2H | 8.9385 | 2.0895 | 5.541

## Slide 6: Right hand side
Chart: Distance from bottom (mm)
| 26 | 21 | 11
Be | 580.3 | 721.344 | 857.671
C | 162.84 | 128.548 | 106.528
Ni | 20.002 | 24.69 | 20.745
Mo
N | 57.192 | 52.596 | 63.0435
O | 628.37 | 697.084 | 749.869
Chart: Distance from bottom (mm)
| 26 | 21 | 11
Be | 231.139 | 231.26 | 247.56
C | 204.087 | 184.7 | 94.819
Ni | 26.6685 | 16.791 | 20.085
Mo
N | 63.1485 | 77.989 | 20.949
O | 238.86 | 273.72 | 335.92
Chart: Distance from bottom (mm)
| 27 | 22 | 12
Be | 328.702 | 320.401 | 323.973
C | 430.498 | 323.991 | 172.773
Ni | 24.825 | 19.1505 | 16.8915
Mo
N | 73.6785 | 53.4405 | 32.8515
O | 235.246 | 317.14 | 373.35
1
5
3

## Slide 7: Left hand side
Chart: Distance from bottom (mm)
| 27 | 22 | 12 | 2
1H | 18.7245 | 19.146 | 12.702 | 17.734
2H | 4.707 | 1.8015 | 5.6535 | 7.7835
Chart: Distance from bottom (mm)
| 26 | 21 | 11 | 1
1H | 35.4105 | 19.026 | 12.621 | 14.1825
2H | 7.401 | 6.0375 | 2.097 | 5.019
Chart: Distance from bottom (mm)
| 26 | 21 | 11 | 1
1H | 24.096 | 23.6445 | 16.156 | 20.2575
2H | 6.825 | 5.694 | 4.041 | 4.869
1
5
3

## Slide 8: Left hand side
Chart: Distance from bottom (mm)
| 26 | 21 | 11 | 1
Be | 360.714 | 267.175 | 304.06 | 427.558
C | 272.469 | 176.655 | 93.153 | 80.7525
Ni | 24.336 | 16.29 | 19.077 | 17.439
Mo
N | 78.579 | 35.115 | 27.762 | 30.0945
O | 352.429 | 309.204 | 373.67 | 527.914
Chart: Distance from bottom (mm)
| 26 | 21 | 11 | 1
Be | 335.317 | 321.435 | 245.32 | 227.094
C | 404.839 | 221.857 | 87.9345 | 75.474
Ni | 20.6955 | 24.5505 | 27.0615 | 27.309
Mo
N | 61.83 | 33.7695 | 17.2335 | 19.3185
O | 307.333 | 359.869 | 325.254 | 350.179
Chart: Distance from bottom (mm)
| 27 | 22 | 12 | 2
Be | 409.786 | 260.17 | 392.55 | 340.94
C | 613.066 | 573.22 | 118.1 | 89.814
Ni | 19.9485 | 20.182 | 26.808 | 18.895
Mo
N | 150.952 | 53.602 | 23.289 | 23.463
O | 135.573 | 241.52 | 509.82 | 485.83
1
5
3

## Slide 9: Back side
Chart: Distance from bottom (mm)
| 27 | 22 | 12 | 2
1H | 9.67 | 7.399 | 12.953 | 11.485
2H | 0 | 0 | 6.567 | 0
Chart: Distance from bottom (mm)
| 26 | 21 | 11 | 1
1H | 10.286 | 6.281 | 10.28 | 16.826
2H | 3.858 | 3.048 | 0 | 0
Chart: Distance from bottom (mm)
| 26 | 21 | 11 | 1
1H | 13.959 | 10.032 | 8.847 | 11.057
2H | 9.0855 | 21.5205 | 7.801 | 0
1
5
3

## Slide 10: Back side
Chart: Distance from bottom (mm)
| 26 | 21 | 11 | 1
Be | 598.836 | 659.2845 | 366.826 | 166.742
C | 40.677 | 34.7265 | 47.412 | 105.021
Ni | 33.7605 | 18.8535 | 48.516 | 64.837
Mo
N | 58.092 | 123.063 | 81.711 | 131.73
O | 571.0545 | 386.799 | 335.596 | 285.681
Chart: Distance from bottom (mm)
| 26 | 21 | 11 | 1
Be | 420.609 | 332.706 | 99.048 | 36.129
C | 63.525 | 38.516 | 49.694 | 118.762
Ni | 41.658 | 49.131 | 49.364 | 38.356
Mo
N | 20.238 | 20.652 | 10.888 | 127.739
O | 477.03 | 401.072 | 181.674 | 163.934
Chart: Distance from bottom (mm)
| 27 | 22 | 12 | 2
Be | 485.36 | 407.57 | 338.66 | 160.91
C | 137.8 | 80.509 | 57.269 | 63.367
Ni | 31.776 | 25.627 | 35.903 | 89.12
Mo
N | 43.811 | 63.395 | 17.925 | 20.577
O | 484.85 | 482.8 | 463.65 | 325.77
1
5
3

## Slide 11: Front side
Chart: Distance from bottom (mm)
| 33 | 27 | 22 | 12 | 2
1H | 12.858 | 9.0165 | 7.9395 | 15.273 | 8.6475
2H | 0 | 6.348 | 10.872 | 2.3415 | 2.475
Chart: Distance from bottom (mm)
| 31 | 29 | 26 | 21 | 11 | 1
1H | 18.3405 | 32.427 | 19.1175 | 15.15 | 10.896 | 19.308
2H | 3.945 | 13.528 | 16.1925 | 7.494 | 0 | 3.51
Chart: Distance from bottom (mm)
| 30 | 27 | 22 | 12 | 2
1H | 10.527 | 11.82 | 9.969 | 11.874 | 8.8335
2H | 1.9455 | 5.949 | 13.2615 | 15.601 | 13.3005
1
5
3

## Slide 12: Front side
Chart: Distance from bottom (mm)
| 30 | 27 | 22 | 12 | 2
Be | 176.454 | 145.46 | 430.336 | 544.86 | 613.599
C | 312.643 | 180.26 | 81.7635 | 40.347 | 55.3785
Ni | 31.8225 | 37.473 | 26.2815 | 30.39 | 24.4935
Mo
N | 68.904 | 60.018 | 78.8805 | 76.816 | 164.839
O | 130.188 | 164.5 | 462.774 | 490.53 | 406.341
Chart: Distance from bottom (mm)
| 31 | 29 | 26 | 21 | 11 | 1
Be | 50.9175 | 186.52 | 235.537 | 287.569 | 297.244 | 223.878
C | 125.01 | 240.53 | 190.477 | 91.668 | 68.3655 | 70.5075
Ni | 25.581 | 25.215 | 18.7335 | 21.999 | 33.5175 | 45.0135
Mo
N | 50.391 | 59.782 | 35.199 | 13.3635 | 14.046 | 22.6725
O | 90.5595 | 207.36 | 252.708 | 381.097 | 457.176 | 422.778
Chart: Distance from bottom (mm)
| 33 | 27 | 22 | 12 | 2
Be | 5.322 | 196.993 | 254.3625 | 318.165 | 181.54
C | 79.9695 | 408.933 | 146.7825 | 55.1445 | 49.503
Ni | 24.756 | 24.636 | 32.343 | 44.4705 | 46.197
Mo
N | 21.5205 | 37.041 | 20.961 | 13.191 | 16.663
O | 48.3735 | 299.293 | 265.5375 | 407.397 | 297.05
1
5
3

## Slide 13: Helium
Chart: Distance from bottom (mm)
| 27 | 22 | 12 | 2
3He | 7.077 | 6.873 | 0.9735
4He | 21.4125 | 15.513 | 3.2745 | 2.016
Probe 5 Left hand side
Chart: Distance from bottom (mm)
| 26 | 21 | 11 | 1
4He | 14.5065 | 3.63 | 4.3185 | 4.905
Probe 3 Left hand side
Single point at front of probe 5 and left side of probe 1

## Slide 14: Summary
W sample analysed in 4 different directions
Be and O amounts are similar in most co-deposits.
He (helium-3 and 4)in a few points mostly on sides
Not much D found on the samples (probes were taken out after ILW-2 campaign ended in hydrogen).
Be and O more further down on sides and front.
C found in greater amount closer to the tip