## Slide 1: Tritium retention in plasma-facing components
E. Pajuste,
A. S. Teimane, A. Vitins, L. Avotina, A. Lescinskis,
P. Kalnina, R.J. Zabolockis, M. Sondars

## Slide 2: OUTLINE
ITER Like Wall plasma facing materials
Tritium sources in JET vacuum vessel
Tritium measurement methods at UoL
Tritium in plasma facing materials
E. Pajuste| WP PWIE 2022 Reporting Meeting | Julich| 2023| Page 2

## Slide 3: Plasma facing materials in ITER Like Wall
E.Pajuste, Physica Scripta, 2021
ITER-Like-Wall (ILW) project has been carried out at Joint European Torus (JET) to test plasma facing materials relevant to International Thermonuclear Experimental Reactor
E. Pajuste| WP PWIE 2022 Reporting Meeting | Julich| 2023| Page 3

## Slide 4: Plasma facing materials in ITER Like Wall
PFM possess very different properties and, therefore, each requires a different approach for the measurements of tritium trapped in the bulk
* Nickel based alloy
Element(s) | Be | W | Ni53Fe19Cr19NbMoTi | C
Atomic mass | 9 | 74 | ~27 | 12
Density, g·cm-3 | 1.18 | 19.3 | 8.1 | 1 -2
Linear thermal expansion, K-1 | 11.4·10-6 | 4.5·10-6 | 11.2·10-6 | (-1-2)·10-6 [G. Pintsuk. 2009]
Melting point, oC | 1287 | 3422 | 1370-1430 | 3500
H chemistry | BeH2 unstable | WH2 and WH4 unstable | Only possible at high pressures (nickel) | Forms stable hydrocarbons
Beryllium
Tungsten
Inconel 718*
CFC
E. Pajuste| WP PWIE 2022 Reporting Meeting | Julich| 2023| Page 4

## Slide 5: Tritium in JET vacuum vessel
in-vessel tritium inventory remaining from previous D–T campaigns;
energetic tritium ion production as a result of D–D reaction;
tritium production in neutron-induced transmutation of beryllium.
During the ITER Like Wall campaigns up to 2021 only stable hydrogen isotopes have been introduced in the vacuum vessel of JET.
Possible sources of tritium:
E. Pajuste| WP PWIE 2022 Reporting Meeting | Julich| 2023| Page 5

## Slide 6: Previous D–T campaigns
Preliminary Tritium Experiment (PTE) in 1991 [1]
First Deuterium-Tritium Experiment (DTE1) in 1997 [2,3]
Trace Tritium Experiment (TTE) in 2003 [4].
In total 35,39 g (5 ·1024atoms or 9 PBq) of tritium has been introduced (5 mg – PTE, 35 g – DTE1 and 380 mg – TTE)
[1] Team, J.E.T., 1992, Nuclear Fusion. 32(2): 187.
[2] Jacquinot, J., V.P. Bhatnagar, J.G. Cordey, et al., 1999, Nuclear Fusion. 39(2): 235.
[3] Keilhacker, M., A. Gibson, C. Gormezano, et al., 1999, Nuclear Fusion. 39(2): 209.
[4] Zastrow, K.D., J.M. Adams, B. Yu, et al., 2004, Plasma Physics and Controlled Fusion. 46(12B): B255.
If to take into account decay of T in 2021 the activity would be ~3PBq.
Most of the remained tritium must be removed together with the extracted CFC tiles during change to ILW metallic tiles.
E. Pajuste| WP PWIE 2022 Reporting Meeting | Julich| 2023| Page 6

## Slide 7: D - D reaction
Produced tritium kinetic energy is 1.01 MeV that leads to its ability to implant into the material[6]
[6] Rubel, M., Journal of Fusion Energy, 2019. 38(3): p. 315-329.
Neutron induced beryllium transmutations
Can be considered to have the lowest contribution since the overall neutron yield are very low: for ILW1 and ILW2 ~5∙1019 neutrons in total.
E. Pajuste| WP PWIE 2022 Reporting Meeting | Julich| 2023| Page 7

## Slide 8: Concepts of tritium measurement
Tritium concentration in PFMs from the ITER Like Wall after D-D campaigns are very small - several orders of magnitude less than that of deuterium.
High sensitivity of the measurement is critical
E. Pajuste| WP PWIE 2022 Reporting Meeting | Julich| 2023| Page 8

## Slide 9: Dissolution/etching method
Materials to be applied for: bulk metals, metallic coatings
Based on controlled dissolution/etching of metallic matrix and measurement of tritium being released
Plasma facing surface
Me+
T+,
HT, DT, T2
DTO, HTO
T0 interstitial
T+ chemically bonded to impurities
HT, DT or T2 in pores
Me
Me
Dissolution/etching
Purge gas
Tritium measurment in gasous phase (proportional gas flow detector)
Tritum measurement by the means of liquid scintillation
Tritium measurements based on its radioactivity
If dissolution/ etching rate is controlled - depth profile can be assessed of tritium released in the gas phase
E. Pajuste| WP PWIE 2022 Reporting Meeting | Julich| 2023| Page 9

## Slide 10: Dissolution method - beryllium
Simultaneous etching of the metal surface and measurements of the released tritium in purge gas (proportional counter) and solution (liquid scintillation)
Be0 + 2H+ → Be 2+ + 2H0
H0 + H0 → H2 (gas ph.)
H0+T0 (solid phase) → HT (gas ph.)
T2 (solid ph.) → T2 (gas ph.)
T+(solid ph.) → T+ (liquid ph.)
Successive layers of Be are removed using diluted sulphuric acid and amount of evolved hydrogen (depicted as ‘H’) and released tritium (depicted as ‘T’) measured.
E. Pajuste| WP PWIE 2022 Reporting Meeting | Julich| 2023| Page 10

## Slide 11: Electrochemical etching- tungsten
H0 + H0 → H2 (gas ph.)
H0+T0 (solid phase) → HT (gas ph.)
T2 (solid ph.) → T2 (gas ph.)
T+(solid ph.) +OH-→ HTO (liquid ph.)
H0 + H0 → H2 (gas ph.)
H0+T0 (solid phase) → HT (gas ph.)
T2 (solid ph.) → T2 (gas ph.)
T+(solid ph.) +OH-→ HTO (liquid ph.)
Successive layers of W are removed using electrochemically in 35% KOH solution where both electrodes are tungsten.
Amount of evolved hydrogen (depicted as ‘H’) and released tritium (depicted as ‘T’) measured. Applied voltage ~3V.
E. Pajuste| WP PWIE 2022 Reporting Meeting | Julich| 2023| Page 11

## Slide 12: Combination of etching methods for layered structures
Successive layers of Be are removed using 4 mol/L sulphuric acid, whereas Inconel - by electrochemical etching in the same solution by applying the 3V voltage.
Chart: Beryllium
Chart: Inconel
E. Pajuste| WP PWIE 2022 Reporting Meeting | Julich| 2023| Page 12

## Slide 13: Thermal desorption
Plasma facing surface
T0 interstitial
T+ chemically bonded to impurities
HT, DT or T2 in pores
Me, CFC,
mixed
Materials to be applied for: all
Based on controlled thermal treatment and measurement of tritium being released as a result of diffusion
HTO,DTO,
HT, DT, T2
Heating
Rate ~5 K·min-1
Tmax ~1300K
Purge gas
Tritium measurement in gaseous phase (proportional gas flow detector)
Me, CFC,
mixed
Before monitor the zinc bed at ~400oC converts HTO/DTO to HT, DT, and traces of T2
E. Pajuste| WP PWIE 2022 Reporting Meeting | Julich| 2023| Page 13

## Slide 14: Full combustion
Materials to be applied for: all combustible
Based on full oxidation of material (destruction of the matrix) itself and and measurement of tritium being released
HTO,DTO,
HT, DT, T2
Heating in moistened air
~1100K
All tritium species are oxidized to water form
Plasma facing surface
T0 interstitial
T+ chemically bonded to impurities
HT, DT or T2 in pores
Me, CFC,
mixed
MeO , CO2,
Example of Be specimen
Measured by the means of liquid scintillation
E. Pajuste| WP PWIE 2022 Reporting Meeting | Julich| 2023| Page 14

## Slide 15: COMPARISON OF METHODS
Dissolution/etching
TDS
Full combustion
ADTVANTAGES
DISADTVANTAGES
Information on
  total tritium amount
  depth profile
  chemical state (can be adapted)
In layered materials information on tritium in each layer can be assessed
Fast
No elevated temperatures used (safe)
Information on
  total tritium amount
  Desorption spectra
Tritium trapping energies can be assessed
Applicable to all kinds of material
High sensitivity
Information on
  total tritium amount
Can be assumed that all tritium is measured since the «hosting matrix» is fully destroid.
Not all tritium might be measured if not sufficient layer thickness is etched (remains in bulk)
Some data might be lost if tritiated water vapor condensates before reaching the Zn bed
Time consuming
Limited information on tritium initial state in the material
E. Pajuste| WP PWIE 2022 Reporting Meeting | Julich| 2023| Page 15

## Slide 16: Studied materials
Bulk beryllium tiles from 3 positions - inner wall (IWGL), outer wall (WPL) and upper part (DP) of the vessel
Beryllium coated Inconle tile from the inner wall (IWC) (indicative position in the vessel regarding toroidal direction)
HGFC
14IG3B
Tungsten coated CFC tiles - High Field Gap Closure tile (HFGC), divertor tile No 1 (14ING1A) and No 3 (14IG3B),
Bulk tungsten lamellas – divertor lamella A24
IWC
W lamellas
Walls
Divertor
E. Pajuste| WP PWIE 2022 Reporting Meeting | Julich| 2023| Page 16

## Slide 17: Tritium distribution in vessel (2011-2012)
W/CFC
(1-10)x1012 T atoms/cm2
W/CFC
2x1012 T atoms/cm2
Bulk W
3.5x1012 T atoms/cm2
Be/Inconel*
15x1012 T atoms/cm2
Bulk Be
(2-9)x1012 T atoms/cm2
Bulk Be
(5-40)x1012 T atoms/cm2
Bulk Be
2x1012 T atoms/cm2
* Particular sample has been 2011 -2015
E. Pajuste| WP PWIE 2022 Reporting Meeting | Julich| 2023| Page 17

## Slide 18: Tritium concentration beryllium tiles
Chart: Logarithm of tritium concentration, LOG (atoms/cm2)
| ILW1 | ILW2 | ILW3
Inner wall | 12.6949 | 12.413 | 11.9345
Outer wall | 13.1805 | 13.2661 | 13.7006
Upper part | 12.3738 | 11.71 | 10.5927
Position, mm | T atoms/cm2 x1012 |  |  |  |  | %
 | ILW1 | ILW2 | ILW3 | Sum | 1-3 | 
Outer wall tile WPL |  |  |  |  |  | 
-146 | 15 | 18 | 33 | 66 | 39 | 59
-33 | 16 | 22 | 39 | 77 | 81 | 105
98 | 4 | 21 | 11 | 35 | 15 | 42
146 | 3 | 2 | 4,6 | 10 | 2,5 | 25
Inner wall tile IWGL |  |  |  |  |  | 
-145 | 2 | 0.5 | 0.3 | 3 | 2.4 | 77
-92 | 4 | 2 | 0.4 | 6 | 2.5 | 41
145 | 2.1 | 1.2 | 0.5 | 4 | 1.2 | 32
Tritium concentration at particular positions in vacuum vessel in tiles exposed to each campaign and tiles exposed throughout all campaigns
E. Pajuste| WP PWIE 2022 Reporting Meeting | Julich| 2023| Page 18

## Slide 19: Tritium distribution in layered material
Beryllium coated Inconel
Beryllium coating
Inconel substrate
1.5x1013 atoms per cm2
4x1011 atoms per cm2
More than 97% of the measured tritium is accumulated in the thin beryllium coating
E. Pajuste| WP PWIE 2022 Reporting Meeting | Julich| 2023| Page 19

## Slide 20: Tritium concentration - divertor, W/CFC
2 mm
2 mm
Chart: HFGC tile - T atoms/cm2
| 138 | 138 | 138 | 138 | 98 | 98 | 98 | 98 | 58 | 58 | 58 | 58
TDS | 1.505e+13 | 1.0413e+13 | 2.4673e+12
FC | 11200000000000 | 1.7122e+14 | 64300000000000 | 1.1307e+14 | 13400000000000 | 1.8342e+13
Chart: HFGC tile - T atoms/g
| 138 | 138 | 138 | 138 | 98 | 98 | 98 | 98 | 58 | 58 | 58 | 58
TDS | 6.3922e+13 | 5.6014e+13 | 1.1877e+13
FC | 39400000000000 | 5.055e+13 | 31300000000000 | 4.365e+13 | 7390000000000 | 6.5794e+12
Samples of a~1 mm surface layer (ranges up to 1,5 mm). Tritium accumulation might be further than that into the bulk
E. Pajuste| WP PWIE 2022 Reporting Meeting | Julich| 2023| Page 20

## Slide 21: TDS
Chart: Time, s
Chart: Time, s
1 a
5 a

## Slide 22: Summary
Tritium concentration in plasma facing materials is in range from 1010 to 1014 atoms per cm2
Variances in tritium accumulation behaviour in different vacuum vessel locations indicate differences in dominant sources: implantation of energetic T ions, D-D reaction products, in outer wall and tritium co-deposition with erosion products on the inner wall and upper parts of vacuum vessel
There are several approaches for tritium measurements depending on the material type and the required information and can be adapted also the mixed materials such as coating and substrate
Methods based on tritium radioactivity measurements can be applied to trace amount measurements – T total amount, thermal desorption spectra, depth estimation in PFMs with T concentration down to 1010 atoms per cm2

## Slide 23
Asoc. Prof. Elina Pajuste
Institute of Chemical Physics
University of Latvia
Jelgavas 1, Riga, Latvia
elina.pajuste@lu.lv
University of Latvia Academic Center of Natural Sciences
Thank you for your attention!