## Slide 1
“Jožef Stefan” Institute (JSI), Dept. of Gaseous Electronics, F6
Jamova cesta 39, Ljubljana, SLOVENIA
Permeation reduction factor of Chromia on Cr films on Eurofer¶
Vincenc Nemanič
vincenc.nemanic@ijs.si

## Slide 2
* Original results presented in ~ 20 peer-reviewed papers.
Over the last years, several „fusion-related materials“ have been investigated in our lab *
by the gas-driven permeation method
Construction materials: AISI316 ITER grade (ITER), Eurofer (DEMO)
First wall metals: Be, W and BeW
Hydrogen permeation barriers (HPBs): TiAlN, SiNx, WN, CrWN, CrN, Cr2N, AlCrN, ZrN which were deposited by various sophisticated techniques
In the present campaign, we investigated the ability to prepare an efficient HPB in situ by controlled oxidation
Introduction

## Slide 3
We determined the HPB efficiency of CrOx
in situ grown on Cr bulk membrane at 400°C, 1 bar O2
in situ grown on Cr film sputtered on Eurofer substrate
sputtered CrOx on Cr film sputtered on Eurofer substrate
CrOx has been frequently studied as a passivation layer on steels but rarely as an HPB. By oxidation, chromia (Cr2O3) is not always achieved but CrOx.
Unfortunately, even pure Cr membrane has been rarely studied in permeation experiments, and data might be erroneous.*
Our first task was thus testing 1 mm thick Cr membranes.
Introduction
*Stöver, D. et. al.; Hydrogen and deuterium permeation through metallic and surface-oxidised chromium, Surf. Coatings Technol. 28, 281–290 (1986).

## Slide 4
Permeation cell design (sample 40 mm, A = 8.5 cm2) with Au sealing sets specific limitation:
temperature 200°C to 400°C,
upstream pressure 50 – 1000 mbar
downstream pressure 10-10 – 0.05 mbar
detection limit of j ~1011H2/cm2/s and j ~106 D2/cm2/s
Permeation rate determined by:
dynamic method applying calibrated QMS
or
gas accumulation method: calibrated capacitance manometers + QMS
Permeation rate (j) measurements

## Slide 5
Three sections: upstream, downstream and analytical. Deuterium is used for a higher discrimination ratio at highly impermeable membranes.
Experiment: All-metal UHV system for permeation
upstream section,
hydrogen pressure:
10 – 1000 mbar
oxygen pressure:
10 – 1000 mbar
downstream section,
hydrogen pressure
0 – 5.10-2 mbar
analytical
section

## Slide 6
Task 1: Determination of Cr permeability and diffusivity
A solid 1 mm thick Cr membrane, termed „referential membrane“ with no Cr oxides, was prepared by well know approach by coating with Pd (100 nm).
Pd has a very high bulk permeability, but due to low thickness, it does not interfere with Cr data but mainly prevents unavoidable Cr oxidation by residual gases in high vacuum.
Pd withstands moderate thermal cycling up to 400°C, but the diffusion of Pd into bulk Cr limits long-term experiments and higher temperatures even in the UHV.
The formalism for simple bulk membranes

## Slide 7
Results on Task 1:
The formalism for simple bulk membranes
Permeability: P0 = 3.23x10-7 mol H2/s/m/Pa0.5 and Ea = 0.68 eV
Diffusivity: D0 = 9.0x10-5 m2/s and Ea = 0.59 eV.
The only published data on diffusivity in Cr is most probably erroneous.[Ref.5]
Ref 5 Stöver, D. et. al.; Hydrogen and deuterium permeation through metallic and surface-oxidised chromium, Surf. Coatings Technol. 28, 281–290 (1986).

## Slide 8
d2 >> d1,
membrane diameter >> d1,d2
Only AISI316 ITER grade and Eurofer could be measured as solid bulk membranes being strong enough to withstand gas load and sealing force!
**
Since most „fusion materials“ exhibit low bulk permeability, a concept of a „double-layered“ membrane enables the permeation tests.
1st layer: thick substrate (0.3 - 1 mm) made of a highly permeable material.
2nd layer: a dense, defect-free and well-matched film (0.5 – 10 µm) capable
of withstanding thermal cycling and long-term operation at high temperatures.
The formalism of simple and double-layered membranes

## Slide 9
Definition: the ratio of the steady permeation rate through the uncoated membrane juncoated versus the permeation rate through the coated membrane jcoated, is termed “the permeation reduction factor” (PRF):
The value of the PRF in the case of a double-layered membrane can be derived from the permeability Pi of each layer. The permeation rate j through a single layer of thickness d, having diffusivity D and solubility Ks is:
(1)
(2)
The formalism of double-layered membranes

## Slide 10
For a thin film barrier, where df << ds, and Pf<<Ps, eq. 4 may be applied to extract the most relevant barrier property, i.e. permeability Pf:
The effective or apparent permeability Pe for the double-layered, (index f for the film and index s for substrate) is:
(5)
where each of the two layers is specified by its thickness and permeability P. The resulting PRF is:
(3)
(4)
The formalism of double-layered membranes

## Slide 11
Measuring procedure: after admittance of hydrogen to the upstream side,
steady hydrogen permeation rate through the bulk substrate is established
within a characteristic time-lag L (gas accumulation method displayed)
bulk membrane double-layered membrane
Experiment: Procedure on double-layered membranes
Double-layered membrane exhibits lower permeation rate and longer L, LDL>LB

## Slide 12
*Sun, P. Z. et al. Limits on gas impermeability of graphene. Nature 579, 229–232 (2020)
**B. Zajec, Int. J. Hydr. Energy 36 (2011) 7353–7361
The true mechanism of efficient hydrogen permeation rate suppression (PRF>1000) by a dense dielectric film has rarely been analysed theoretically (=ab initio calculations)*. We do not have a general model of proton migration in the lattice. All data in Table 1 are related only to „thin films“ <10 µm.
Experimental data with a lower PRF (than predicted) were mostly explained by film cracks and defects, which are difficult to confirm by SEM or other methods.**
Review of hydrogen permeation barrier (HPB) efficiency achieved from double-layered membrane experiments

## Slide 13
* data on bulk Cr permeability and Cr2O3 is rare; thickness of Cr2O3 was estimated, not measured.
Table 1 from V Nemanič, Nuclear Materials and Energy 19 (2019) 451–457
Motivation
In situ grown hydrogen permeation barriers

## Slide 14
Motivation for our work: The attractive property of an ad-layer grown in situ in (Ar + D2 + D2O) at 700°C and 800°C, was claimed; no data on characterisation of Cr oxide properties was reported.
In-situ grown hydrogen permeation barriers

## Slide 15
For highly impermeable materials, the effect of in situ grown ad-layer on hydrogen permeation rate is difficult to evaluate. Cr exhibits low bulk hydrogen permeability, so an ad-layers effect can hardly be detected even when the ad-layer is grown in situ.
In-situ grown hydrogen permeation barriers
An old publication on CrOx* and an only recent one **.
An approach that simplifies the task is to prepare first a double-layered membrane:
highly permeable substrate + less permeable film Cr.
three-stage testing follows
* D. Stover, et. al, Surf. Coat. Technol. 28 (1986) 281–290
** V Nemanič, M Žumer, J Zavašnik, J Kovač, Intern. J of Hydrogen Energy, in press

## Slide 16
Task 2:
1) Permeation rate evaluation of a double-layered membrane at selected T.
2) The Cr surface is exposed to oxygen (p, T, t), (1 bar O2, 400°C, 2-20h)
3) Repeated permeation rate evaluation by hydrogen at 400°C
The effective PRF exhibits the role of the Cr2Ox ad-layer.
The highest PRF = 3800 at 400°C was achieved after 2h oxidation in O2 and corresponded to ~28 nm thick Cr2Ox. ** This value could not be repeated!
Cr2Ox seems to be the most effective barrier material ever reported:
PCr(400°C) = 7.0x10-20 mol H2/s/m/Pa0.5
The formalism of double-layered membrane testing
* V Nemanič, M Žumer, J Zavašnik, J Kovač, Intern. J of Hydrogen Energy, in press

## Slide 17
Cr is brittle – testing of our 40 mm diameter membranes thinner than 1 mm was not feasible. Sealing by golden gaskets exerted high and not uniform pressure which caused cracking.
Using 3.3 µm Cr film sputtered on 0.5 mm Eurofer, a strong double-layered membrane with PRF = 1.03 was prepared. Cr film has thus a negligible impact on permeation rate.
Testing of the influence of various gases on hydrogen permeation rate through modified Cr surface became substantially easier, as at 400°C,
PCr/PEurofer = 0.2 shorter evaluation period
DCr/DEurofer = 0.004 lower detection limit
This double-layered membrane in oxidation experiments is „analogue“ to
~0.1 mm thick bulk Cr.
Advantage of double-layered membrane: Cr film on Eurofer
Task 3:

## Slide 18
Substrate: 40 mm O.D., 0.5 mm thick Eurofer
Cr film, 3.3 µm thick, deposited by the magnetron sputtering technique
Cr film additionally coated by 0.7 µm thick CrOx film, (magn. sputt.)
Layered membranes (Eurofer + Cr film and Cr + CrOx film)
Substrate: 40 mm O.D., 0.5 mm thick Eurofer+Cr film, 3.3 µm thick, deposited by the magnetron sputtering technique

## Slide 19
As a thin CrOx on Cr film was formed during unavoidable thermal treatment in a high vacuum on bulk Cr, two referential membranes with 100 nm Pd on Cr film were first prepared and tested. The permeation rate for both samples was almost identical and claimed to have a PRF=1.
Surprisingly, the equal preparation stage resulted in a rather large scattering of PRF values on Cr film coated samples.
CrOx thickness was d ~1.5 nm, as revealed by XPS on a special sample not tested by permeation. Stoichiometry could hardly be determined.
Further oxidation in pure O2 was to be far less efficient than at bulk Cr.
Sputtered CrOx had a very low impact on the permeation rate!?
Oxidation of layered membranes - results

## Slide 20
Key data of 5 selected Cr samples (out of 10) vs. referential Pd coated samples are presented.
Unavoidable residual vacuum exposure during the preparation stage resulted in a PRF from 4 to 30.
Oxidation of layered membranes - results

## Slide 21
Further oxidation in pure O2 was far less efficient than at bulk Cr where
the highest PRF=3800 has been achieved. We could not repeat this high PRF in similar exposures to oxygen.
At present, we do not have a better explanation than that smooth Cr surface prevented CrOx growth much more efficiently than on bulk Cr.
PRF ~10 at ~1.5 nm thickness is a good value.
Another unexpected fact was that 0.7 m thick sputtered CrOx had a very low impact on the permeation rate!?
The answer is that the atmosphere in the deposition chamber was not optimised for achieving stoichiometric chromia.
Oxidation of layered membranes - results

## Slide 22
New phenomena by 5%O2/95%H2 mixture at 400°C were observed:
catalytic reaction at hot surface was recorded at the upstream side of Pd and CrOx surface, but kinetics was substantially higher on Pd, but:
no impact of oxygen on permeation rate through referential membranes
permeation blocking by reaction on CrOx surface.
Repeated measurement in pure H2 restored initial low PRF
Oxidation of layered membranes – results

## Slide 23
Oxidation of layered membranes - results
Referential Pd coated membrane
Selected CrOx coated membrane

## Slide 24
Summary and outlook for next experiments
Double-layered membranes used as a „substrate“ represent a simplification in studying the effect of fusion-related metals, Be and W, as well as oxide ad-layers grown in situ when the bulk membrane material is highly impermeable.
Our data on bulk Cr match reports on permeability but differ greatly in diffusivity. Arguments for errors in the single published paper are given.
High PRF=3900 of CrOx was only confirmed for the in situ grown ad-layer~28 nm CrOx. Sputtered 0.7 m CrOx had no impact on the permeation rate

## Slide 25
Summary and outlook for next experiments
Original results reveal an ultra-thin layer (2D) formed at the topmost CrOx layer at specific testing conditions as being an extremely efficient HPB: PRF >5000. Ab initio calculations and complementary methods needed to confirm this.
In pure hydrogen, the HPB decomposes, and the initial state is restored.

## Slide 26
Outlook for 2023 - next experiments
In 2023, we want to further study the role of oxygen in hydrogen at forming an HPB at Fe, as hydrogen permeation rate blocking was observed on Eurofer. Is Cr involved in HPB formation? Is oxygen in the mixture sufficient to form HPB?