## Slide 1: Retention and permeation modelling for DEMO (2022)
J. Mougenot1, R. Delaporte-Mathurin2,1, E. Hodille2, Y. Charles1, C. Grisolia2
1Université Sorbonne Paris Nord, LSPM, CNRS, UPR3407, F-93430, Villetaneuse, France
2CEA, IRFM, F-13108 Saint-Paul-lez-Durance, France

## Slide 2: Fuel retention task
One of the TSVV#7 objectives: Assessment of tritium in-vessel inventory (co-deposition, bulk retention with He-induced and neutron damage)

## Slide 3: Summary of work done in 2022
(for M2.9) 3D effects on hydrogen transport in ITER-like monoblocks with FESTIM code
(for M4.6) Modelling H-He interactions in W
Paper to be submitted – on Eurofusion Pinboard (ID: 33309)
32nd Symposium on Fusion Technology –September 10-23 2022 –Dubrovnik, Croatia
on Eurofusion Pinboard (ID: 30921)

## Slide 4: Monoblock for DEMO (ITER-like)
W
Cu
CuCrZr
5 mm
1 mm
1.5 mm
¼ of a monoblock
+0.5 mm of CuCrZr over Z (pipe continuity, 1 mm space between the monoblocks)
You et al. Journal of Nuclear Materials 544, 152670 (2021)
Several simulations were run with the monoblock thicknesses (e)
varying from 4mm to 14 mm
e/2

## Slide 5: General model description
R. Delaporte-Mathurin – To be submitted
Transient heat tranfer
Kinetic trapping of trapped hydrogen
Fick diffusion of solute hydrogen
Chemical potential continuity at interfaces
Trap properties

## Slide 6: Scenario and boundary conditions
R. Delaporte-Mathurin – To be submitted
Transient simulations up to 106 s (no cycling for DEMO ?)
2 cases are considerated
Solved with FESTIM code now open-source: https://github.com/RemDelaporteMathurin/FESTIM

## Slide 7: Temperature and mobile H field
Stationnary
e=6 mm
Similar to 2D field
(zero thermal flux on the toroidal face)
After 106 s
e=6 mm
Instantaneous recombination
R. Delaporte-Mathurin – To be submitted
Solubility effect

## Slide 8: Some temporal evolutions
R. Delaporte-Mathurin – To be submitted
No recombination = zero flux ≈ 2D case
Retention is over estimated by 2D simulations
Flux to coolant is zero before 104 s (H diffusion need time) and decrease 105 s thank to the desorption on the CuCrZr pipe extrusion

## Slide 9: Thickness effect
R. Delaporte-Mathurin – To be submitted
t= 104s
The variation for the no recombination case is due to CuCrZr pipe extrusion
The retention is higher for the thicker, because H is stored futher from a desorption surface

## Slide 10: And study of the baking phase
R. Delaporte-Mathurin – To be submitted
No more plasma, just constant heating during baking phase. Starting point: steady state retention field e=6 mm case
The higher the temperature, the faster the desorption.
After 30 days
The desorption to the coolant represents ≈ 10% of the total desorption

## Slide 11: Next steps (planned for 2023)
Add new trap induced by neutron damages
3D simulations with the Soret effect (data on the heat of transport will be available, the code is ready)
3D simulations with other parametric study (thickness of the W armor ?) and/or others exposure conditions (given by plasma code) and geometry
Evaluate the possibility of IMASization the FESTIM open source code

## Slide 12: Summary of work done in 2022
(for M2.9) 3D effects on hydrogen transport in ITER-like monoblocks with FESTIM code
(for M4.6) Modelling H-He interactions in W
Paper to be submitted – on Eurofusion Pinboard (ID: 33309)
32nd Symposium on Fusion Technology –September 10-23 2022 –Dubrovnik, Croatia
on Eurofusion Pinboard (ID: 30921)

## Slide 13: He nanobulles
S. Blondel . Nuclear Fusion 58, 126034 (2018)
R. Delaporte-Mathurin . Scientific Reports 11, (2021)
R. Delaporte-Mathurin – 32nd SOFT (2022)
Adding a bursting effect in our HeFenics code
In collaboration with S. Blondel and cross-check with Xolotl code

## Slide 14: He nanobulles
R. Delaporte-Mathurin – 32nd SOFT
It allows to predict more realistic bubble size close to the surface
But what is the value of ?

## Slide 15: Some proposal to couple with H transport
R. Delaporte-Mathurin – 32nd SOFT (2022)
?
With some TDS analys we can estimate

## Slide 16: Next steps
Working on the implementation of different k busting laws
Add new traps induced by helium in the 3D simulation of H transport. It is only a surface effect, the impact will be low on the total inventory
Add other surface effects modelled in the frame of TSVV#7 ?

## Slide 17: CEA Team changes for 2023
Christian Grisolia goes into retirement, Floriane Montupet-Leblond will take its place in the project from 2023
Rémi Delaporte-Mathurin goes to the USA, as planned he will not be involved anymore in the project

## Slide 18
Questions/remarks?