## Slide 1: Erosion studies in PSI-2
Study of erosion and redeposition of W atoms/ ions using spectroscopy
W targets: poly W, W (111), W (110), W (100)
Plasma pressure : 0.01…0.1 Pa
Electron temperature: 1..20 eV
Electron density: 1010…1012 cm-3
Magnetic field: 0.025…0.1 T
Ionization degree: 1-5%
Targets: 13x13mm2
5
(1-5 are the line-of-sights)

## Slide 2: Comparion of erosion rate for W target
In the energy range of
60 … 160 eV the difference is within of 20-30%
@498 nm line
One observes a very small difference in erosion rate for different W models
Results are consistent for different gases (Ne, Ar, Kr) for 20 - 180 eV
      and different spectral lines (401nm, 498 nm, 505 nm, etc..)
Redeposited W was
not studied here

## Slide 3: Laser Absoprtion Spectroscopy at PSI-2
Laser system at PSI-2
Sackers et al, J. Phys D. : Appl. Phys. 54 (2021) 395001
Measurements of absorption on W atoms (401 nm and 505 nm lines)
Until now not succesfull
  Probably very weak absoprtion signal
Ar I line