## Slide 1
SMART material studies
within the work package PWIE SP A3
P. Bittner, A. Litnovsky, H.R. Koslowski, J.W. Coenen and Ch. Linsmeier
Forschungszentrum Jülich GmbH, Institut für Energie- und Klimaforschung – Plasmaphysik (IEK-4)

## Slide 2
Z. Haratyunyan et al. (MEPhI) (SMART-WCrY)
M. Zhao et al. (IPP Garching) (W-Y2O3)
higher D-retention in WCrY than pure W
high temperature TDS peak in WCrY
SPS-ed: higher D-retention after annealing
SPS-ed: after annealing desorption is not zero even at 1200 K in TDS
As-sintered/rolled: high temperature TDS peak as in WCrY
spark-plasma sintered samples annealed at 2170 K for 3 h in vacuum (p ~ 2·10-6 Pa)
as-sintered: cold isostatic presssing + high temperature sintering
570 K
TDS: 15 K/min
6·1024 D/m²
D-loading:
450 K
TDS: 15 K/min
6·1024 D/m²
D-loading:
Both authors suggest that the HT-peak and additional retention could be caused by (submicron) pores in the material
non-annealed
annealed
yellow arrows = pores
yellow arrows = pores

## Slide 3: Study the effect of porosity on D-retention in WCrY SMART
FAST 4827
before annealing
FAST 5652
after annealing 1000 °C, 7h
FAST 5099
FAST 4823
FAST 4835

## Slide 4: Investigate the effect of porosity on D-retention in WCrY
Planning to do two D-loading experiments with PSI-2
Experiment 1: investigate differences in D-retention caused by different porosities
  3 x as-sintered , one of them annealed @1000°C, 7h
  1 x as-sintered
  1 x as-sintered
  if available, include reference pure W sample for comparison
  all samples are already cut into PSI-2 geometry
  grinding and polishing will be finished next week
  new density measurements on samples with low density after grinding
  PSI-2 Deuterium loading
    ion energy:
    ion flux:
    ion fluence:
  post-characterization (mass loss, etc.) and NRA and TDS after exposure
Experiment 2: check reproducibility with 2-3 new samples
  all samples must still be produced  will take weeks from now
exposure time (and for whole experiment with preparation etc.)
Experiment 1: expect PSI-2 exposure to be conducted end of March /
beginning of April
Experiment 2: PSI-2 exposure
not before end of April