## Slide 1
Investigation of cluster formation in DP-ps-LIBS of graphite (for LAMIS application):
catching clusters with different configurations (SP, DP355-1064 nm, DP 355-355 nm) and analysing cluster sizes
Measuring D content of plasma exposed, pre-damaged tungsten samples with DP-ps-LIBS
Investigation of influence of different gas atmospheres on DP-ps-LIBS parameters
Continue the development of multi-pulse scanning ps-LIBS for:
Composition measurement in mix materials by CF-LIBS quantative analysis method
depth profiling
hydrogen isotopes measurement
Investigation of dynamical deuterium retention by ns-LIBS in different types of tungsten samples (annealed under different temperatures, pre-damaged, fiber-reinforced...) during and after plasma loading in PSI-2 under different fluences and plasma fluxes
FZJ plan for 2023

## Slide 2: Multi-pulse scanning ps-LIBS
High repetition ps-laser (1030nm, 50kHz - 2MHz, pulse duration 2 ps, pulse energy < 35J) equipped with 2-axis galvo scanner with f-theta lens f= 500 mm or f= 80 mm
X
Y
1 scan
492x623 m2
100 scans
528x625 m2
X-Y galvo scanner
Time resolved spectra
13.5 nm