## Slide 1: WP PWIE: SPE Kick off Meeting 2024
Notes: Please Indicate your subproject

## Slide 2: IAP analysis plan for 2024
IAP
    Cutting of limiter tiles and W lamellae
    Samples to be shipped for analysis to FZJ, CCFE, HR, UoL and VTT, according to future instructions. Includes Louvre clips. (More of a coordinating activity)
    TDS analysis of Be samples
    Louvre clips: chemical structure of co-deposits with XPS
    Fuel retention studies using GDOES and TDS
C. Porosnicu| WP PWIE SP E kick-off meeting

## Slide 3: IAP analysis plan for 2024
IAP
    Cutting of limiter tiles and W lamellae
    Samples to be shipped for analysis to FZJ, CCFE, HR, UoL and VTT, according to future instructions. Includes Louvre clips. (More of a coordinating activity)
    TDS analysis of Be samples
    Louvre clips: chemical structure of co-deposits with XPS
    Sample preparation for GDOES and TDS
    Fuel retention studies using GDOES and TDS
C. Porosnicu| WP PWIE SP E kick-off meeting

## Slide 4: Rough cutting procedure
It is essential that no vibrations are present!
Vibrations induce:
Blade damage
Equipment damage
Unprecise cutting
Thicker blade trace – loss of material and dust production!
HEAT!!
The cutting was performed in dry environment, using a carbide hardened band saw (made in USA) having 2300 mm in length and 19 mm width.
C. Porosnicu| WP PWIE SP E kick-off meeting
For temperature monitoring in real time a FLIR® E-Series Advanced Thermal Imaging Camera, (+/- 1 oC ; 20-900 oC) is used
During cutting the tile temperature did not exceed so far 48 oC

## Slide 5: Cutting process recording document
Tracking system of the Be sample
C. Porosnicu| WP PWIE SP E kick-off meeting

## Slide 6: SPE.1: Coordination activity (IAP)
Using the beryllium processing facility, complete cutting of IWGL tile 1XR18 with runaway electron damage was performed
Typical sample sizes: 10 mm x 10 mm x 10-12 mm or 10 mm x 10 mm x 2.5 mm
Microscopy measurements from top and side surfaces have been made for all the samples.
Cutting of Louvre CLips:
Deliverable: PWIE.SPE.1.T001.D002
Status: Completed
Facilities: Hot cells at IAP
Human Resources: 2 PM
Involved RU: IAP and CCFE as a collaborator
Linked WP or TSVV: WPTE
All 37 samples are packed
Ready to be shipped
Final sample extraction
Cutting plan as agreed with CCFE
Primary and edge sectioning
Louvre clips cutting and sectioning
Samples to be shipped for analysis to FZJ, CCFE, HR, UoL and VTT, according to future instructions
Notes: PD: Plasma Devices as in PEP listed
HHF: High Heat flux as in PEP listed
IBF: Ion beam Facility as in PEP listed
Other facilties as in PEP listed

## Slide 7: Lamellae cutting and sample preparation for TDS and GDOES
Cutting and processing of the samples was required prior to GDOES
Deuterium thermo-desorption spectra (TDS) for the designated samples
Cutting and processing of the sample
Initial TDS GDOES
Sample temperature monitored by IRcamera
Diamond milling disc in action
Special cutting discs containing more than 21% diamond powder embedded in a copper alloy were used;
Lamella temperature during cutting - monitored: must not exceed 70oC
C. Porosnicu| WP PWIE SP E kick-off meeting

## Slide 8: SP E.2 Comparison of hydrogenic retention quantification by different techniques and fuel removal assessment: IAP
Since GDOES demonstrated that D is present in Be deposits but also in W/Mo coatings it is difficult to identify with precision the retention mechanism
Tile 4
Tile 6
Tile 7
Tile 8
TDS was performed on the remaining samples, after GDOES.
We took into account only the non sputtered part during the GDOES measuring process.
TDS was performed from room temperature to 1050oC with a 10oC/min ramp.
One interesting fact in the TDS measurements is the total release done until the maximum temperature reach for most of the samples (11 of 14)
Several desorbtion peaks are present for the samples from all tiles.
High intensity peaks are present at 325-375oC, followed by shoulders for some samples at temperatures between 525 and 800oC
C. Porosnicu| WP PWIE SP E kick-off meeting

## Slide 9: Post-mortem analysis of PFC and other objects in JET: IAP
Initial TDS GDOES
C. Porosnicu| WP PWIE SP E kick-off meeting

## Slide 10: Be samples support
C. Porosnicu| WP PWIE SP E kick-off meeting
Deposition | Substrate | Sample size (mm) | Gas | Thickness (um) | Pieces
Be+H(20%), Bias -150V, 5um, W 4_5 | W | 5*5 | H 20% | 5 | 5
Be+D (1%), 10 um, (10*10) Si_1_1 | Si | 10*10 | D 1% | 10 | 2
Be+D (5%), 10 um, W_2_2 | W | 12*15 | D 5% | 10 | 1
Be+D (5%), 10 um, Si 1 | Si | 12*15 | D 5% | 10 | 1
Be+D(5%), 5um, Si (Sus) 1_1 | Si | 12*15 | D 5% | 5 | 3
Be+D (5%), 20 um, W_2_2 | W | 12*15 | D 5% | 20 | 1
Be+D (5%), 20 um, Si 1 | Si | 12*15 | D 5% | 20 | 1
Be+D(5%), 5um, Si 1_1 | Si | 12*15 | D 5% | 5 | 4
Be+D (5%), 5um, (12*15) Si_2_5 | Si | 12*15 | D 5% | 5 | 2
Be+D(10%). 5um, Si 2_4 | Si | 12*15 | D 10% | 5 | 1
Be (rough) + D (10%), 5 um, W 2_2 | W | 12*15 | D 10% | 5 | 1
Be+D (10at%), 10 um, Si 1 | Si | 12*15 | D 10% | 10 | 3
Be+D (10%), 1 um, (10*10) Si 1_1 | Si | 10*10 | D 10% | 1 | 2
Be+D (10%), 10 um, (10*10) Si 1_1 | Si | 10*10 | D 10% | 10 | 2
Be+D (10at%), 10 um, (12*15) Si 3 | Si | 12*15 | D 10% | 10 | 1
Be+D (10at%), 10 um, Si 2 | Si | 12*15 | D 10% | 10 | 1
Be+D (10%), 5um, (12*15) Si_2_12 | Si | 12*15 | D 10% | 5 | 1
Be+D (10%), 10 um, Si 3 | Si | 12*15 | D 10% | 10 | 1
Be+D(20%), Bias -150V, 5um, W 5_7 | W | 5*5 | D 20% | 5 | 2
Be samples available for LIBS experiments at VTT
Additional samples can be prepared LIBS experiments at VTT
Schematic description of the coating system used for Be-D/Be-H (4:1 at ratio) layer deposition