## Slide 1
  IST activities in 2024: IBA analysis of JET PFCs – plans
  WP PWIE SP E: Kick-off meeting, 23th January, 2024
  Norberto Catarino, Rui Silva, Eduardo Alves

## Slide 2: Pending analyses : 2ON G7A (2013-2016)
2
2ONG7A - 8b
2ONG7A - 7b
2ONG7A - 5b
2ONG7A - 3b
2ONG7A - 1b
8
6
4
2
1a
7a
5a
3a
1b
8b
7b
5b
3b
1c
8c
7c
6c
5c
4c
3c
2c
1d
4d
7d
IAP
VTT
IST
CCFE
NCSRD
Be
+ 2ON G8B (2013-2016) + 14BN G4A (2013-2016)

## Slide 3: Pending analyses : 2ON G7A (2013-2016)
2
2ONG7A - 8b
2ONG7A - 7b
2ONG7A - 5b
2ONG7A - 3b
2ONG7A - 1b
Be
3He+ ; 2,3 MeV
3He+ ; 2,3 MeV
RBS
NRA
EBS
PIXE
1b ->
<- 8b
<- 1b
<- 8b
Erosion

## Slide 4: RC’s 2015-2016 ILW3 (Silicon collectors)
Divertor
◧ ◨ ☒ 2IN
◧ ◨ ☒ 12W (12W-wedge RC – as received – both slits were “opened” )
◧ ◨ ☐ 2OW (Broken pieces, not assembled)
12W
2OW
ILW 1 2 3
2IN

## Slide 5: RC’s 2015-2016 ILW3 (Silicon collectors)
Chart: 
D(3He,p)4He, 2.3 MeV
9Be(3He,p0)11B, 2.3 MeV
Chart: 
12C(3He,p1)14N, 2.3 MeV
Chart: 
The spectra are not analyzed because there is no LP data on tile 4 in ILW-3.

## Slide 6: RC’s 2015-2016 ILW3 (Silicon collectors)
RTI - Reflectance Transformation Imaging

## Slide 7: 2024 Plans
SP E.2
Characterisation of divertor tiles 0 and 1 - Before and after LID-QMS ?
SP E.3
characterize Be limiter tiles - 2XR19(ILW3) and 2XR9 (ILW2+3)
Ion beam analysis of JET plasma facing and diagnostic components - mirror cassettes (tubes)
IST
    Fuel retention studies using IBA (Be limiter samples)
    IBA analyses before and after TDS (for baking studies)
    IBA analysis of mirror cassettes (tubes) for metal migration
2 PM | 2 day of Accelerator
4 PM | 5 days of Accelerator