## Slide 1: VR SPE kick-off meeting 2024
Per Petersson

## Slide 2: Time of Flight Elastic Recoil Detection Analyisis
W
I (scattered beam)
Inconel family
16O
15N
14N
12C
9Be
D
1000
800
600
400
ToF ERDA on Be flake from the dump plate
0 400 800 1200
Energy channel
ToF channel
16O
15N
14N
12C
15N only on very surface
Further analysis of components by ToF-ERDA. Keeping track of 15N and 18O
Combination with NRA for 18O and D Less sensitivity for roughness
Review of existing data sets to gather information about 15N and 18O Keeping track of where they has been found and where it has not been found
Possibility for µ-NRA for spots etc.

## Slide 3: Mirrors as deposition monitors
Number (Å ion)
0 0.2 0.4 0.6
Depth (µm)
Aim: Assess the impact of radiation damage on fuel retention (and reflectivity)
Very simple to remove
Mo mirrors irradiated with 98Mo3+ at 1.6 MeV to 2 dpa and 20 dpa.
SRIM prediction: Quasi-uniform damage up to 0.3 µm
Should be studied both for fuel retention (NRA, ToF ERDA) and reflectivity
10 mm
10 mm
20 dpa
2 dpa
Total reflectivity: 5-10% decrease at 20 dpa.
Diffuse reflectivity increased at 20 dpa: 0.2–3.0%
Total reflectivity (%)
SRIM
Reflectivity of pre-damaged mirrors
Has to be evaluated what can be done with respect to tritium and radiation