## Slide 1: SP X: KoM - plans for 2024
STAFF: Pavel Veis, Pavol Ďurina, Tomáš Roch, Michal Stano, Matej Veis
Post docs: Sahithya Atikukke, Dhanada Sukumaran, Ivan Urbina
PhD. st.: Shweta Soni, Jairo Peralta, Pavitra G. Bhat,
Sanath Shetty, Vaishnavi Sudhakaran (CU Bratislava team)
Notes: Please Indicate your subproject

## Slide 2
LIBS experimental setups
1) Picosecond LIBS setup at MUNI, Brno, CZ
Nd:YAG laser (Brilliant B, Quantel)
Mechelle M5000 spectrometer
Andor iStar 340 T ICCD camera
2) Comenius University, Bratislava, Slovakia
new LIBS cartography ATOMtrace system
Detection of light elements
(H, N, O, Be, B, C, Sn …) LIBS
Broadband spectra
LIBS, CF LIBS
Te, ne
Molecular spectra
Trot, Tvib
1. Trace element detection in complicated matrixes(Mo, W, Fe...)
2. Spectral lines profiles: Stark broadening => ne
Stark and isotopic shifts, D/H ratio
ns OPO laser
ns/ps Nd:YAG
x-y-z translation stage
AtomTrace chamber

## Slide 3: LIBS AtomTrace cartography setup
Cartography is done by performing a raster scan over the sample.
The AtomController software facilitates the control between the computer and the chamber.
The depth of the ablated craters is then studied using confocal microscopy.

## Slide 4: LIBS enhancement approaches
Double pulse LIBS
Laser-induced fluorescence assisted LIBS
Vacuum UV LIBS
Microwave enhanced LIBS
Spark assisted LIBS
Magnetic confined LIBS
Nd:YAG
Mechelle
McPherson
PC
PC
Sample holder
XY Translation
Dichroic mirror
iCCD
iCCD
Focusing lens
Vacuum Chamber
Optical fiber
Gas inlet
Gas outlet
Quartz window

## Slide 5: Vacuum UV LIBS

## Slide 6: Work done in 2023 and plans for 2024
Work done in 2023 and continuation in 2024
  Campaign of LIBS measurements in VTT in May 2022
  Analysing LIBS results from last Be-coating samples with gas impurities
  and CuBe sample - ps/ ns regimes comparison, depth profiling
Notes: This presentation has the follow principal points:
The motivation for performing this work. What is the problem for measuring light elements?
A very brief explanation of what LIBS and CF-LIBS are.
The main advantages of the simulatneous use of VUV and UV-NIR ranges
The experimental setup employed in this work.
The main results.
And finally, some conclusions.

## Slide 7
W and Mo as substrates
Regime | Mo | W
ps | 85 ±13 nm/pulse | 55 ±11 nm/pulse
ns | 318 ±63 nm/pulse | 207 ±42 nm/pulse
Comparison ns/ps LIBS measurements
A. M. Roldán et. al., Fusion Engineering and Design 172 (2021) 112898.
ps
ns
Notes: This presentation is composed by 7 parts. First, the introduction, where I would talk about the motivation and paleoclimatic proxies. Parts 2 to 6 are related to the analysis of all these proxies by laser spectrocopy, being separated in analysis of speleothems by LIBS, the evaluation of the LIBS technique, the anbalysis of other tan speleothems proxies by LIBS, and finally, imaging by LIBS. The last and final part will be the conclusions.

## Slide 8
W and Mo as substrates
A. M. Roldán et al., Fusion Engineering and Design 172 (2021) 112898.
Regime | Mo | W
ps | 85 ±13 nm/pulse | 55 ±11 nm/pulse
ns | 318 ±63 nm/pulse | 207 ±42 nm/pulse
Comparison ns/ps LIBS measurements
ps
ns
Notes: This presentation is composed by 7 parts. First, the introduction, where I would talk about the motivation and paleoclimatic proxies. Parts 2 to 6 are related to the analysis of all these proxies by laser spectrocopy, being separated in analysis of speleothems by LIBS, the evaluation of the LIBS technique, the anbalysis of other tan speleothems proxies by LIBS, and finally, imaging by LIBS. The last and final part will be the conclusions.

## Slide 9
ps LIBS measurements on WTa w and wo D
W and Mo as substrates
ps LIBS regime
Has shorter lifetime
Notes: This presentation is composed by 7 parts. First, the introduction, where I would talk about the motivation and paleoclimatic proxies. Parts 2 to 6 are related to the analysis of all these proxies by laser spectrocopy, being separated in analysis of speleothems by LIBS, the evaluation of the LIBS technique, the anbalysis of other tan speleothems proxies by LIBS, and finally, imaging by LIBS. The last and final part will be the conclusions.

## Slide 10
ps LIBS measurements on WTa w and wo D
W and Mo as substrates
Promising CF LIBS results on Wx%Ta samples wo D.
Next ps LIBS measurements
on Wx%Ta samples w D.
Notes: This presentation is composed by 7 parts. First, the introduction, where I would talk about the motivation and paleoclimatic proxies. Parts 2 to 6 are related to the analysis of all these proxies by laser spectrocopy, being separated in analysis of speleothems by LIBS, the evaluation of the LIBS technique, the anbalysis of other tan speleothems proxies by LIBS, and finally, imaging by LIBS. The last and final part will be the conclusions.

## Slide 11
Resonant LIBS Analysis of WTa/Mo samples
Depth profile at resonant excitation
Depth profile at off-resonance
R-Ablation @ 255.135 nm (W I)
Energy- 2 mJ m, air atm. press..
Ablation rate- 90 nm/pulse
Layer thickness- 7.7 μm
NR- Ablation @ 222.75 nm
(out of W I-II, Ta I-II)
Energy- 2 mJ m, air atm. press..
Ablation rate- 250 nm/pulse
Layer thickness- 6.2 μm
Depth profile via GDOES – 7 μm

## Slide 12: Plans for 2024
Plans for 2024
  Comparison ps / ns CF and depth profile LIBS measurements of relevant samples (e.g. WTa, CuBe) with and without D
  (different exp. conditions: laser wavelength, fluence, iCCD camera delay and gate time, gas , pressure)
  - Goal: pre-study for ps LIBS RH system campaign
  - in collaboration with P. Dvorak (Brno, CR) and E. Grigore groups
  - first results will be presented at Nordic LIBS conference at Tampere in March 2024.
  Participation on ps LIBS RH system campaign in JET and data treatment for quantitative analysis
  Resonant/off-resonance CF and depth profile LIBS measurements of relevant samples
  (different exp. conditions: laser wavelength, fluence, iCCD camera delay and gate time, gas , pressure)
  - Goal: enhancement of LIBS spectrum and increasing of depth resolution.
  Top flat beam profile CF and depth profile LIBS measurements – first test and application on relevant samples (Magnum PSI loaded samples,…)
  Confocal microscopy for evaluation of ablated matter and ablation rate
  Cartography LIBS system for depth profile and X-Y mapping of fusion relevant samples
  Vacuum UV OES
  - Goal: for light element depth profile LIBSE analysis (Boron,….)
Notes: This presentation has the follow principal points:
The motivation for performing this work. What is the problem for measuring light elements?
A very brief explanation of what LIBS and CF-LIBS are.
The main advantages of the simulatneous use of VUV and UV-NIR ranges
The experimental setup employed in this work.
The main results.
And finally, some conclusions.