## Slide 1: SP-X.2: Optimization of laser-based surface analysis diagnostics
Indrek Jõgi
University of Tartu

## Slide 2: Tasks and deliverables 2024
2. CF)-LIBS results He loaded samples and surface modifications
  2024: Analysis of He in Magnum-PSI loaded samples and deposited coatings with He.
  (publication of VTT and DIFFER campaign results)
1. Analysis of B containing coatings and/or W coatings with (CF)-LIBS: absolute content and composition
  2024: Analysis of WEST samples.
  Deposited B containing coatings?
Chart: Wavelength (nm)
Chart: LIBS shot nr.
B | 95178.0054 | 150134.6587 | 128395.5343 | 75557.2705 | 46271.9368 | 40556.2139 | 32049.3118 | 29725.8501 | 23490.0827 | 25101.1571 | 23829.2931 | 24498.3444 | 18898.6691 | 21108.3035 | 21122.1345 | 17284.8611 | 17167.6039 | 19469.0927 | 19638.572 | 19044.9141 | 20229.0741 | 18267.1853 | 18186.5648 | 18257.217 | 17390.945 | 16392.9886 | 21016.7861 | 17417.3483 | 17467.324
O | 8381.9352 | 7984.458 | 9069.9186 | 6650.3881 | 4089.7773 | 3857.494 | 1519.3158 | 1944.6275 | 2630.5382 | 1435.1632 | 1030.785 | 963.3357 | 1205.0547 | 115.061 | 761.2976 | 425.0434 | 376.6489 | 422.4331 | 434.1009 | 672.4542 | 237.82 | 781.1646 | 1018.5341 | 142.9545 | 391.0689 | -101.658 | 241.3453 | 1264.4849 | 117.2111 | 502.674
Mo | 10900.5636 | 10481.5902 | 11790.8972 | 11530.7715 | 11245.1855 | 13852.2986 | 11911.8701 | 11133.6138 | 12371.9944 | 10778.7543 | 9076.592 | 9541.9127 | 9202.8232 | 8202.7819 | 8745.1952 | 8416.7824 | 8507.531 | 8798.6542 | 8089.9394 | 7614.3022 | 7045.38 | 6548.3487 | 6952.5324 | 6443.5689 | 6341.6893 | 6525.3908 | 5071.8439 | 4811.2714 | 6212.467 | 5439.3691
Chart: Crater nr
 | 671.3972 | 1585.0546 | 2556.7799 | 2452.3041 | 1703.6581 | 444.7446 | 345.2258
1 μm c-W
Edge 16·1015 at/cm2
Center 250·1015 at/cm2
ToF-ERDA
LIBS

## Slide 3: Tasks and deliverables 2024
3. Reference measurements of outgassing, recycling, and retention after D plasma loading: absolute content and composition in W and reference samples
  2024: Analysis of D in Magnum-PSI loaded coatings (publication of results)
4. (CF-)LIBS on Be containing coatings with different type of fuel content
  2024: participation in LIBS JET campaign and preliminary tests in VTT.
  (publication of previous VTT campaign results)
Chart: LIBS shot nr
 | 308.6349 | 341.3106 | 722.3646 | 507.7134 | 313.7811 | 142.8422 | 169.8887 | 68.7071 | 147.3241 | -1.8255 | 87.3232 | 114.6419 | 142.9188 | 94.9685 | 50.8822 | -27.3586 | 45.4954 | 30.0853 | 69.3092 | -8.133 | 17.4674 | 15.739 | 83.5167 | -5.3543 | -23.9793 | -20.5811 | 5.5488 | -75.3393 | -21.9812 | -34.0644 | 19.5547 | 71.2586 | -22.0719 | -6.4432 | -62.6096 | -120.3636 | -3.134 | 9.7801 | -19.6742 | -17.4394
 | -77.7715 | 236.3946 | 237.3977 | 220.0475 | 879.5004 | 581.3049 | 866.0505 | 715.6683 | 1103.2894 | 861.6737 | 1023.9452 | 990.3148 | 1113.6402 | 1032.4224 | 993.2487 | 887.8537 | 1241.6563 | 1039.1853 | 1532.2958 | 1113.5029 | 1316.1838 | 1472.7328 | 1451.1683 | 1306.2931 | 1474.0798 | 1685.1781 | 1529.8958 | 2036.8805 | 1688.6963 | 2177.8496 | 1941.7796 | 1779.2566 | 1538.5596 | 2021.1298 | 1832.7143 | 1940.7334 | 2068.9857 | 2102.0527 | 2189.0785 | 1828.2257
 | 7425.3869 | 2991.4266 | 3001.3392 | 2847.659 | 3364.6745 | 5653.2341 | 5562.032 | 5148.6899 | 3901.9517 | 4195.6368 | 4091.7909 | 3987.3679 | 3670.6801 | 2993.2227 | 3457.3152 | 3577.8979 | 3185.9568 | 2986.1585 | 2119.831 | 2034.1981 | 2058.7653 | 1799.4652 | 1877.3313 | 1417.6923 | 2381.3747 | 1400.2669 | 1262.0113 | 896.2504 | 1003.4494 | 1128.9072 | 702.0813 | 649.7776 | 297.6813 | 282.4735 | 512.4985 | 64.8828 | -281.3539 | 266.8979 | -67.5897 | 733.2593
1 μm c-W D2-N2
5 μm c-W D2-N2
Chart: LIBS shot nr
1 μm c-W
Chart: Crater nr
 | 63.5409 | 61.8448 | 43.9546 | 36.9256 | 35.8366 | 53.9898 | 73.1352
 | 100.9387 | 52.3104 | 47.3202 | 40.0154
5 μm c-W
Chart: Crater nr
 | 13.8437 | 15.011 | 14.6213 | 15.8308 | 15.975 | 16.3038 | 17.1146
 | 6.7374 | 7.1588 | 4.7048 | 3.2704
Depth profiles of D, W and Mo
D spatial distribution on coating

## Slide 4: H isotope detection at different pressures
Chart: FWHM (nm)
| 0.27 | 0.21999999999999997 | 0.20250000000000001 | 0.20250000000000001 | 0.18 | 0.20500000000000002 | 0.17750000000000002 | 0.16500000000000001 | 0.14500000000000002 | 0.125 | 0.11499999999999999
 | 1990.2436 | 1832.0331 | 1645.4643 | 1585.0228 | 1369.8842 | 1471.4401 | 958.6645 | 730.9787 | 566.2268 | 466.4597 | 396.1048
 | 16153.0304 | 9861.7688 | 7269.5219 | 5085.5031 | 4432.3897 | 4425.153 | 2243.515 | 1392.2435 | 1130.5665 | 917.5425 | 751.8243
 | 2079.4052 | 1288.4765 | 848.0675 | 572.3307 | 425.9392
 | 2117.3944 | 169.5427 | 44.927 | 16.2819 | 12.5496
 | 13225.6119 | 9994.5927 | 5831.4602 | 4436.1571 | 1099.5477 | 360.343 | 204.2206 | 83.5162
 | 640.1796 | 568.4599 | 490.3062 | 514.5294 | 521.6673 | 267.0069 | 157.4584 | 93.8242 | 59.5476
Chart: Distance (mm)
| 0.5 | 1 | 1.5 | 2 | 2.5 | 3 | 3.5 | 4 | 5
 | 0.095026 | 0.55728 | 1.0041 | 0.57465 | 0.55218 | 0.036895 | 0.038378 | 0.02353 | 8.5646e-05
 | 0.0029957 | 0.0047899 | 0.0089842 | 0.039951 | 0.17062 | 0.35243 | 0.70219 | 0.87927 | 0.99996 | 0.93066 | 0.44225 | 0.0049094
Chart: Distance (mm)
| 0.5 | 1 | 1.5 | 2 | 2.5 | 3 | 4 | 5 | 6 | 7 | 8
 | 0.23436 | 0.6353 | 1.0012 | 0.98537 | 0.61138 | 0.29328 | 0.15514 | 0.090817 | 0.033036 | 0.0035504 | 0.00017699
 | 0.0022126 | 1.9493e-05 | 0.0022694 | 0.0088276 | 0.057037 | 0.1746 | 0.45882 | 0.86851 | 0.9994 | 0.42637 | 0.08976
Chart: Distance (mm)
| 0.5 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14
 | 0.1487 | 0.46242 | 0.85249 | 0.87084 | 0.91644 | 0.99981 | 0.76593 | 0.5494 | 0.30918 | 0.12142 | 0.031871 | 0.010322 | 0.0051962 | 0.0043521 | 0.0010513
 | 0 | 0.0068701 | 0.018597 | 0.12858 | 0.42624 | 0.7669 | 1 | 0.83964 | 0.73964 | 0.13678 | 0.081486 | 0.0029451 | 0 | 0.0021964 | 0
Chart: Distance (mm)
| 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10
 | 0.043227 | 0.43867 | 0.87612 | 0.99909 | 0.70002 | 0.33911 | 0.19553 | 0.12318 | 0.031931 | 0.018569 | 0.0069728
 | 0.0002381 | 0.37392 | 0.41373 | 0.5954 | 0.28246 | 0.88925 | 0.89945 | 0.98738 | 0.98738 | 0.48351 | 0.63959 | 0.23977 | 0.0063958
Chart: Distance (mm)
| 0 | 0.5 | 1 | 1.5 | 2
 | 0.27153 | 0.77913 | 1.0001 | 0.74115 | 0.14869
 | 6.9784e-05 | 6.9784e-05 | 0.073336 | 0.19429 | 0.7969 | 1.0003 | 0.67884 | 0.52516 | 0.31454
Chart: Distance (mm)
| 0.5 | 1 | 1.5 | 2 | 2.5 | 3 | 3.5 | 4 | 4.5
 | 0.78758 | 1.001 | 0.36591 | 0.037448
 | 0.057969 | 0.17683 | 0.44173 | 0.9384 | 0.99994 | 0.5817 | 0.44566 | 0.19805 | 0.042661
H and Mo intensity as the function of distance from target at 1 μs
N2
Ar
Intensity vs FWHM at different pressures in Ar and N2