## Slide 1
R&Ds for Fusion Reactor Materials at SWIP
Presented by：CHEN Jiming
Southwestern Institute of Physics, Chengdu, China
Co-authors:
PENGFEI ZHENG, LONG ZHANG, YOUYUN LIAN, PINGHUAI WANG, JUAN DU, LONG WANG, Fusion Reactor Material Research Team at SWIP;

## Slide 2
Outlines
1. Introduction
2. Material strategies for reactors
3. Progress of material researches
3.1 W-base PFMs
3.2 CLF-1 RAFM steel
3.3 V-base alloy
3.4 Tritium-breeding materials permeation barrier
3.5 Neutron irradiation tests
4. Summary

## Slide 3: Scopes
SWIP has been focused on materials for in-vessel components for > 35 years.
Structural material for blanket and divertor, including ITER TBM
PFMs for FW and divertor
Tritium breeders and n-multipliers
Tritium permeation barrier
For ITER FW and shielding blocks
Copper alloys for ITER FW and DEMO divertor
1

## Slide 4: List of the materials and technologies
PFMs
B-, Si-doped Gs for Tokamak
VHP-Be from ITER
CVD W coating (0.5mm/h)
W-K, W-Y2O3
W-Ta alloy
Liquid metal surface
Large-scale ingots
RT ductility
High recrystallization temp.
Thermal shock test
W/Cu brazing & HIP joining
Thermal fatigue performance
Structural mateials
316L with Ti-modified
HT-9, HT-7 ferritic steel
CLF-1 RAFM steel
ODS-RAFM steel
V-W-Ti, V-Ti-Al, V-4Cr-4Ti
CDS-V4Cr4Ti
Large-scale products
Neutron irradiation
Mechanical strength
thermal creep / fatigue
Corrosion in liquid Li / He
Electron irradiation damage
Heat sink materials
CuCrZr alloy
ODS-Cu
Strengthening
Bonding techn.
Functional mater.
Li4SiO4 pebbel
Be pebbles
Pebble bed
Compatibility with RAFM steel
......
2

## Slide 5
1. Introduction
2. Material strategies for reactors
3. Progress of material researches
3.1 W-base PFMs
3.2 CLF-1 RAFM steel
3.3 V-base alloy
3.4 Tritium-breeding materials permeation barrier
3.5 Neutron irradiation tests
4. Summary
3

## Slide 6: Map for neutron irradiation
FPP (2050~ )
Max. > 200 dpa
~2050 in operation
ITER
（2038~2052 ？）
Material for TBM & W FW
1~2 GW DEMO
(2040~ )
HL-3 Tokamak
DT, Material with fusion n
Test Reactor
(2035~ )
Steady burning
T self-sustaining
Max. 10~20dpa
HFETR
Fission neutron
7~8 dpa/y
D+→Li or D+→T (under design) Fusion neutron sources (10 dpa/FPY, 2~10 appm He/dpa)
Fast reactor (2035~ )
30~50 dpa/FPY
Maximum 50~100 dpa
200~300 dpa
4
<100 dpa
<50 dpa
3~4 dpa
> 50 dpa
10~20 dpa
> 20 dpa
? dpa
? dpa
Material changes? limited volume for material irradiation of the fusion neutron source?

## Slide 7: Fusion neutron source under design
Mission: to verify other irradiation, to provide support for test reactor.
Similar the one in US, to be constructed from 2024~2028.
D-T source: 300kV 100mA D+, 100 kPa T gas target.
Neutron fluence: 2.67×1016 n/s.
To provide an ~60 cm3 volume, ~10 dpa/FPY for materials test.
5
Considering more material to be irradiated and high dose irradiation demand, more fusion neutron sources are required.

## Slide 8: Missions for a test reactor before DEMO
500~600 MW, 20~30% duty factor, 3~5 dpa/FPY, as a fusion neutron source to test its materials and those for DEMO.
Deasign based on fission neutron irradiation, together with a fusion neutron source for verification
Blanket & divertor structure: CLF-1 RAFM steel (reuqire >20 dpa data)
PM W and CuCrZr as PFM and heat think ( require > 2~5 dpa data)
Develope materials to large scale for reactor component.
Develope material technologies for components, such as W/CuCrZr
To establish correlation between fission and fusion neutron irradiation.
6

## Slide 9: Material approches for DEMO and FPP
HFTER fission neutron to 50~100 dpa for DEMO;
D+ accelerator type neutron source to varify the fission neutron irradiation results, together with test reactor results
FPP, too high dose to be reached by fusion neutron sources, assuming to use fast reactor (in plan) for the purpose.
CLF-1 RAFMs as the major structural materials for DEMO, Partially ODS or V4Cr4Ti alloy, aimed at future use in FPP;
W-K or Wf/W as the major PFMs; Cu alloy or ODS-Cu as heat sink;
Supposing no material capable for > 200 dpa fusion neutron irradiation—— no higher dose irradiation test is required. In-situ annealing to recover irradiation damage should be investigated (with its demonstration in test reactor and DEMO).
7

## Slide 10
1. Introduction
2. Strategies for various reactors
3. Progress of material researches
3.1 W-base PFMs
3.2 CLF-1 RAFM steel
3.3 V-base alloy
3.4 Tritium-breeding materials permeation barrier
3.5 Neutron irradiation tests
4. Summary
8

## Slide 11: 3.1 W-base PFMs and mock-ups technologies
40 kg/pc,
Swaged W-Y2O3 and W-K bars
Aiming at large-scale W alloy with RT ductility and >1600℃ recrystallization;
High strength ODS-Cu developed;
Brazing W (alloy)/CuCrZr for mono-block and flat moch-ups.
(see report from Dr. LIAN Youyun, day 2)
SWIP: Cu Casting + Vacuum Brazing Tech.
W/OFCu joints
Flat W Mock up, 15MW/m2, 300 cycles
Mono-block
20MW/m2 Tolerability.
Divertor unit with HVT cooling
6mm W
9

## Slide 12: 3.2 CLF-1 RAFM steels
  Database established
  Physical & tensile properties @ RT-650℃
  Impact properties @ -120℃ ~ RT
  Aging @ 550℃ & Creep tests, up to 10,000 hrs
  Fatigue @ RT-600℃, million cycles
  Neutron irradiation: on-going to 28 dpa
  Spallation neutron irradiation >20 dpa
  Ion irradiation to 200 dpa.
Forging
Forged Bars
10-55mm Plates
Engineering qualification completed.
(See report from Dr. ZHANG Long, Day 3)
Various welding technologies developed, including TIG, Laser, EB, HIP bonding, friction stir welding. etc.
Friction stir welding
10

## Slide 13: CLF-1/ W bonding FW technologies
HIPed
(Fe2W)
HIPed+NHT
(Fe2W+C)
HIPed+THT
(Fe2W+Fe3W3C)
HIPed. NHT & THT
NHT: 980℃/45min + Air Cooling,
THT: NHT+ 740℃/90min+ Air Cooling
HIP bonding joint at 900℃ / 150 MPa
HHFT at 1MW/m2,1000 cycle: 70℃ water cooling
Stable bonding strength: > 250 MPa
(by RT shear test)
11

## Slide 14: 3.4 Development of vanadium alloy
Flowchart of vanadium alloy preparation
(a)
(b)
Three ingot, 34.6 kg for each
17.5kg vanadium alloy hot-rolled plate from each ingot.
Ingot casting
Hot forging
Hot rolling
Heat treatment
V4Cr4Ti alloy product in 100 kg scale
12

## Slide 15
The total highly active elements: < 150wppm;
C + N + O: < 210 wppm.
Good impurities control and high strength at elevated temperature
Element
Ingot
Hot-rolled plate
RT TE: 30%, ~340 MPa strength to 700℃
13

## Slide 16
V-4Cr-4Ti
Powder Process
Ball-milling
Sintering
Casting molding
Ball-milling
HIP Sintering
Hot rolling
Plasma Rotating Electrode
V-4Cr-4Ti + MAX Phases
Sample | Cr | Ti | C | N | O
Original | 4.22 | 4.26 | 0.0041 | <0.002 | 0.025
Casting | 4.23 | 4.68 | 0.0042 | <0.002 | 0.044
Powders | 4.16 | 4.66 | 0.0059 | <0.002 | 0.050
Table1: Chemical composition test /wt.%
MAX Phases Dispersion Strengthened V-4Cr-4Ti Alloy
Good impurities control & much better thermal creep property.
14

## Slide 17
Vanadium first wall technologies
Nuclear heating：27MW/m3；Coolant flow：100m/s；In/outlet temp.:400/490℃
Pressure drop: 0.14MPa
V4Cr4Ti/W diffusion bonding developed, > 100 MPa
Equivalent strain (%)
Equivalent stress
at 8MPa + Temp. field
Temperature map
at 1 MW/m2
399~709℃
 510 MPa
 0.71%
15

## Slide 18
Reliable diffusion-bonding with RAFMs and CDS-V4Cr4Ti
V4Cr4Ti
CDS-V
CDS-V
Interface
Position (mm)
Hardness (HV)
V4Cr4Ti
CDS-V
Interface
100μm
V4Cr4Ti
CDS-V
RT shear bonding strength > 300 MPa
CLF-1 RAFM steel
SWIP-30
V4Cr4Ti
CDS vanadium alloy
V4Cr4Ti-1.5Y-0.3Ti3SiC2
Good HIP diffusion bonding V4Cr4Ti/RAFMs and V4Cr4Ti-melted /CDS-V4Cr4Ti.
Bonding strength > 240 MPa achieved.
Tritium permeation under investigation.
16

## Slide 19
He-cooling W/V4Cr4Ti/CLF-1 FW mock-up
Water-cooling W/V4Cr4Ti/CLF-1 FW mock-up, with equivelent stress and Maxi. temperature
V4Cr4Ti mock-ups for FW
Reliable materials bonding
No UT indication of defect
No damage at 1.25 MW/m2 for 1500 cycles.
2mm-thick W, >700℃ of V4Cr4Ti
EMS-400 at SWIP for HHFT, to be updated to 800 kW
17

## Slide 20: 3.4 T-breeding materials
Ceramic: Up to 10kg / batch.
New facilities for Li4SiO4 in SWIP.
Physical & mechanical properties measured.
(see report from Dr. ZHANG Long, day 3)
Beryllium pebbles
Li4SiO4 pebbles
Li4SiO4 producing facility (new in SWIP)
Beryllium fabrication facility
8500mm
Li-Pb loop 300-550℃, 0-5m3/h
Into operation by 2025
Superconductor Magnet
Ha:0-104
Magnetic filed B: 0-4T
200*500*500mm3
Liquid LiPb
Loop under construction, for (1) MHD study, (2) Material corrosion test, (3) heat transfer, etc
18

## Slide 21: Hydrogen isotopes permeation— facilities
Comprehensive hydrogen analysis platform (CHAP) at SWIP
Gas driven permeation systems
Hydrogen permeability, diffusion coefficient
High downstream vacuum (10-8Pa)
High heating rate (W heater)
Tubes and module testing
Distinguish He and D (ongoing)
Thermal desorption spectrum (TDS)
Hydrogen retention amount
Hydrogen desorption temperature
High temperature for W
Distinguish He and D (ongoing)
in situ testing after D He implantation
(ongoing)
N/O/H analysis instrument
Hydrogen amount in materials
H test scope (0.08ppm-2500ppm)
Precision (0.04ppm or 0.4%RSD)
In situ testing design
Gas chromatography
H2 content in Ar
H2 content in He
He content in Ar
He content in H2
Test scope (＞20ppm)
Small atoms analysis
(H、D、T、He、Li)
Laser-induced breakdown spectroscopy
Depth distribution of H and Li
＞10ppm
Spectral resolution of 0.1nm（FWHM）
Wavelengths of180nm-1100nm
19

## Slide 22: Progress on Hydrogen isotopes permeation
Hydrogen traps density of RAFM (CLF-1) steel was evaluated by electrochemical method.
Fusion Engineering and Design 201 (2024) 114280
Corrosion of RAFM (CLF-1) steel by Li2TiO3 and Li4SiO4was studied.
Corrosion product with a double layered structure decreased the deuterium permeability
Fusion Engineering and Design 173 (2021) 112856
Electrolytic cell for Hydrogen permeation
Hydrogen permeation test under corrosion can be achieved.
Annealing decreased hydrogen traps
Irreversible hydrogen traps in CLF-1
20

## Slide 23: Progress on Hydrogen isotopes permeation
Tritium permeation barrier with high corrosion resistance are being stuied.
Al2O3 composite coating with high irradiation resistance was developed.
Al2O3 composite coating was complete after 50 dpa Au+ irradiation.
Preparation of ZrN, Al2O3 etc. coating
Al2O3 composite coating behaved good hydrogen resistance after irradiation.
Al2O3 coating can protect CLF-1 from being corroded by Li4SiO4 with the formation of LiAlO2.
Surface & Coatings Technology 410 (2021) 126960
21

## Slide 24: 3.5 Neutron irradiation
N Fluence (E>1MeV): 2.5E+14 n/(cm2.s)
Specimens
Al tube
Capsual
Fillers
Fuse wire
to monitor temperature
Nuclear heating up specimens
Miniature specimens:
Tensile, bending, Charpy, TEM discs, etc.
22

## Slide 25
7 and 14 dpa irradiation completed.
Data available in this year.
Bi-Sb fuse wire developed for temperature monitoring from 300~600℃
HFETR Neutron irradiation progress
An ODS steel to 7 dpa:
Irradiation hardening,
Reduction in ductility
Bi-Sb alloy stub for temp. monitoring.
(Sb content →)
23

## Slide 26: Summary
24
Great challenge for fusion reactor materials, a step-by-step approach is supposed.
SWIP is heading forwards to actual nuclear fusion, including DT operation of HL-3, an engineering test reator and a D-T neutron sources to solve the material issues.
Materials are scaling up for reactor construction, focusing on material data base construction, neutron irradiation test and material technologies for in-vessel components.

## Slide 27
Thanks for listening!
Questions or Comments?