## Slide 1
EU DEMO Divertor: Design revision and R&D
Jeong-Ha YOU
on behalf of EUROfusion DEMO Divertor team
4th Technical Exchange Meeting on the China-EU Collaboration on CFETR and EU-DEMO Reactor Design
19-22.03.2024

## Slide 2
EU-DEMO 2020 baseline (Pfus: 2 GW, Psep: 154 MW, : ~0.8, PNH: ~8 W/cm³ max.)
Power to exhaust (to be revised in 2024: DEMO-A)
nuclear: 139 MW, particle: 122 MW, radiation: 78 MW
Peak power density at the SP: ~20 MW/m² (bevelled surface: ~13 MW/m² nominal q)
Required shielding for the VV: ≤ 1 dpa/6 fpy
Specified lifetime: ≥ 1.5 fpy
Reduced activation (no HLW), ILW allowed (ALARA)
R.A.M.I. + recyclability
EU DEMO Divertor: high-level requirements
2
48 cassette modules, 16 lower ports

## Slide 3
Pre-conceptual design phase (2014-2020)
deliver a first feasible design concept compatible with the DEMO requirements (done)
2. develop & verify high-heat-flux technologies for the targets (done)
EU DEMO Divertor: objectives
3
Conceptual design phase: 1st stage (2021-2023)
explore alternative design options to enhance RAMI (done)
2. launch key technology R&D for the entire cassette/PFCs system (done)
Conceptual design phase: 2nd stage (2024-2027)
define & verify baseline design with justification
2. demonstrate manufacturing technologies with small/medium-scale mock-ups

## Slide 4
EU DEMO Divertor: architecture
Baseline 2 (as of 2023): DEMO-A
- Water-cooled (single-phase)
- Dual cooling circuits (CB/VT)
- Parallel circuit for IVT/OVT
- PWR cooling for the steel CB
- ITER-like HHF technology (LT coolant)
- XPR / MD / reattachment considered
- Suppressed ELMs
ITER-like target (Baseline 1)
Block width: 23 mm (ITER: 28 mm)
Armor thickness: 8 mm (ITER: ~7 mm)
Block thickness: 12 mm
W
CuCrZr
4
W block: stress mostly strain-controlled (not load-controlled)
 UTSirr is more relevant than (pseudo)ductility/toughness
J.H. You et al., FED (2022)

## Slide 5
Baseline design I (as of 2020): water-cooled (separate dual cooling circuits)
Cassette body/shielding liner: EUROFER97 (180-210 °C, 3.5 MPa)
2. Target: W monoblocks/Cu pipe (130-137 °C, 5 MPa)
EU DEMO Divertor: design baselines
5
Technology R&D topics: (2021-2027)
Cassette body: joining (welding/HIP), AM, fixation units, pipe joining, insulation
2. Target: W wire-Cu composite pipe, support unit (steel), fixation, baffle, end cap, armor shaping
corrosion protection, swirl tape fretting, laminate W armor block (UTSirr?)
3. Shielding liner/dome: W coating, joining (welding/HIP)
Baseline design II (as of 2024): water-cooled (separate dual cooling circuits)
Cassette body: EUROFER97 (295-328 °C, 15.5 MPa)
2. Target: W monoblocks/Cu pipe (140-147 °C or 150-157 °C, 7.5 MPa)

## Slide 6
EU DEMO Divertor: cooling issues (cassette body: EUROFER steel)
Baseline 1 (as of 2020)
- Coolant temp. in CB: 180 - 210 °C
- Solid temp. in CB: 200 - 555 °C
Baseline 2 (as of 2023)
- Coolant temp. in CB: 295 - 325 °C
- Solid temp. in CB: 315 - 670 °C
Regions where
temp. > 550 °C
Too cold (embrittled)
Optimal (ductile)
Too hot (softened)
6
ODS EUROFER/HT EUROFER: low TRL, weldability? code/MPH (irrad.)?
J.H. You et al., FED (2022)

## Slide 7
allowable cooling regime
for 10 - 20 MW/m²
(≤ 16 m/s, CHF margin: ≥ 1.4)
monoblock width: 26 mm
armour thickness: 6 mm (shaped)
pipe thickness: 2 mm
peaking factor: 1.7
EU DEMO Divertor: cooling issues (new design space)
1900°C
D. Marzullo, A. Quartararo, FED (2024)
1.4
1.2
1.0
150 °C
7

## Slide 8
allowable cooling regime
for 10 - 20 MW/m²
(≤ 16 m/s, CHF margin: ≥ 1.2?)
1.4
1.2
1.0
EU DEMO Divertor: cooling issues (new design space)
8

## Slide 9
EU DEMO Divertor: cooling issues (target: CuCrZr pipe)
130/140°C 174/183°C - 293/302°C ~430/440°C
loss of ductility reduced strength
(cooling) (10 MW/m²) (20 MW/m²)
optimal range
(250°C - 300°C)
20 MW/m²
10 MW/m²
Operation temp. range of the cooling pipe
Baseline 1 (as of 2020)
- Coolant temp. in VT: 130 - 137 °C
- Solid temp. in VT pipe: 174 - 293 °C (10 MW/m²)
213 - 431 °C (20 MW/m²)
Baseline 2 (as of 2023)
- Coolant temp. in VT: 140 - 147 °C
- Solid temp. in VT pipe: 183 - 302 °C (10 MW/m²)
218 - 436 °C (20 MW/m²)
Too cold (embrittled)
Optimal (ductile)
Too hot (softened)
Pipe: ODS copper? (loss of toughness at HT, embrittlement at LT irradiation, swelling by deoxidiser?, anisotropy, low MTRL)
9
He: ~60 appm/fpy
(effects not saturated)
~7 dpa/fpy (effects saturated?)
J.H. You et al., FED (2022)

## Slide 10
No crack found (in all 292 tested monoblocks)
Remained fully intact (at least up to 2000 cycles)
Surface damage insignificant (at least up to 2000 cycles)
J.H. You, J. Nucl. Mater. (2021)
1st pulse
500th pulse
H beam irradiation (GLADIS) with short pulses (10s)
1
2
3
4
G. Pintsuk, J.H. You et al., NME (2024)
1: 20 MW/m2, 10 s / 10 s, 200 cycles
2: 20 MW/m2, 300 s / 10 s, 200 cycles
3: 20 MW/m2, 600 s / 10 s, 200 cycles
4: 20 MW/m2, 120 s / 10 s, 1000 cycles
e- beam irradiation (JUDITH2) with long pulses
Effect of focused e- beam scanning?
New tests with a larger beam spot in plan
High-heat-flux performance: ITER-like tungsten monoblock target (20 MW/m2)
10
500 cycles
2000 cycles
(HADES)

## Slide 11
Irreversible microstructural change unavoidable regardless of metallurgy or grades
Recrystallization or grain growth is not necessarily a cause of crack initiation
J.H. You, et al. JNM (2021)
High-heat-flux performance: ITER-like tungsten monoblock target (20 MW/m2)
J.H. You, Nucl. Mater. Ener. (2022)
11
dpa damage present?
H/He outgassed?
Re/dpa effect?

## Slide 12
Neutral H beam, GLADIS (MPG-IPP)
12
25 MW/m², 500 cycles (longitudinal cut)
ENEA 23
(coolant: 20 °C)
High-heat-flux performance: ITER-like tungsten monoblock target (25 MW/m2)
J.H. You, Nucl. Mater. Ener. (2022)
Tmax: 2500 - 2700 °C

## Slide 13
High-heat-flux performance: ITER-like tungsten monoblock target (25 MW/m2)
J.H. You, Nucl. Mater. Ener. (2022)
Tmax: 2500 - 2700 °C

## Slide 14
High-heat-flux performance: ITER-like tungsten monoblock target (25 MW/m2)
J.H. You, Nucl. Mater. Ener. (2022)
14
Surface temperature matters!
(heat loads, armour thickness, thermal conductivity: no internal barriers)

## Slide 15
500 pulses
1000 pulses
2000 pulses
4000 pulses
5000 pulses
(µm)
350
280
210
140
70
0
Front face roughness (laser profilometry)
IR thermography
5000 pulses
500 pulses
H beam (GLADIS)
Pulse: 0.4 s (transient)
Pause: 1.2 s
0.63 Hz
High-heat-flux performance: ITER-like tungsten monoblock target (40 MW/m2)
J.H. You, Nucl. Mater. Ener. (2022)
15

## Slide 16
H beam (GLADIS)
Pulse: 0.4 s
Pause: 1.2 s
0.63 Hz
No armour crack found
Structural integrity remained intact
Similar recrystallization feature as the 20 MW/m² load case
No abnormal grain growth
High-heat-flux performance: ITER-like tungsten monoblock target (40 MW/m2)
J.H. You, Nucl. Mater. Ener. (2022)

## Slide 17
EU DEMO Divertor: technology R&D activities
Wire-reinforced composite pipe
& target
Plasma-sprayed W coating
PFC insulation
HRP/Brazing
HIP (9Cr steel)
9Cr steel
Additive manufacturing (LPBF/WAAM)
Ti alloy
W lattice
9Cr steel
CuCrZr
W
Cu
9Cr steel
Welding
Corrosion protection coating
DLI-MOCVD
Pipe joining
17

## Slide 18
Flow-assisted corrosion: CuCrZr cooling pipe
Exposure time: 425 h
Flow rate: 9 m/s (80 bar)
Temperature: 250 °C (water/Cu)
Dissolved O2: 5 ppm O2 (in effluent)
Erosion rate: 20 µm (~600 µm/fpy)
Exposure time: 828 h
Flow rate: 9 m/s (80 bar)
Temperature: 250 °C (water/Cu)
Dissolved O2: <0.01 ppm (in effluent)
Dissolved H2 4 ppm (in effluent)
Erosion rate: < 0.1 µm (~1 µm/fpy)
J. Öijerholm et al, Nucl. Mater. Ener. (2023)
18
Oxidizing medium
Reducing medium

## Slide 19
Baseline design I (completed: frozen as it is)
Cassette body/shielding liner: justification for semi-brittle steel, lifetime/waste, nucleate boiling
2. Target: uncertainty in heat loads, long-pulse, justification for brittle pipe, He transmutation (Cu)
Summary: status & outstanding issues
19
Technology R&D (launched recently: long-term program)
Cassette body: low TRL, design-dependent, irradiation/PIE
ITER-like target: new design, advanced target (low TRL), irradiation/PIE (HHF test): mock-up test?
3. shielding liner/dome: low TRL (options t.b.d.)
4. DDC/MPH/SSTT/IRRAD for the baseline materials (critical basis for design)
Baseline design II (in progress: design dossier due by Q2 2025)
Cassette body: nucleate boiling, local hot spots (> 550 °C), creep-fatigue, semi-brittle rule (< 350 °C)
2. Target: the same issues as in baseline l, design modification (dimensions, shaping), refurbishment
(BR2/JUDITH3)

## Slide 20
DEMO Central Team
(Plant System Design, Plasma)
Divertor Target
Technology R&D
Divertor Cassette
Architecture design
Limiter PFCs
Design/Technology R&D
Corrosion test
& protection
Divertor Cassette
Technology R&D
EU DEMO Divertor: project organigram
High-heat-flux Testing
Structural Integrity
WPDIV-DEMO
WPDIV
(IDTT, W7X, JT-60SA)
20
Laboratories (EUROfusion RUs)
Universities (EUROfusion LTP)
Industry partners,
External collaborators

## Slide 21
21
D. Terentyev, NF (2022)