## Slide 1
Divertor Design in BEST
Rui Ding, Xuebing Peng for the BEST team

## Slide 2
CONTENTS
Requirements and Considerations
Physics basis
Engineering design
Summary
2

## Slide 3
Requirements on Plasma Exhaust Solution for BEST
Main requirements
  High heat load on divertor target (PSep/R ~14)
  Efficient particle exhaust for long pulse operation
  Reliable and robust operation
  Remote handling maintenance
Limits on Physics parameters
  Ppeak ≤ 10 MW/m2
  Te ≤ 5-10 eV
  Zeff, sep < ~ 2.5
  CHe, sep < ~ 3%
3

## Slide 4
The Conventional Divertor Design
A V-shape corner
  Higher neutrals compression
  Same heat exhaust ability of vertical target and reflector plate
Flexible OSP locations for the outer divertor
  Slope target: recycling of neutrals towards the SOL for deeper detachment
  Vertical target: easier detachment near strike point
Pumping slot at the outer corner
W-based materials for PFCs
  Impurity seeding for power dissipation
4

## Slide 5
CONTENTS
Requirements and Considerations
Physics basis
Engineering design
Summary
5

## Slide 6
Modeling of Edge Plasma for BEST Using the SOLPS-ITER
Simulation setup
  PCEI= 50MW (Q>5), Pe=Pi
  Transport coefficients for H mode condition
  Impurity puffing at outer divertor: Ne/Ar
  D2 puffing from upstream
  Different strike point locations: Slope target / Vertical target
  Drift effects included
D2 puff
Ne, Ar
𝝀𝒒 ~ 1.0mm
Pump
6

## Slide 7
Higher Power Dissipation and Core Contamination by Ar seeding
Upstream
Downstream
Radiation can be increased by higher impurity seeding rate and fueling rate, Zeff can be effectively reduced by enhancing D2 puffing
Much higher Zeff and Lower upstream pressure by Ar Seeding
  Lower heat flux and Te at the target
Vertical targets
7

## Slide 8
Higher Power Dissipation and Core Contamination by Ar seeding
Radiation fraction in the core plasma is much higher for Ar seeding even with lower seeding rates
  6% for Ne, 26% for Ar
  2 times Zeff in the core for Ar
Vertical targets
ΓD2=5.0×1022/s, ΓNe=6.0×1019/s
ΓD2=5.5×1022/s, ΓAr=3.0×1019/s
Prad= 24.8MW
PCore=0.8MW
Prad= 27. 3MW
PCore=6.8MW
8

## Slide 9
Higher Power Dissipation and Core Contamination by Ar seeding
Inner target
Outer target
Deeper detachment at the inner target than the outer target
  Higher Te at the far-SOL region at the outer target
Vertical targets
9

## Slide 10
Upstream
Downstream
Full detachment for slope target and partial detachment for vertical target achieved with Ne Seeding
Low core contamination can be maintained with full detachment slope target
Ne seeding
Deeper Detachment for Slope Target Compared to Vertical Target
10

## Slide 11
Ne seeding
ΓD2=3.0×1022/s, ΓNe=5.0×1019/s
Prad= 27.7MW
PCore=1.5MW
Prad= 24. 8MW
PCore=0.8MW
Deeper Detachment for Slope Target Compared to Vertical Target
ΓD2=5.0×1022/s, ΓNe=6.0×1019/s
slope
Vertical
Power radiation is higher for slope target even with lower seeding rates
  Similar upstream profiles for both targets
11

## Slide 12
Inner target
Outer target
Deeper Detachment for Slope Target Compared to Vertical Target
Slope target enhance the buildup of neutral density near the strike point and the far-SOL region
  Pumping requirements: ~65 Pa m3/s
Ne seeding
12

## Slide 13
Evaluation of W Erosion Rate and Core Contamination
DIVIMP modeling with background plasma from SOLPS
  Much higher W erosion rate and impurity concentration for vertical target
  W concentration is below the limit for all the cases
  Slope target has a longer target lifetime
cW, sep = 5.4x10-7
Ne
vertical target
cW, sep = 2.2x10-9
Ar
vertical target
W net erosion rate
 | Ne slope ΓD2=3.0×1022/s ΓNe=5.0×1019/s | Ne vertical ΓD2=5.0×1022/s ΓNe=6.0×1019/s | Ar vertical ΓD2=5.5×1022/s ΓAr=3.0×1019/s
Target lifetime | s | s | s
 | Ne slope ΓD2=3.0×1022/s ΓNe=5.0×1019/s | Ne vertical ΓD2=5.0×1022/s ΓNe=6.0×1019/s | Ar vertical ΓD2=5.5×1022/s ΓAr=3.0×1019/s
Target lifetime |  |  | 
W density
13

## Slide 14
BOUT++ nonlinear modeling suggests different ELM regime for Q>1 scenario and Q>5 scenario
Q>1 scenario
  Grassy ELM, ΔW/W ~ 0.2%
  ~56 MW/m2, ~0.2ms
Q>5 scenario
  Type-I ELM, ΔW/W ~ 4%
  ~628 MW/m2, ~0.5ms
Estimation of ELM Type and Transient Heat Flux
Q>5
Q>1
14

## Slide 15
CONTENTS
Requirements and Considerations
Physics basis
Engineering design
Summary
15

## Slide 16
Overall Design
Overall features
  PFU: integrated design with flat type and monoblock
  All PFCs are actively cooled
  PFCs separately maintained (IVT + Dome , OVT).
Main parameters | 
Toroidal degree | 7.5°
Quantity | 48
L, W and H | 2.0×(0.28-0.56)×1.02 m
Deadweight | ~1.6 t
Design heat flux of PFU/PFC | 15 MW/m2/10 MW/m2
Shielding structure
(45° in toroidal)
Divertor (7.5° toroidally)
48 divertors (360°)
16

## Slide 17
PFU with Monoblock and Flat-type
  Strike zone: monoblock, non-strike zone: flat type.
  DOME is similar to non-strike zone of IVT/OVT PFU.
  Interface: explosive welding R120, ribs to strength the structure.
Monoblock
Flat-type
~614mm
~51mm
Tungsten
Copper
CuCrZr
316L
Design of PFU
17

## Slide 18
Total mass flow rate is 10.3 kg/s, total pressure drop of Divertor, IVT & Dome and OVT are about 1.85 MPa, 0.72 MPa and 0.78 MPa, respectively.
Flow distributions within each branch channels of IVT and OVT are acceptably uniform, the average deviations of IVT and OVT are about 6.28 % and 0.96 %.
Design of Cooling Circuit for PFCs
inlet
outlet
1
inlet
2
3
4
5
6
7
8
1
2
3
4
5
6
10.3 kg/s
Coolant flow direction
∆P = 1.85 MPa < 2MPa
Velocity in the high heat flux zone
@ OVT: ~ 8.5 m/s
@ IVT: ~9.5 m/s
@ Dome: ~ 7.8 m/s
8-10 m/s
Meet requirement
18

## Slide 19
Monoblock shaping
  Toroidal chamfer: 0.5 mm
Design of shaping for PFCs
 | Location | Dimension | Tolerance
Toroidal gap dimension | Inter-PFU | 1 mm | ± 0.2 mm
 | Inter-cassette | 10 mm | ± 2 mm
Radial step | Inter-PFU | -0.5 mm | ± 0.3 mm
 | Inter-cassette |  | ± 2 mm
Monoblock Shaping, radial misalignment= 0.3 mm
W 1380 ℃
CuCrZr
374 ℃
1200 ℃
1.3 mm
Tungsten thickness
6 mm
1 mm
0.3 mm
Shadow length: X
High heat flux
θ
IVT& OVT shaping
  Rotation: β = 0.83 °
IVT & OVT shaping, radial step = 2 mm
Rotation: β
Shadow length: X
High heat flux
CuCrZr
450 ℃
1200 ℃
3.3 mm
Tungsten thickness
6 mm
W
1670 ℃
19

## Slide 20
RH Compatible Design
RH process for PFC: cut pipe → remove bolts → grab PFC → move PFC
PFCs bolts and pipe covers
M30
Pipe cover
Area 1
Cross section
Pipe cover
Area 2
85
116
193
120
Cutting pipe（Φ51x3）
160mm
IVT&Dome moving
IVT&Dome removal procedure
IVT&Dome lifting
Bolts removal
4xM30
M30
M36
Pipe cover
Pipe cover
IVT
DOME
OVT
Area 1
PFCs maintained separately
Area 2
315
70
mm
85
U shape pipe
20

## Slide 21
Thermal results: steady state heat load
Max. temperature is within the allowable value
Component |  | Tmax (℃) | Allowable value (℃)
PFU | Tungsten | 1096 | 1200
PFU (Copper) | Cooper | 384 | 550
PFU () | CuCrZr | 338 | 450
PFU () | SS316L(N)-IG | 261 | 450
SSS |  | 110 | 450
Cassette body |  | 131 | 450
Bolt |  | 96 | 450
HTC near SP
~ 105 W/(m2·K)
Heat flux distribution near SP
Temperature distribution on bolt
21

## Slide 22
Thermal results: transient heat load
  The “base” surface temperature depends on the energy fluence
  Type I ELM may not lead to W melting and W recrystallization
ELM type | QELM (MW/m2) | tELM (ms) | fELM (Hz) | Qinter (MW/m2) | Tbase (℃) | ∆TELM (℃)
Type I | 628 | 0.5 | 10 | 3 | 348 | 846
Grassy | 56 | 0.2 | 500 | 3 | 495 | 41
ELM type |  | tELM (ms) | fELM (Hz) |  | Tbase (℃) | ∆TELM (℃)
Type I | 628 | 0.5 | 10 | 3 | 348 | 846
Grassy | 56 | 0.2 | 500 | 3 | 495 | 41
  Type I, =628MW/m2
  Grassy, =56MW/m2
Temperature during ELMs
  Q>5 Scenario
  Q>1 Scenario
22

## Slide 23
Component materials |  | Stress type | Safety factor |  |  |  | 
 |  |  | Testing | Baking | NO | MD event | VDE event
PFU | SS316L(N)-IG | Pm | 1.46 | 12.10 | 11.31 | 11.31 | 12.25
 |  | PL+Pb | 1.06 | 15.13 | 13.78 | 13.78 | 13.78
 |  | PL+Pb+Q | - | 1.88 | 1.20 | 1.20 | 1.20
PFU pipe |  | Pm | 4.18 | 12.18 | 12.18 | 12.55 | 7.39
 |  | PL+Pb | 1.35 | 8.75 | 16.34 | 16.34 | 2.42
 |  | PL+Pb+Q | - | 3.73 | 5.26 | 5.26 | 3.18
SSS | SS316L(N)-IG | Pm | 3.20 | 9.31 | 12.25 | 24.50 | 8.65
 |  | PL+Pb | 2.48 | 4.65 | 10.02 | 15.75 | 7.88
 |  | PL+Pb+Q | - | 1.68 | 1.39 | 1.42 | 2.86
 | XM-19 | Pm | 5.91 | 1.90 | 2.39 | 2.22 | 3.36
 |  | PL+Pb | 1.13 | 1.73 | 2.16 | 2.04 | 3.51
 |  | PL+Pb+Q | - | 2.08 | 2.27 | 2.20 | 3.45
CB |  | Pm | 4.90 | 13.44 | 16.33 | 9.19 | 21.00
 |  | PL+Pb | 3.45 | 10.68 | 12.97 | 10.50 | 16.96
 |  | PL+Pb+Q | - | 1.12 | 1.02 | 1.01 | 1.31
Support |  | Pm | 4.45 | 15.13 | 18.38 | 10.50 | 18.38
 |  | PL+Pb | 2.04 | 22.69 | 14.70 | 7.11 | 14.70
 |  | PL+Pb+Q | - | 1.37 | 1.44 | 1.37 | 1.44
Bolt |  | Pm | 4.5 | 4.88 | 5.04 | 5.13 | 5.04
 |  | PL+Pb | 2.67 | 2.58 | 2.59 | 2.6 | 2.59
 |  | PL+Pb+Q | - | 2.42 | 1.91 | 1.92 | 1.91
Structural results: load combinations
All the stress can meet the design criteria, the value listed in the table is safety factor.
23

## Slide 24
Electro-Magnetic analysis
The Halo current direction and distribution refer to two cases1；
In case 2, according to the plasma evolution2, the halo current is up to 2.05 MA.
TPF3=2 was selected as the worst case for evaluation.
BEST VDE halo current definition-V1.0_20230306；
TSC simulation BEST down&up halo current description of inputing file _20230306；
best disruption physical input_20221212
case 1
Ihalo =104.2 kA
Ip=7.3 MA, TPF=2
Itotal halo=2.5MA
Idivertor halo =2*2.5MA/48=104.16 kA
Ip=7.3 MA, TPF=2
Itotal halo=2.05MA
Idivertor halo =2*2.05MA/48=85.42 kA
case 2
Ihalo =85.5 kA
VDE event
24

## Slide 25
analysis method
Maxwell electromagnetic analysis model
According to the current distribution, 1/16 model was used。
Current flow in
VDE event 1(ideal distribution)
？%
？%
？%
40%
65%
？%
？%
？%
100%
100%
Current distribution in
VDE event 1
analysis result(maxwell distribution )
Current distribution in
VDE event 2
Magnetic field distribution in VDE event 1
Magnetic field distribution in VDE event 2
Current flow in
VDE event 1(maxwell distribution)
Current flow in
VDE event 2(ideal distribution)
Current flow in
VDE event 2(maxwell distribution)
inflow of current
outflow of current
20%
20%
25%
40%
65%
0%
0%
0%
100%
100%
analysis method
VDE event
25
Electro-Magnetic analysis

## Slide 26
R&D for the divertor
PFUs and HHF test
Two methods (Explosive welding + brazing and HIP) were implemented for PFUs. .
One PFU passed 1000 + 1000 cycles HHF test of 15 MW/m2.
‘V’ PFC passed 1000 cycles HHF test of 10 MW/m2.
PFU mock-up and HHF test
750 ℃ @ 15 MW/m2
‘V’ PFC mock-up and HHF test
620 ℃ @ 10 MW/m2
RH tool for PFC
RH compatibility
Successfully tested for PFCs grabbing and move horizontally and vertically.
Pipe welding and cutting process are under developing and testing.
26

## Slide 27
CONTENTS
Requirements and Considerations
Physics basis
Engineering design
Summary
27

## Slide 28
Summary
A conventional divertor solution has been designed and evaluated by edge modeling, which can meet the physics requirements for BEST divertor operation
  Deeper detachment can be achieved with Ne seeding for the slope target compared to the vertical target.
Divertor engineering Design was performed to fulfill the requirements in heat flux, cooling, EM loads, RH maintenance, etc.
  Design loads including the coolant pressure, heat loads, EM loads (VDE, MD) were assessed against design criteria from the thermal, structural and fatigue points of view, justified the structural integrity.
Next step:
  Full cycles of HHF test for PFCs mock-up.
  Divertor cassette module fabrication and series test (HHF, mass flow rate distribution, pressure drop, baking cycles, accuracy of manufacture and assembly).
  Further RH test using CRAFT RH platforms (bolting, unbolting, welding, leak test).
28

## Slide 29
Thank You for Your Attention!