## Slide 1: WP PWIE: Re-deposition of W in the WEST divertor based on post-mortem analyses
M. Diez, C. Arnas, M. Balden, I. Bogdanovic, E. Fortuna-Zalesna, C. Martin, M. Richou, Z. Siketić, E. Tsitrone
09.04.2024
Notes: Overview of the activities regarding WEST within SPB.
Give you a taste of what is going in SPB regarding WEST, and
Not everything is presented here ; it is just to give a taste of the activities

## Slide 2: Configuration of the WEST divertor
WEST phase 1
WEST phase 2
Beveled W coated Gr tiles, including erosion markers
Actively cooled bulk W ITER-like PFUs -> “non beveled PFUs phase 1”
full ITER-like divertor -> « beveled PFUs phase2 »
today
PFUs phase 1
PFUs phase 2
W coated Gr tiles

## Slide 3: A large variety of tiles available for the erosion/redeposition programme
Beveled erosion Markers C1-C5
Surface characterization on whole tile + coring + samples analysis 2020-2023
Beveled standard Gr tiles
C4 tiles: Coring + helium content analysis
C5 tiles: Cutting + cross section analysis 2024
Non beveled PFUs phase 1
Surface characterization on whole tiles 2020-2023
Cutting on progress 2024
Analysis of a few samples 2023
Beveled PFUs phase 2
Post mortem not available yet BUT
in-situ collection of deposited layers 2023
Surface chemical composition 2023
WEST phase 2
full ITER-like divertor -> « beveled PFUs phase2 »
WEST phase 1
Beveled W coated Gr tiles, including erosion markers
Actively cooled bulk W ITER-like PFUs -> “non beveled PFUs phase 1”
today

## Slide 4
OUTLINE
Redeposition profile on WEST divertor: thin films
Redeposition profile on WEST divertor : thick films
Effect of the bevel on the redeposition profile
4. Conclusion and perspectives
[M. Diez, NME 2023]

## Slide 5
OUTLINE
[M. Diez, NME 2023]
Redeposition profile on WEST divertor: thin films
Redeposition profile on WEST divertor : thick films
Effect of the bevel on the redeposition profile
4. Conclusion and perspectives

## Slide 6: Thin boron rich layers at the inner end of the divertor
Thin films area : inner end of HFS
  IBA, LIBS, SEM, Raman, SIMS performed either on Gr tiles or/and ITER-like PFUs
  Rainbow coloured structured films (W oxides)
  Significant B found in far SOL thin deposits by Tof-ERDA (but also evidenced in thick deposits)
  Thickness of deposited layers < 1µm
  Arcing, delamination on Gr tiles (=> C source)
Gr tiles
Post C4
Boron
[I. Bogdanovic, ISFNT 2023]
Notes: Significant B found in far SOL thin deposits by Tof-ERDA (but also evidenced in thick deposits), in agreement with results obtained with other techniques (SIMS, NRA)

## Slide 7
OUTLINE
[M. Diez, NME 2023]
Redeposition profile on WEST divertor: thin films
Redeposition profile on WEST divertor : thick films
Effect of the bevel on the redeposition profile
4. Conclusion and perspectives

## Slide 8: Experimental procedure to measure the thickness of redeposited layers
  FIB cuts on the whole EM tiles (C3, C4, C5)
  FIB cuts on the EM cored samples (C3, C4, C5)
  Metallographic cuts on standard tiles (C5)
  FIB cuts on tape samples from ITER-like PFUs phase 2 (C5-C7)
All tiles have a toroidal bevel ; All tiles are located on max ISP
s = 0 mm
s = 326 mm
Thick deposits

## Slide 9: Deposited layers over 50µm thick
 | Cumulated plasma duration | Thickness (µm) | 
C1-C3 | ≈2h30 | 10-15 | W coated Gr tiles
C1-C4 | ≈6h | 30-35 | 
C1-C5 | ≈7h15 | 45 | 
C5-C7 | ≈6h45 | 40-50 | ITER-like
Thickness gradually increasing with plasma duration
> 50 µm after ≈7h of plasma
25-30 µm attributed to C4 only
Data points resulting from "different techniques & analysis"

## Slide 10
C3
10 µm
Thick deposits
Not homogeneous deposits over the surface
W rich layers
Boron-rich crystals
W+O, W+B
sample ‘iJ’
41 µm
Deposits with very complex structure
Competition between erosion and redeposition
Multi layers
Mix of W, O, B, C
s = 180 mm
C5

## Slide 11
Thick deposits
Local delamination observed in the thick deposits area
D~30 µm
D~50 µm
D~5 µm
100 µm
0
b
a
5 µm
> 30 µm
50 µm
W O B Pt
s = 200 mm
C5 erosion marker tile
Notes: When Delamaination happened ? During campaign ? After campaign ?

## Slide 12: Impurities content using RBS / NRA / Tof ERDA
W as main element of the deposits. Source of W? ISP/OSP erosion? Upper divertor ? Antennas protections ?
Large contribution of B, C and O in the thick deposits
Boron contributes largely to the impurities content, more or less in line with conditionning
  C3 (3 boro)
  C4 (13 boro)
  C5 (2 boro)
Few metallic impurities detected in the thick deposits: Cu, Fe, Cr
ISP
OSP
Tof ERDA analysis at very near surface (up to 250nm)

## Slide 13: Deuterium in the deposits, helium in the erosion area
Highest D content in the deposits. D into C? B? WO?
Significant He amount found in the strike point areas (Tof-ERDA)
  6 at.% at ISP
  10 at.% at OSP
He retention >1021 He/m² in WEST at the OSP >> He retention in ASDEX for He campaign in 2015
He implanted deeper than 150nm -> FIB/TEM scheduled on OSP sample (@PIIM) to see helium/W interactions (He nanobubbles? nanostructures?)
ISP
OSP
Deuterium
Helium
ISP
OSP

## Slide 14
OUTLINE
[M. Diez, NME 2023]
Redeposition profile on WEST divertor: thin films
Redeposition profile on WEST divertor : thick films
Effect of the bevel on the redeposition profile
4. Conclusion and perspectives

## Slide 15: Non uniform deposition due to the toroidal bevel
xt = 4,5 mm
xt = 13,5 mm
xt = 22,5 mm
C5 tiles
s=160mm
xt
4,5
13,5
22,5
Exposed
area
Shadowed
area
Toroidal bevel: designed to protect leading edges from plasma overloading
Change of redeposition profile evidenced during visual inspections
Deposits thick in exposed area, thinner and thinner as approaching shadowed area
Strong adhesion of deposited layers, no flaking (Gr tiles)
20 µm
20 µm
20 µm
36 µm
55 µm
26 µm
25 µm
14 µm
C
C
C
W
W
W
Deposits
Deposits
Deposits

## Slide 16
Thick deposits
- adherent -
Thin deposits
- tend to delaminate easily -
Thin deposits in areas shadowed by the toroidal bevel
These deposits tend to flake when exposed to air (?)
Transport mechanisms ?
s=202mm
MB 12
MB 8
MB 8
MB 12
Toroidal bevel on PFUs phase 2 gives rise to flaking deposits
Photographs taken after C7 (high fluence)
Notes: Deposits observed on areas shadowed by the toroidal bevel
In contrast with the adherent HFS thick deposits, these deposits have a different thin foil like structure, and tend to delaminate easily.

## Slide 17: Adherent thick deposits in the plasma exposed area
Thick deposits
[C. Martin, PSI 2024]
Tape sampling method
FIB cut
Complex structure with different layers, structures and composition
25-55 µm thick
Dense W layers attributed to high fluence campaign
Light elements detected (B, O, C) but less carbon than during phase 1
Deposited layer collected after C5+C6+C7 on WEST beveled PFUs phase 2
23 µm
Notes: No post mortem / only analysis performed on these thick deposits. Chemical composition missing although EDX shows W, O, B in agreement with plasma scenarios

## Slide 18: Composition of deposits by XRF in line with visual observations
Thick deposits
MB 1
XRF measurements along PFU phase 2 after high fluence campaign
XRF Not suitable for light elements detection
[M. Richou, private comm.]
W predominates but Cu and Fe are present in the deposited layers (max at s=125mm)
Notes: No post mortem / only analysis performed on these thick deposits. Chemical composition missing although EDX shows W, O, B in agreement with plasma scenarios

## Slide 19
Flaking thin deposits in the shadowed area
Flakes collected during dust collection (post high fluence)... but also easily manually detachable for characterization
Foil-like structure
2-3 µm thick
Pure W
Thin deposits
Low magnification
High magnification
20 µm
1 µm
W
Still under investigation
10 µm
100 µm
[C. Arnas, PSI 2024]
Notes: these deposits have a different thin foil like structure, and tend to delaminate easily.

## Slide 20
OUTLINE
[M. Diez, NME 2023]
Redeposition profile on WEST divertor: thin films
Redeposition profile on WEST divertor : thick films
Effect of the bevel on the redeposition profile
4. Conclusion and perspectives

## Slide 21: Summary and perspectives
Summary
Successful collaboration work within SP.B !
Post mortem data about redeposition in WEST -> detailed characterization of the deposited layers (thickness, composition, fuel retention)
Results presented here have to be completed with IBA/LIBS/GDOES/SIMS data
Thin deposits
< 1µm thick
B-rich + oxydes
Thick deposits
Up to 50 µm after 7h of plasma
Mix of B, O, C, W + traces of Cu, Fe
Non uniform deposition along toroidal bevel
Flaking of thin deposits in the shadowed areas
Perspectives
Transport of W in the shadowed area (and into the poloidal gaps) ?
Effect of the ripple on the deposited layers ? Beveled tiles vs unbevelled tile ?
Effect of toroidal bevel on deposition (and erosion) ?
Interactions between W and He ?
etc
Notes: PFUs phase 2 : investigation of thick + flaking deposits

## Slide 22
Thank you for your attention !

## Slide 23
Progress on cutting ITER-like PFU samples

## Slide 24: Some history…
ITER-like PFUs phase 1 retrieved from WEST -> available for post mortem analysis
2021
2022
2023
2024
Surface analysis on the whole PFUs : identification of areas of interest
2020
Analysis of thin films, erosion/redeposition pattern, heavy impurities, emissivity, …
PFU cut into 3 segments so it could fit into AURIGA
Purchase of a cutting machine
Erosion/redeposition pattern, arcing, fuel retention
Construction of a temporary « contaminated area »
ITER-like PFU cutting into small samples

## Slide 25: Construction of a temporary « contaminated area »
Cutting machine
Polishing machine
Air measurement
Portable contamination monitor
Container for contaminated water
Notes: Environnement contrôlé
Travail en tenue
Decoupes -> contrôle en surface pour sortie de ZC -> contrôle en volumique pour envoi public domain

## Slide 26: Status of the work
Cutting of the monoblock samples takes much more time than originally anticipated -> re-prioritization performed
  Batch A (VTT, NIFS, UT)
  Batch B + batch C (RBI, WUT, CEMTHI or PIIM)
  Batch E (Demokritos, RBI, PIIM)
All samples cut !
Post-cutting radiation measurements on going ; the samples will be sent right after receiving the results !

## Slide 27: Transport of deposited material inside the poloidal gaps
Thick deposits
Side A and B : similar deposition deposition pattern
Chemical composition
Fe+Cu close to the top surface, Oxygen
W, C, B
Transport mechanisms into the the gaps ?