## Slide 1
P. Tsavalas1, K. Mergia1, D. Papadakis1, A. Lagoyannis1, S. Fazinic2, G. Provatas2, C. Pardanaud2, C. Porosnicu3
1National Center for Scientific Research “Demokritos”, Athens, Greece
2Ruder Boškovic Institut, Zagreb, Croatia
3Aix-Marseille Université, Marseille, France
3National Institute for Laser, Plasma and Radiation Physics, Magurele, Bucharest, Romani
Impact of surface temperature, roughness and impurities on fuel retention & crystalline structure in Be reference samples

## Slide 2: Be-(O)-D/H on W - Reference Samples
Film Composition | Deposition Temperature (oC) | Roughness (nm)
Be-D(5%) | 25 | 100
 | 100 | 
 | 400 | 
 | 25 | 500
 | 100 | 
 | 400 | 
 | 25 | 2000
 | 100 | 
 | 400 | 
Be-D(10%) | 25 | 400
 | 100 | 
 | 200 | 
 | 400 | 
Film Composition | Annealing Temperature (oC)
Be-O-D(20%) | 25
 | 50
 | 100
 | 150
 | 200
 | 250
 | 300
 | 350
 | 400
 | 450
 | 500
Be-O-H(20%) | 25
 | 50
 | 100
 | 150
 | 200
 | 250
 | 300
 | 350
 | 400
 | 450
 | 500
Film Composition | Annealing Temperature (oC)
Be-D(20%) | 25
 | 50
 | 100
 | 150
 | 200
 | 250
 | 350
 | 400
 | 450
 | 500
Be-H(20%) | 25
 | 50
 | 150
 | 200
 | 250
 | 300
 | 350
 | 400
 | 450
 | 500
Deposition Temperature & Roughness
Annealing Temperature, hydrogen isotope & O effect

## Slide 3: Methodology
SEM
Experimental details
Energy: 20 keV
Nuclear reaction analysis (NRA)
Beam: 3He(2 MeV), d(1.6 MeV)
Detection angle: 135°(3He), 170°(d)
Determination of
Elemental amount & depth profile
Experimental details
Determination of
Surface morphology
Experimental details
Source: Cu, K
Incidence angle: 1°
Grazing Incidence XRD (GIXRD)
Determination of
Texture
Crystallite size
Lattice strain
21
inc
Q
kin
kdiff
22
inc is kept constant
The scattering vector Q rotates as 2 is scanned
3He
1H
2H
4He
Q-value = 18352 keV
2H(3He, 1H)4He
135o

## Slide 4: Be-D(5%) on W Deposition Temperature & Roughness Effect

## Slide 5: Be-D(5%): D quantification vs Tdep & Roughness
- 0.023∙T+9.1
- 0.020∙T+7.7
- 0.021∙T+8.1
D amount decreases as the deposition temperature increases; similar rate for the 3 roughness values
D concentration is at all deposition temperatures below 2 at% which is lower than the nominal value (5 at%)
D amount
Be-D Layer Thickness
D Concentration
3He NRA spectrum

## Slide 6: Be-D(5%): D release activation energy
The determined activation energy is in agreement with that obtained by A. De Temmerman et al. Nucl. Fusion 48 (2008) 075008
E=(0.12±0.02) eV
An Arrhenius relation is assumed since the desorption
of gases from metals is a thermally activation process
E=(0.11±0.01) eV

## Slide 7: Be-D(5%): Structural characterization vs Tdep & Substrate Roughness
Non-textured Be: I(100):I(002):I(101)=30:25:100
Be crystallizes at hexagonal P63/mmc space group
Texture evolution with the increase of Tdep:
    From enhanced texture at RT along Be [002] to non-textured material at 400oC
T=100oC: highest C.S., T=400oC: lowest C.S.
The increase of the Tdep results in the relief of the tensile lattice strain in Be
T=400oC: Rough surface
Crystallite size
GIXRD spectrum
Lattice Strain
10 mm
10 mm
10 mm
Substrate Ra: 100 nm
RT
100 oC
400 oC

## Slide 8: Be-D(10%) on W (Ra = 400 nm) Deposition Temperature Effect

## Slide 9: Be-D(10%): D quantification vs Tdep
Decrease of D content as the deposition temperature increases (exponential decrease)
T=400C: D concentration decreases by a factor of about 80 from that at RT
D is found at depths in the range from 2 to 5 m; no clear dependence on deposition temperature
D Content
Be-D Layer Thickness
D Concentration
10∙e-0.01∙T

## Slide 10: Be-D(10%): Structural characterization vs Tdep
Be crystallizes at hexagonal P63/mmc space group
As Tdep increases the texture changes as follows:
  Enhanced texture along [002] at RT; enhanced texture along [100] at 200 C to non textured material at 400 C (similar behavior with Be-D(5%))
The crystallite size increases up to T=200oC; for higher Tdep is almost constant (exponential behavior vs T)
The lattice strain along [101] decreases almost linearly
The roughness increases as Tdep increases
400 oC
30 μm
30 μm
30 μm
30 μm
RT
100 oC
200 oC
400 oC
5 μm
Crystallite size
GIXRD spectrum
A-Be-kT
Lattice Strain
-1.24∙10-5∙T+0.005

## Slide 11
Be-(O)-D/H (20%) on W
Annealing Temperatures Effect

## Slide 12: Be-O-D(20%): D quantification vs Tann
D amount
D concentration
Be-O-D(20%) layer thickness
D amount shows non monotonous behavior; a peak at 300oC appears
D concentration decreases linearly for T>=350oC
Depth profile:
Similar depth profile for all annealing temperatures
A small increase of D concentration at around 5 mm depth
Carbon (8-15 at%) is found at the interface of Be-O-D layer with W
Depth Profile
100oC
d NRA spectrum

## Slide 13
Be-O-D(20%)
Be-O-H(20%)
Be-D(20%)
Be-H(20%)
Oxygen affects texture: Enhanced texture along [002] at the most of the temperatures
Be-D/H: no enhanced texture material
Oxygen results on non monotonous texture evolution (not expected) with the increase of the annealing temperature
The texture for Be-O-D differs with that of Be-O-H (the most pronounced difference is at 200, 300, 400 and 450 oC)
FWHM of the Bragg peaks decreases as T increases; this indicates increase of crystallite size
Lattice constants change with the increase of the annealing temperature
Be-(O)-D/Η(20%): GIXRD spectra vs Tann
Non-textured Be:
I(100):I(002):I(101)=30:25:100

## Slide 14
Be-(O)-D/Η(20%): Crystallite size vs annealing temperature
Be-(O)-D(20%)
Be-(O)-H(20%)
For Be-O-D(20%) and Be-D(20%) crystallite size increases linearly with temperature with similar rate
For Be-O-H(20%) crystallite size increases exponentially with T; whereas for Be-H(20%) the crystallite size increases linearly
10+0.05∙e0.11∙T
0.018∙T+8.1
0.031∙T+6.5
0.027∙T+5.9

## Slide 15
Be-(O)-D/Η(20%): Lattice strain vs Tann
Annealing temperature of 500oC results in the relief of the lattice strain of the Be films; no significance dependence on O presence or hydrogen isotope
Lattice strain along the [101] direction is reduced with temperature almost linearly for all compositions with a similar rate
Be-(O)-D(20%)
-1.10∙10-5∙T+0.005
-1.52∙10-5∙T+0.007
Be-(O)-H(20%)
-8.7∙10-6∙T+0.004
-9.0∙10-6∙T+0.004

## Slide 16
Summary Results
Crystallite size
Lattice strain
Deposition
Temperature
Annealing
Temperature
Deposition temperature affects more drastically the crystallite size than the annealing temperature (a small linear increase)
Lattice strain along the [101] direction is reduced with surface (deposition & annealing) temperature almost linearly for all compositions with a similar rate

## Slide 17
Conclusions
The impact of the surface temperature, substrate roughness and oxygen on the fuel retention and the crystalline structure was investigated on Be – based reference layers
The increase of deposition temperature results in the rapid decrease of the D concentration; non monotonous behavior of D concentration as the annealing temperature increases
Oxygen affects the texture evolution as a function of annealing temperature; enhanced texture along [002] is observed after annealing at 300C in Be-O-D different from that in Be-O-H;.
The increase of the annealing temperature causes a linear increase of the crystallite size (grain growth); Deposition temperature has a more drastic effect in grain growth.
The increase of the annealing/deposition temperature results in the relief of the tensile strain of the Be layers

## Slide 18
Thank you for your attention