## Slide 1
Material deposition, fuel retention and W re-deposition using NRA and SEM on JET W-coated divertor tiles
P. Tsavalas1, K. Mergia1, A. Lagoyannis1, M. Axiotis1, S. Fazinic2, G. Provatas2, J. Likonen3
1National Center for Scientific Research “Demokritos”, Athens, Greece
2Ruder Boškovic Institut, Zagreb, Croatia
3VTT Technical Research Centre of Finland, Finland

## Slide 2
Outline
ILW 1-3 JET Tokamak Divertor Tile 0 & 1
Elemental deposition & fuel retention → amount & depth profile
SEM & elemental mapping of characteristic feature
ILW 2-3 JET Tokamak Divertor Tile 4, 6, 7 & 8
Elemental deposition, erosion & fuel retention → amount & depth profile
SEM & elemental mapping of characteristic feature

## Slide 3
ILW 1-3 JET Tokamak Divertor Tile 0 & 1

## Slide 4: Divertor Tile 0 & 1: Samples & Methodology
Exp. Campaign | Tile | Sample No | S-coordinates
2011-16 | HFGC 14NRH (Tile 0) | 1a | 132
 |  | 3a | 90
 |  | 5a | 50
 | 14IW G1A (Tile 1) | 1 | 405
 |  | 3 | 363
 |  | 6 | 301
 |  | 9 | 240
 |  | 10 | 217
 |  | 11 | 195
HFGC
G1A
14IW G1A (2011-16)
HFGC 14NRH (2011-2016)
1a
3a
5a
1
3
6
9
10
11
Surface analysis
3He NRA (2 MeV)
d NRA (1.62 MeV)
SEM & EDS (10 keV)
Cross Section analysis
SEM & EDS (10 keV)

## Slide 5: Tile 0 Sample 1a: Deposition & fuel retention
Element | Amount (1018 at/cm2)
D | 2.4
Be | 54.4
C | 1.9
N | 1.1
O | 20.3
W | 1.0
50 μm
W layer
Mo layer
CFC
Deposition layer
Cross section
NRA quantitative results
Elemental depth profile
Near Tile 1: High deposition region
Deposited layer thickness:
NRA: >12 μm
SEM/EDS: (6 - 23) mm; Not constant
Deposited layer composition:
Rich in D, Be (dominant), C, N & O
Plenty of impurities (EDS)
Elemental concentration
Chart: Element
NRA | 7.5 | 60.4745 | 3.4196 | 3.0697 | 25 | 1.2512
EDS | 56.28 | 7.37 | 7.125 | 21.65 | 0.97 | 6.605
For the top layer (2-3) mm
Rest elements: Al, Cl, Ca, Ti, Cr, Mn, Fe, Ni, Cu & Mo
For layer thickness of 10 mm
NRA spectra
3He beam
d beam

## Slide 6: Tile 0 Sample 1a: SEM - characteristic surface features
25 μm
50 μm
Area rich in O
Smooth surface with cracks
Areas/particles:
Rich in W due to absence of deposition
Rich in O
200 μm
Areas rich in W
SEM image
50 μm
50 μm
200 μm
40 μm

## Slide 7: Tile 0 Sample 5a: Deposition & fuel retention
Element | Amount (1018 at/cm2) | 
 | Sample 5a | Sample 1a
D | 3.0 | 2.4
Be | 28.4 | 54.4
C | 1.7 | 1.9
N | 0.7 | 1.1
O | 11.5 | 20.3
W | 21.7 | 1.0
NRA quantitative results
For layer thickness of 10 mm
Elemental depth profile
Elemental concentration
For the top layer (2-3) mm
Rest elements: Al, Cl, Ca, Ti, Cr, Mn, Fe, Ni, Cu & Mo
Chart: Element
NRA | 7.5 | 60.4745 | 3.4196 | 3.0697 | 25 | 1.2512
EDS | 56.28 | 7.37 | 7.125 | 21.65 | 0.97 | 6.605
50 mm
Cross section
W layer
Mo layer
CFC
Deposition layer
In the middle of Tile 0; Low deposition region
Be & O amount almost half
Much more W amount
Deposited layer thickness:
NRA: 8 μm
SEM/EDS: (3 - 9) mm
Rich in impurities (same as Sample 1a)
Compared with Sample 1a

## Slide 8: Tile 0 Sample 5a: SEM - characteristic surface features
10 μm
Particle rich in Fe & Cr
Areas rich in O & Cl
Particle rich in Mo & Ca
SEM image
Morphology of fibers BUT NOT enhanced C concentration
Smooth surface with cracks
Oriented Humps
Areas/particles:
Rich in Fe & Cr
Rich in Cl & O
Rich in Mo & Ca
10 μm
25 μm
25 μm
200 μm
200 μm
50 μm

## Slide 9: Tile 1 Sample 1: Deposition & fuel retention
Chart: Element
NRA | 12.5 | 61.2206 | 2.7782 | 2.7208 | 20 | 0.78041
EDS | 51.82 | 12.0967 | 4.06 | 26.3967 | 2.44 | 3.1833
Element | Amount (1018 at/cm2)
D | 3.3
Be | 30.1
C | 1.5
N | 0.7
O | 9.0
W | 26.4
NRA quantitative results
Elemental depth profile
Elemental concentration
For the top layer (2-3) mm
Rest elements: Al, Cl, Ca, Ti, Cr, Mn, Fe, Ni, Cu & Mo
Cross section
W layer
Mo layer
CFC
Deposition layer
(Mostly Be)
Near Tile 3: Low deposition region
Deposited layer thickness:
NRA: 6 - 8 μm
SEM/EDS: (1 - 6) mm
Rich in impurities
50 μm

## Slide 10: Tile 1 Sample 1: SEM - characteristic surface features
10 μm
Particle rich in W, O and N
200 μm
Smooth surface with cracks
Oriented humps
Deposited areas/particles:
Rich in N; the rest of elements have homogeneous distribution
Rich in W, O and N
SEM image
40 μm
200 μm
Rich in N

## Slide 11
Tile 1 Sample 9: Deposition & fuel retention
Element | Amount (1018 at/cm2) | 
 | Sample 9 | Sample 1
D | 5.8 | 3.3
Be | 77.9 | 30.1
C | 7.1 | 1.5
N | 2.0 | 0.7
O | 25.8 | 9.0
W | 1.6 | 26.4
Elemental depth profile
Elemental concentration
NRA quantitative results
For the top layer (2-3) mm
Rest elements: Al, Cl, Ti, Cr, Fe, Ni, Cu & Mo
In Tile 1 middle; High deposition region:
Be, N & O amount more than double
C amount more than triple
Very low W amount
Highest D retention
Deposited layer thickness:
NRA: > 16 μm
SEM/EDS: (25- 45) mm
For layer thickness of 10 mm
Compared to
Tile 1 Sample 1
Cross section
W layer
Mo layer
CFC
Deposition layer
50 μm
Chart: Element
NRA | 15 | 45.7 | 5 | 19 | 15 | 0.4
EDS | 56.31 | 12.72 | 10.155 | 17.54 | 0.73 | 2.42

## Slide 12: Tile 1 Sample 9: SEM - characteristic surface features
SEM images
Rough surface with wide cracks
Oriented humps
Deposited areas/particles:
Rich in W with Cr, Ti, Fe & Ni
Rich in W – Mo
O & Cl
Deposited W with impurities
Rich in O & Cl
Rich in W - Mo
200 μm
200 μm
100 μm
100 μm
10 μm
100 μm
100 μm
100 μm

## Slide 13: Tile 1 Sample 11: Deposition & fuel retention
Element | Amount (1018 at/cm2) |  | 
 | Sample 11 | Sample 9 | Sample 1
D | 4.0 | 5.8 | 3.3
Be | 79.9 | 77.9 | 30.1
C | 4.8 | 7.1 | 1.5
N | 1.9 | 2.0 | 0.7
O | 23.0 | 25.8 | 9.0
W | 1.4 | 1.6 | 26.4
NRA quantitative results
For layer thickness of 10 mm
Elemental depth profile
Elemental concentration
Chart: Element
| D | Be | C | N | O | W | Rest
NRA | 9.6607 | 59.365 | 5.5893 | 5 | 20 | 0.385
EDS | 58.645 | 11.16 | 10.455 | 16.195 | 0.435 | 2.925
100 μm
W layer
Mo layer
CFC
Deposition layer (Mostly Be)
Cross section
For the top layer (2-3) mm
Rest elements: Al, Cl, Ca, Ti, Cr, Mn, Fe, Ni, Cu & Mo
Near Tile 0; High Be deposition region:
Similar deposition with Sample 9
Deposited layerthickness:
NRA: > 16 μm
SEM/EDS: (25 – 55) mm

## Slide 14: Tile 1 Sample 11: SEM - characteristic surface features
5 μm
Rich in W - Mo
200 μm
Rough surface with cracks
Deposited areas/particles:
Rich in W along with Cr, Fe, Ni &Cu
Rich in W - Mo
Rich in O & Cl
200 μm
Rich in O & Cl
Deposited W with impurities
SEM images

## Slide 15: Tile 0 & 1: Summary Results
Deposition & Fuel retention
Composition of deposited layer: Be (dominant), D, C, N, O & many impurities
S- coordinate 50: Low deposition: layer thickness ~6 mm
S- coordinate 95 - 240: High deposition region: layer thickness >16 mm
S- coordinate 240 - 405: Low deposition: layer thickness <8 mm
Morphology
S- coordinate 50 - 132: fibre morphology, smooth surface & cracks
S- coordinate 195 – 240: rough surface & wide cracks
S- coordinate 301 – 405: smooth surface & cracks
Surface characteristic features
100 μm
2.5 μm
10 μm
10 μm
W deposition
W – Mo deposition
O - Cl deposition
Fe - Cr deposition

## Slide 16
ILW 2-3 JET Tokamak Divertor Tile 4, 6, 7 & 8

## Slide 17: Tile 4, 6, 7 & 8: Samples & Experimental Details
Exp. Campaign | Tile | Sample | S-coordinate
2013-16 | 14BN G4D | 3b | 868
 |  | 5b | 824
 |  | 7b | 779
 |  | 9b | 735
 | 2BN G6C | 5a | 1405
 |  | 7a | 1447
 | 2ON G7A | 2 | 1668
 |  | 4 | 1716
 |  | 6 | 1764
 | 2ON G8B | 2b | 1865
 |  | 4b | 1919
 |  | 6b | 1973
 |  | 8b | 2027
 |  | 10b | 2053
14BN G4D
2BN G6C
2ONG7A
2ONG8B
10b
8b
6b
4b
2b
6
4
2
7a
5a
7b
5b
3b
JET Tokamak Divertor
Surface
d NRA (1.6 MeV)
SEM & EDS (5 keV & 30 keV)
9b

## Slide 18: Tile 4 Sample 9b
Element | Amount (1017 at/cm2)
D | 16.1
Be | 36.9
C | 40.75
N | 5.8
O | 36
NRA quantitative results
Elemental depth profile
Elemental concentration
Highest D
retention
Chart: Concentation (at%)
| Be | C | N | O | Ni | W | Rest
EDS | 6.315 | 47.455 | 4.78 | 23.655 | 0.93 | 15.905 | 0.95
Rest elements: Cu, Fe, Cl
100 μm
W deposition
Cl - Na deposition
Highest D amount
Elemental concentration decreases with depth (up to depth of ~4 mm)
Smooth surface
Detection of W, W - Mo, O and Cl & Na deposition areas
2.5 μm
5 μm
W - Mo deposition
5 μm

## Slide 19: Tile 6 Sample 7a
Chart: Elements
| Be | C | N | O | Ni | W | Rest
EDS | 34.155 | 11.955 | 17.1 | 31.055 | 1.405 | 2.825 | 1.505
NRA quantitative results
Elemental depth profile
Elemental concentration
100 μm
5 mm
Particle rich in W - Mo
The sample with the highest deposition (Be, C, N & O)
Thick deposition layer (>13 mm)
Rough surface with wide cracks
W deposition on Be deposition layer
W - Mo deposition particle
Element | Amount (1017 at/cm2)
D | 3
Be | 910
C | 128
N | 34
O | 58.5
Rest elements:
Cu, Fe, Cl, Mo, Na, Al
Highest deposition
Highest Be
W deposition on thick Be layer
100 μm
10 μm

## Slide 20: Tile 7 Sample 2
Element | Amount (1017 at/cm2)
D | 1.2
Be | 35.1
C | 19.6
N | 6.1
O | 8.4
NRA quantitative results
Elemental depth profile
Elemental concentration
Chart: COncentration (at%)
| C | N | O | Mo | W | Rest
EDS | 40.275 | 8.85 | 10.95 | 6.6 | 32.2 | 1.13
Rest elements: Ni, Fe, Cu
(Be under detection limits)
100 μm
100 μm
Mo spots
Mo after W erosion
W - Mo deposition on Mo
Elemental deposition decreases, but the deposition depth is higher than 6 mm (detection limit)
Sample has suffered erosion and W - Mo deposition
10 μm
2.5 μm
Highest Mo

## Slide 21: Tile 8 Sample 2b
Element | Amount (1017 at/cm2)
D | 1.5
Be | 5.645
C | 4.9
N | 0.975
O | 0.75
NRA quantitative results
Elemental depth profile
Elemental concentration
Lowest deposition
W - Mo deposition
W deposition
Ni & O
Lowest deposition, thinnest deposition layer (<1 µm)
Poor in elemental abundance (EDS)
Smooth surface with cracks
W - Mo and W deposition
Rest elements: Fe, Cu
100 μm
10 μm
50 μm
Chart: Cocentration (at%)
| C | N | O | Ni | W | Rest
EDS | 32.24 | 10.585 | 11.52 | 0.92 | 44.165 | 0.57
Highest W

## Slide 22: Tile 4, 6, 7 & 8: Summary
Fuel retention
High D amount ((2.4 - 16.1) × 1017 at/cm2) on Tile 4, the highest one near Tile 3
Material deposition
The elemental (Be, C & N) amounts change similarly versus S-coordinate:
Tile 4: Material deposition decreases from tile 3 to tile 5
Tile 6: The highest deposition at the same S-coordinate (1447)
Tile 7: It presents higher deposition than Tile 8
Tile 8: Elemental amounts almost constant with S-coordinate
Tile 3
Tile 9
Surface characteristic features
W erosion &
Mo-W deposition
Mo
W - Mo deposition
Ni-O areas
O
Al-O
Cl-Cu
Cl-Na
Fe
10 μm
2.5 μm
10 μm
5 μm
10 μm
10 μm
10 μm
5 μm
2.5 μm
2.5 μm
W
W erosion
W deposition

## Slide 23
Thank you for your attention