## Slide 1: Material Migration Studies: Tracer Experiments with 15N and 18O in JET-ILW
M. Rubel, P. Petersson, L. Dittrich, S. Moon, P. Ström, A. Widdowson

## Slide 2: Background Information and Motivation
Oxygen is always detected on surfaces exposed to plasma in controlled fusion devices: PFC, wall probes, dust.
Nitrogen is always detected on PFC, probes & dust from devices with N-based edge cooling.
Questions about the origin of N and O on analysed surfaces:
Co-deposition of plasma impurity species during the machine operation?
Adsorption from air (water, oxygen) when materials are transferred/stored from the torus?
Does the oxidation take place in the vessel?
Injection of marker gases (tracers):
18O (natural abundance 0.37%)
15N (natural abundance 0.22%)
High resolusion, high sensitivity quantitative analyses:
Nuclear reaction analysis (NRA) using protons: 18O(p, α)15N 15N(p,g4He)12C
Time-of-flight heavy ion elastic recoil detection (HIERDA) with 80Br7+32 MeV or 127In+ n = 8 or 10; 36 or 44 MeV

## Slide 3: A bit of history
1985, TEXTOR: first experiments with 18O, no success, difficulties in NRA measurements.
2009, TEXTOR: first 15N experiments, very conclusive experiment and HIERDA measurements
followed by a series of experiments and modelling of 15N and metal markers (W, Mo).
P. Petersson et al. Nucl. Instrum. Meth. B, M. Rubel et al., J. Nucl. Mater. 438 (2013) S170. A. Weckmann et al., Nucl. Mater. Energy 17 (2018) 83.
2011, ASDEX-Upgrade, conclusive experiments with 15N, NRA measurements and modelling.
P. Petersson et al., J. Nucl. Mater. 438 (2013) S616. P. Petersson et al., Phys. Scr. T159 (2014) 014042.
2012, TEXTOR, very successful experiments on ICWC with 18O tracer
A. Garcia-Carrasco et al., Phys. Scr. T159 (2014) 014017.
2012, JET-ILW, local injection of 15N in the divertor.
P. Petersson et al., J. Nucl. Mater. 463 (205) 814.
2016, JET-ILW, injection of 15N and 18O in separate discharges.
The original idea of Per Petersson: the use of ”isotopic air”: 80% 15N + 20% 18O

## Slide 4: Tools: Erosion-Deposition Diagnostics in JET-ILW Marker Tiles and Probes
The aim is to have a complete overview of material migration and material damage, not just a number (even large) of analysis points and isolated findings.
Be
Be
Be
on
Inconel
Be
W/CFC
W/CFC
Bulk W
Be
RH
AN

## Slide 5
Inner
Outer
Base
Be
W
Quartz microbalance
  Covers
  Crystals
Test mirrors
Spatial blocks
Rotating deposition monitors
Louvre clips
Sticking monitors
Wall inserts in IWC
Dust monitors

## Slide 6: Gas injection system in JET
15N in ILW-1
15N in ILW-3
18O in ILW-3

## Slide 7: Gas injection history
Gas | Injection point | ILW-1 | ILW-2 | ILW-3
1H | GIM, pellets | 2.5·1024 | 2.7·1025 | 8.0·1025
 | DMV | - | 1.3·1024 | 1.0·1025
2D | GIM, pellets | 9.1·1026 | 5.8·1026 | 6.4·1026
 | DMV | - | 2.4·1026 | 1.4·1026
3He | main chamber GIM | - | 8.2·1022 | 7.4·1022
4He | main chamber GIM | - | 2.5·1021 | 3.3·1022
CD4 | GIM 11 | - | - | 3.7·1023 a
C2D4 | GIM | - | - | 4.3·1021 b
14N | GIM 4, 8, 11 | 9.7·1023 | 3.8·1024 | 2.1·1024
15N | GIM 14, 10 | 1.3·1022 (GIM 14) | - | 8.5·1023 (GIM 10)
16O | GIM 11 | - | - | 2.0·1022 d
18O | GIM 11 | - | - | 2.8·1022
Ne | divertor GIM | 2.1·1021 | 1.2·1023 | 1.3·1023
 | DMV | - | 3.8·1023 | 1.2·1024
Ar | divertor GIM | 2.9·1021 | 8.5·1021 | 1.3·1022
 | DMV | - | 2.0·1025 | 9.2·1024
Kr | divertor GIM | - | - | 7.1·1021
 | DMV | - | 2.0·1024 | 1.3·1025
Xe | divertor GIM | - | - | 7.9·1019
aCD4 was puffed in two series: 1.1⋅1023 in the middle of ILW-3 and 2.6⋅1023 at the last session, 8 shots before the last one.
bC2D4 puffed approx. 400 shots before the end of ILW-3.
15N injection during two last sessions in ILW-3.
18O injection during 4 shots in the penultimate ILW-3 session; 30 shots before the last discharge.
Laura Dittrich et al., Fusion Eng. Des. 192 (2023) 113620

## Slide 8: HIERDA spectra
All species present in the torus are then detected in co-deposits:
H, D, 3He, 4He, Be, 12C, 14N, 15N, 16O, 18O, Ne and heavier

## Slide 9: Analysis of Outer Poloidal Limiters
Tile | Position | Areal density in 1015 atoms cm-2 |  |  |  |  |  |  |  |  |  |  |  |  | 
 |  | 1H | 2D | 3He | 4He | Be | C | 14N | 15N | 16O | 18O | Ne | Ar | Cr, Fe, Ni, Mo | W
4D14 (ILW-1) | LH wing C1R4 | 57 | 170 | - | - | 8054 | 183 | 132 | - | 320 | - | - | - | 91 | 12
4D14 (ILW-3) | LH wing C1R4 | 18 | 74 | 35 | - | 7854 | 207 | 224 | 44 | 527 | - | 10 | 3 | 84 | 9
 | LH Int. 1 C2R4 | - | 87 | - | - | 8637 | 68 | 35 | 19 | 216 | - | 1 | - | 22 | 1
 | LH Int. 2 C1R4 | 9 | 65 | - | - | 8908 | 12 | 3 | 13 | 80 | - | - | - | 9 | -
 | Center C4R4 | 10 | 32 | - | - | 8918 | 8 | 5 | 11 | 93 | - | - | <1 | 20 | 1
4D15 (ILW1-3) | LH wing C3R4 | 49 | 116 | - | - | 7472 | 257 | 165 | 68 | 773 | 0 | - | 25 | 119 | 31
 | LH wing C1R4 | 16 | 59 | 31 | 5 | 7818 | 206 | 226 | 37 | 567 | 1 | 3 | 7 | 101 | 12
 | LH Int. 1 C2R4 | 14 | 79 | - | - | 8240 | 168 | 135 | 31 | 356 | - | - | - | 68 | 9
 | LH Int. 2 C1R4 | - | 29 | - | - | 8974 | 8 | - | 13 | 58 | - | - | - | 13 | -
 | RH Int. 2 C3R6 | - | 72 | - | - | 8923 | 3 | 3 | 17 | 63 | 1 | - | - | 18 | 1
 | RH Int. 2 C1R6 | 2 | 58 | - | - | 8937 | 7 | 5 | 17 | 50 | 2 | - | - | 20 | 1
 | RH Int. 1 C2R6 | - | 112 | - | - | 8833 | 13 | 12 | 21 | 75 | 2 | - | - | 21 | 2
 | RH wing C3R6 | 21 | - | - | - | 6925 | 309 | 608 | 247 | 728 | 17 | - | - | 212 | 28
 | RH wing C2R3 | 35 | 33 | - | - | 6963 | 305 | 582 | 198 | 729 | 9 | - | <1 | 215 | 27
Laura Dittrich et al., Fusion Eng. Des. 192 (2023) 113620

## Slide 10: Analysis of tiles
Analyses were also performed for Inner Wall Guard Limiters (IWGL) , Upper Dump Plates (UDP), Inner Wall Cladding (IWC); detailed data for IWGL and UDP are in the Appendix.
IWGL: 15N up to 290x1015 cm-2 , 18O up to 14x1015 cm-2
in deposition zones at the end sections of the tiles.
UDP: 15N up to 9x1015 cm-2, 18O detected only in one spot 1x1015 cm-2, i.e. just above the
detection limit of 0.5- 1x1015 cm-2.
However, 15N was clearly detected on the molten Be flake from the UDP.
IWC: 15N content at the detection limit of 0.5- 1x1015 cm-2.
(Laura Dittrich et al., Phys. Scr. 96 (2021) 124071)

## Slide 11: Upper Dump Plates: Be flake
W
I (scattered beam)
Inconel family
16O
15N
14N
12C
9Be
7Li
D
1000
800
600
400
ToF Heavy Ion ERDA on Be flake from the dump plate
6Li
0 400 800 1200
Energy channel
ToF channel
16O
15N
14N
12C
15N only on very surface
1000
800
Something for modellers:?
How 15N reached the UDP?
Petter Ström, Per Petersson, VR Stockholm

## Slide 12
Tracers on the Wall Probes
Mirrors
QMB: covers and crystals
Spatial blocks

## Slide 13: Mirror & Cassette
4.5 cm
3.0 cm
2.0 cm
1.5 cm
0.0 cm
1 cm
Mo
Standard
Notes: The mirror is 1 cm cubic Polycrystalline Molybdenum.
Mirrors were installed with cassettes.
And the mirror carriers have several different position and baffles to test different aspect ratio and solid angle.
The position means distance from the mouth of cassettes.
And this is the baffles in cassette.
27 hours of JET operation
Correspondence to 20 ITER pulses (400s, full power) scaled by energy input,
2-3 pulse scaled by expected divertor fluxes (R. Pitts, PPCF, 47, 2005)

## Slide 14: Mirrors are perfect deposition monitors in tracer experiments
H
D
Be
C
N
O
18O
ToF channel
Energy channel
Mirror from the Outer Divertor (1.5 cm ILW 1-3)
  Injected: 2.8 x 1022 atoms
  Position: inner divertor base
First Results :18O: 7 ×1015 cm-2
Detection of O-18
Deposition within campaign
Injection of 18O on the last operation day of ILW-3 to check in-vessel oxidation.
Sunwoo Moon et al., Nucl. Mater. Energy 19 (2019) 59.
Notes: The mirror also works as deposition monitors
From the outer divertor, not only outer divertor, but I show this result, we can find oxygen eighteen and nitrogen fifteen on the top surface.
The mirror is perfect deposition monitor with flat surface

## Slide 15: Tracers on QMB covers and crystals
Petter Ström et al., J. Nucl. Mater. 516 (2019) 202.
15N not detected on the covers.
No tracers on the crystals.
Module13 IW
Module2 IW
Module2 IW
Module2 OW
Notes: The mirror also works as deposition monitors
From the outer divertor, not only outer divertor, but I show this result, we can find oxygen eighteen and nitrogen fifteen on the top surface.
The mirror is perfect deposition monitor with flat surface

## Slide 16: Tracers on spatial blocks
Petter Ström et al., J. Nucl. Mater. 516 (2019) 202.
15N not detected on the blocks.
Spatial blocks: Inconel 600 cubes (15 mm) attached to the CFC ribs of the divertor modules: Module 14 Inner Wide
Notes: The mirror also works as deposition monitors
From the outer divertor, not only outer divertor, but I show this result, we can find oxygen eighteen and nitrogen fifteen on the top surface.
The mirror is perfect deposition monitor with flat surface

## Slide 17: Other Deposition Monitors
Dust monitors: analysed with HIERDA, no tracers detected. M. Rubel, Fusion Eng. Des. 136 (2018) 579.
Louvre clips: HIERDA done VTT, results to be re-analysed / evaluated.
Rotating deposition monitors: no HIERDA performed.
Wall inserts: no HIERDA performed, but no tracers detected on the IWC tiles.
Sticking monitors: no data available.

## Slide 18: Concluding remarks
Tracers have been found on most studied surfaces thus indicating the long-range transport.
A large amount of data have been obtained:
  18O - deposited mainly on probes from the inner divertor (close to the injection).
  15N - little detected on the divertor probes, much more on the limiter tiles.
Modelling may be considered but with some caveats:
  Leaks and transport behind the tiles (as concluded after 13C experiments in JET)
  Interest from PWIE, ITER ??
We have good analysis tools. One can consider experiments with other tracers in several machines: 10B, 21Ne, 22Ne

## Slide 19
APPENDIX

## Slide 20: Analysis of Inner Wall Guard Limiters
Laura Dittrich et al., Fusion Eng. Des. 192 (2023) 113620
Tile | Position | Areal density in 1015 atoms cm-2 |  |  |  |  |  |  |  |  |  | 
 |  | 1H | 2D | Be | C | 14N | 15N | 16O | 18O | Ar | Cr, Fe, Ni, Mo | W
2XR10 (ILW-1) | RH wing C4R7 | 61 | 90 | 7476 | 298 | 84 | - | 910 | - | - | 172 | -
 | Center C7R2 | 14 | - | 8960 | 11 | 6 | - | 87 | - | - | 17 | 5
2XR10 (ILW-2) | RH wing C1R4 | 69 | - | 7677 | 166 | 103 | - | 948 | - | - | 122 | 15
 | RH wing C3R4 | 185 | - | 7104 | 249 | 261 | - | 933 | - | - | 157 | -
 | Center C6R4 | 15 | 29 | 8941 | 38 | - | - | 68 | - | - | 8 | -
 | Center C6R5 | 29 | - | 8933 | 25 | - | - | 70 | - | - | 5 | -
2XR11 (ILW1-3) | RH wing C1R4 | 19 | 45 | 8492 | 59 | 35 | 8 | 351 | 2 | 3 | 65 | 12
 | RH wing C3R3 | - | 125 | 7461 | 268 | 470 | 232 | 450 | 8 | 3 | 70 | 5
 | RH wing C3R7 | 8 | 135 | 7483 | 365 | 353 | 289 | 378 | 14 | 3 | 63 | 5
 | Center C5R4 | - | 10 | 9009 | 3 | 1 | 5 | 59 | - | 2 | 6 | 1
 | LH Int. C1R4 | - | - | 8952 | 22 | 16 | - | 97 | - | - | 11 | 1
 | LH Int. C3R4 | 16 | 113 | 7945 | 179 | 320 | 144 | 274 | 6 | 1 | 88 | 9

## Slide 21: Analysis of Upper Dump Plates
Laura Dittrich et al., Fusion Eng. Des. 192 (2023) 113620
Tile | Position | Areal density in 1015 atoms cm-2 |  |  |  |  |  |  |  |  |  |  |  | 
 |  | 1H | 2D | 3He | Be | C | 14N | 15N | 16O | 18O | Ar | Cr, Fe, Ni, Mo | W | 
2B4C (ILW-3) | C6R2* | - | - | - | 9053 | 1 | 1 | 2 | 30 | 1 | 4 | 6 | 1 | 
 | C6R8* | 10 | 4 | - | 8855 | 14 | 6 | 9 | 144 | - | 5 | 28 | 5 | 
3A8 (ILW1-3) | C2R9 | 30 | 66 | - | 7295 | 175 | 191 | - | 970 | - | 5 | 293 | 57 | 
 | C2R12 | 34 | 65 | - | 7021 | 171 | 236 | - | 1057 | - | 10 | 384 | 55 | 
 | C2R14 | 32 | 54 | - | 7098 | 176 | 256 | - | 1049 | - | - | 350 | 51 | 
 | C4R9* | <1 | 4 | - | 9012 | 3 | 3 | 3 | 57 | - | 1 | 12 | 1 | 
 | C4R12* | 5 | 28 | - | 8698 | 21 | 61 | 7 | 224 | - | 10 | 37 | 5 | 
 | C5R9 | 18 | 115 | 19 | 6574 | 207 | 175 | - | 1515 | - | 12 | 369 | 60 | 
 | C5R12 | 21 | 127 | 26 | 6586 | 183 | 156 | - | 1550 | - | 14 | 356 | 56 | 
 | C5R14 | 23 | 117 | 26 | 6647 | 167 | 153 | - | 1487 | - | 11 | 380 | 59 | 
* Molten area

## Slide 22
Carbon and tracers (N-15 and O-18) on Be limiters
Table Limiter | Sample | N-14 | N-15 | O-18 | D | C*
OPL | 540 | 6 | 45 | 0 | 17 | 12
OPL | 546 | 24 | 67 | 6 | 18 | 20
OPL | 553 | 18 | 22 | 3 | 15 | 9
OPL | 558 | 85 | 25 | 3 | 15 | 59
IWGL | 511 | 3 | 14 | 0 | 11 | 7
IWGL | 513 | 36 | 131 | 5 | 29 | 48
Deuterium, carbon, nitrogen and tracer species (N-15 and O-18) on beryllium limiters from ILW-3 in 1015 at/cm2.
* Very positive result: small C content on Be.

## Slide 23: Mirrors from Divertor: Surface composition
ILW3
ILW1-3
Chart: 
| Base 0.0 | Base 1.0 | Base 1.5 | Base 2.8 | Inner 0.0 | Inner 2.5 | Inner 4.5 | Outer 0.0 | Outer 1.5 | Outer 3.0
H | 14319313286979292 | 38256767393609416 | 49318588169861368 | 37376588052508960 | 24663670300073084 | 14379181896273472 | 21643917993833252 | 13045558919423296
D | 1.606e+17 | 3.6507e+17 | 3.3857e+17 | 2.4659e+17 | 1.9065e+18 | 2.9142e+17 | 67335983328191768 | 1.1306e+18 | 73265047494465152 | 73126329845867248
Be | 9.7878e+17 | 1.8245e+18 | 1.8259e+18 | 1.4254e+18 | 8.6255e+18 | 2.2854e+18 | 8.5422e+17 | 6.6411e+18 | 3.6927e+18 | 3.1047e+18
C | 57447055085234592 | 80801165606229728 | 59487083478756136 | 50066274057014704 | 1.5875e+17 | 60442090456854904 | 1.1821e+17 | 62257608534945112
N | 71849949828945392 | 1.4239e+17 | 1.6293e+17 | 1.4598e+17 | 5.5527e+17 | 2.137e+17 | 1.9924e+17 | 1.7333e+17
O | 9.1365e+17 | 1.3379e+18 | 1.0771e+18 | 8.1941e+17 | 1.0679e+18 | 4.8062e+17 | 1.7282e+18 | 9.6e+17
Ni | 39733108366894312 | 46936986979612224 | 35078822038718424 | 27872176943179368 | 1.1359e+17 | 53775294617003632 | 11707476950534868 | 3.7907e+17 | 73391335676694032 | 37643537594104624
#REF! | 1
W | 57880207485604664 | 45498614066335776 | 20699081132161908 | 18449166332305572 | 4.2503e+17 | 32532675118266184 | 17741822153574092 | 1.5638e+17 | 26325297903135556 | 8273508070748495
Chart: 
| Base 0.0 | Base 1.0 | Base 1.5 | Base 2.8 | Inner 0.0 | Inner 2.5 | Inner 4.5 | Outer 0.0 | Outer 1.5 | Outer 3.0
H | 4306102527851535 | 19047535724456572 | 9807177414609246 | 6242191892221353 | 24392717307739492 | 3213938907822658 | 6139424726248415 | 21666014332146684 | 18669361323343212
D | 35358889316755944 | 1.2549e+17 | 28842326732425740 | 18730495221615848 | 7.3837e+17 | 87272294188583040 | 26293436957843864 | 3.877e+15 | 1.0016e+17 | 93937906152782176
Be | 4.9522e+17 | 6.6117e+17 | 6.5195e+17 | 5e+17 | 2.9708e+18 | 1.1833e+18 | 3.2287e+17 | 1.6945e+17 | 2.9756e+18 | 2.5277e+18
C | 20331791887997012 | 23975214302011972 | 16993511728100444 | 17380393286261206 | 75437019198889024 | 28604569145422752 | 70252703786491808 | 75844607825013296 | 46206705744092144
N | 32308673650260600 | 39131410630972856 | 58071551611262168 | 59866214457612424 | 2.4813e+17 | 60621924320326368 | 16026928560941096 | 1.3912e+17 | 1.3234e+17
O | 5.6161e+17 | 5.7371e+17 | 5.6978e+17 | 4.979e+17 | 5.2871e+17 | 2.3369e+17 | 1.3976e+17 | 1.2433e+18 | 5.9966e+17
Ni | 21717866588603416 | 21277827914552504 | 20058098026706324 | 15244557844028920 | 40468740000000000 | 26117602742562016 | 11130249817695984 | 26667708960045408 | 2.8069e+17 | 63662923933929208
#REF! | 1
W | 22550050664787876 | 12963199121174160 | 5254052672114835 | 4181308394386570 | 1.4738e+17 | 28055306607084048 | 8001295789972732 | 27614556199249504 | 30385176793375028 | 7267868974127800
Sunwoo Moon et al., Nucl. Mater. Energy 19 (2019) 59.

## Slide 24: Mirrors: Visual inspection
Inner Divertor
Outer Divertor
Divertor Base
ILW3
ILW1-3
0.0 cm
2.5
4.5
ILW3
ILW1-3
ILW3
ILW1-3
0.0
1.5
3.0
0.0
1.0
1.5
2.8
0.0 cm
1.5
1.5 b
4.5 b
4.5
Main Chamber Wall
Sunwoo Moon et al., Nucl. Mater. Energy 19 (2019) 59.
Notes: ILW1-3 mirror has only slight less
ILW1-3 Base 1.0 mirror was taken in different condition: exposure time 0.5 s. The others were in 1.0 second

## Slide 25
JET – ITER like Wall