## Slide 1: WP PWIE Midterm Meeting 2024 LID-QMS at FZJ and JET on tiles 0 and 1
M. Zlobinski, G. Sergienko, I. Jepu, C. Rowley, A. Widdowson, R. Ellis, D. Kos, I. Coffey, M. Fortune, D. Kinna, M. Beldishevski, A. Krimmer, H. T. Lambertz, A. Terra, A. Huber, S. Brezinsek, T. Dittmar, M. Flebbe, R. Yi, R. Rayaprolu,, J. Figueiredo, P. Blatchford, S. Silburn, E. Tsitrone, E. Joffrin, A. Hakola, K. Krieger, Y. Corre, THE EUROFUSION TOKAMAK EXPLOITATION TEAM AND THE JET CONTRIBUTORS

## Slide 2: Outline
The LID-QMS method
Ex situ experimental Setup at FZJ: FREDIS
Ex situ measurements on JET tiles
Sample overview
In situ experimental Setup at JET
In situ measurements inside JET
Overview of all in situ LID-QMS measurements

## Slide 3: LID-QMS method
high energy laser (~20 J, 1 ms)
CFC substrate
Laser-Induced Desorption (LID)
Laser only heats the surface, no ablation, no crater formation, no plasma needed
Possible surface modifications due to heating :
roughening of surface
melting (only for high power)
minor evaporation
layer delamination due to thermal stresses in short time
Laser spot diameter ~3 mm
vacuum chamber
RGA (Residual Gas Analysis) e.g. by QMS (Quadrupole Mass Spectrometry)
H2, D2, HD, DT,…
Be melting point
Be layer thickness in JET (thicker in ITER) is heated and thermally releases retained gases
substrate
Example of calculated temperature
W Mo
Be
Be
W
plasma deposit
Mo
CFC
Gas released by the laser heating is quantified → space resolved in situ diagnostic of the fuel content

## Slide 4: FREDIS (Fuel REtention Diagnostic Setup) @ FZJ
LID
TDS
hi-res. QMS (MKS) 0-6 u/e
glove boxes for safe handling of Be
air stream
pyrometer
camera
laser beam
TP
TP
TP
TDS oven (open)
load lock
TP
manipulator drive
LID sample
TDS sample
GV
x/y/z stage
overview QMS (Pfeiffer) 0-100 u/e
air lock (open)
laser head
fibre-optic cable from laser
GV
GV
GV
door
TP
GV
GV
tritium detector
CuO catalyst
gas washing bottles
tritium trap (under construction)
exhaust
distance measure-ment
load lock
1 m
filter
filter
FREDIS features: beryllium compatible
Ref: M. Zlobinski et al., Fus. Eng. Des. (2019) doi:10.1016/j.fusengdes.2019.02.035
tritium compatible
located in radiation controlled area (HML)
Laser-Induced Desorption
Thermal Desorption Spectrometry

## Slide 5: JET Sample Overview for LID-QMS @ FZJ
Tile 0 (HFGC14N LH, ILW3) remaining part after coring + core 3b
Tile 1 (14IN G1C, ILW3) remaining part after coring + core 11a
Tile 0 (HFGC??? RH, ILW1-3) remaining part after coring
Tile 1 (14IWG1A, ILW1-3) remaining parts after coring
W lamella cuts
Be limiter 2XR10 from ILW3 for poloidal D profile
IWC 4/2 (2011-2016) 19, 32

## Slide 6: Ex situ LID-QMS of JET divertor tile 0 from ILW3
Ref [1]: J. Likonen et al, Nuc. Mat. En. 19 (2019) 300-306 doi:10.1016/j.nme.2019.03.012
JET inner divertor tile 0 exposed in ILW3 (2014-2016). Then ex situ LID-QMS performed in FZJ.
Good agreement of LID-QMS with TDS except close to plasma heated side due to mechanical damage of surface before LID
constant D inventory
tile 0
tile 1
2c
4c
6c
7c
1c
3c
5c
LID-QMS: Ø3 mm laser spots
TDS of cored samples
5c low
3c low
1c low
LH14N

## Slide 7: JET Sample Overview for LID-QMS @ FZJ
Tile 0 (HFGC14N LH, ILW3) remaining part after coring + core 3b
Tile 1 (14IN G1C, ILW3) remaining part after coring + core 11a
Tile 0 (HFGC??? RH, ILW1-3) remaining part after coring
Tile 1 (14IWG1A, ILW1-3) remaining parts after coring
W lamella cuts
Be limiter 2XR10 from ILW3 for poloidal D profile
IWC 4/2 (2011-2016) 19, 32
different laser energies: 5 J, 7.5 J, 10 J, 4 pulses with 10 J, 12 J, 15 J @ 3 ms pulse duration
5 J shows incomplete D desorption
2nd shot with 10 J releases <5% of 1st shot
Requested for NRA inside laser spots

## Slide 8: JET Sample Overview for LID-QMS @ FZJ
Tile 0 (HFGC14N LH, ILW3) remaining part after coring + core 3b
Tile 1 (14IN G1C, ILW3) remaining part after coring + core 11a
Tile 0 (HFGC??? RH, ILW1-3) remaining part after coring
Tile 1 (14IWG1A, ILW1-3) remaining parts after coring
W lamella cuts
Be limiter 2XR10 from ILW3 for poloidal D profile
IWC 4/2 (2011-2016) 19, 32
different laser energies: 10 J, 15 J @ 3 ms pulse duration
No significant difference (both above limit for complete D desorption)
Requested for NRA inside laser spots

## Slide 9: JET Sample Overview for LID-QMS @ FZJ
Tile 0 (HFGC14N LH, ILW3) remaining part after coring + core 3b
Tile 1 (14IN G1C, ILW3) remaining part after coring + core 11a
Tile 0 (HFGC??? RH, ILW1-3) remaining part after coring
Tile 1 (14IWG1A, ILW1-3) remaining parts after coring
W lamella cuts
Be limiter 2XR10 from ILW3 for poloidal D profile
IWC 4/2 (2011-2016) 19, 32
JET tile 1 from ILW3 now installed in FREDIS: It will need 2 ventings for one poloidal scan in order to shoot the laser rectangular onto the 3 slopes

## Slide 10: JET Tile 0 (HFGC??? RH, ILW1-3) remaining part after coring
Poloidal scan:
One retention plateau like for ILW3 only
2nd poloidal scan next to 1st scan can be done.
Toroidal scan:
D retention maximum quite far on the right-hand side
Toroidal scan could be continued. It was limited by motor movement of 7 cm.
Chart: poloidal position / mm
| 55 | 61 | 71.5 | 80 | 92 | 100 | 112.5 | 119.5 | 130.80000000000001 | 153 | 169.5
 | 2e-10 | 2e-10 | 5.5e-10 | 3e-09 | 7.5e-09 | 7.3e-09 | 7.2e-09 | 7e-09 | 7.5e-09 | 4.5e-09 | 2.9e-09
Mass 3 desorption to be added
Chart: toroidal postition / mm
| 59 | 64 | 69 | 49 | 44 | 39 | 32 | 27 | 22 | 17 | 12 | 7 | 2
toroidal position / mm | 4.5e-09 | 2.5e-09 | 1e-09 | 5.5e-09 | 6e-09 | 6e-09 | 6.5e-09 | 6.5e-09 | 5.8e-09 | 6.4e-09 | 8.5e-09 | 9e-09 | 6.1e-09
Mass 3 desorption to be added

## Slide 11: JET W lamella cuts
Sample name and surface dimensions:
175 (7.8 mm x 5.5 mm)
190 (8.1 mm x 7.7 mm) 5.1 mm before kink
176 (6.8 mm x 5.7 mm)
169 (8.2 mm x 5.7 mm)
Only one 3 mm diameter laser spot possible
Danger: no data if QMS in wrong sensitity range!
1st time to melt W in FREDIS:
Nominal laser max energy 100 J would be sufficient, but current max energy 75 J, not sufficient to melt W
Telescope optics after laser fibre changed to reduce spot size: 1 mm spot melts W, but no const temperature inside spot, only temperature gradient everywhere → spot edge effects dominate → uncontrolled desorption
New telescope optics for 2 mm diameter spot designed, in production
Two 2 mm laser spots on each sample will be possible
bulk W test sample

## Slide 12: JET Sample Overview for LID-QMS @ FZJ
Tile 0 (HFGC14N LH, ILW3) remaining part after coring + core 3b
Tile 1 (14IN G1C, ILW3) remaining part after coring + core 11a
Tile 0 (HFGC??? RH, ILW1-3) remaining part after coring
Tile 1 (14IWG1A, ILW1-3) remaining parts after coring
W lamella cuts
Be limiter 2XR10 from ILW3 for poloidal D profile
IWC 4/2 (2011-2016) 19, 32
2XR10

## Slide 13: In situ LID-QMS setup at JET
1
M1
M2
M3
M4
M5
Torus Hall:
M11: flat, dielectric M15: flat, dielectric
Roof Lab above Torus Hall
Field Lens
movable mirror
cooledBeam Dump
Coaxial Camera
Fibre to pyrometers
Laser fibre
passive Beam Dump
Optics Table
Pyrometers
Total Transmission of Laser beam path: ~53%
Transmission of vacuum window: ~85% Light reflection on surface: ~25%
Total laser power for heating: ~34%
Diode-pumped Fibre Laser: Ytterbium 1071 nm, 25 kW (IPG YLS-25000)
Coaxial camera observation and temperature measurement of the laser spot
3 cylindric mirrors squeeze laser beam to be circular on the target

## Slide 14: Detection System
sub-divertor
Octant 8
QMS5
Laser
RGA3, RGA7, …
QMS1,QMS2
Octant 8
JET torus
The gases desorbed from the laser spot are quantified by Residual Gas Analysis (RGA) using mainly Quadrupole Mass Spectrometers (QMS):
4 QMS in the sub-divertor
3 QMS in the main torus
RGA = Residual Gas Analyser main type used: QMS = Quadrupole Mass Spectrometer

## Slide 15: Laser accessible area
Laser accessible area: upper inner divertor of JET
142 mm
2.29 mm
3.06 mm
tile 1 ≈ 64° ≈ 13°
≈ 27°
tile 0 laser angle ≈ 48° (to surface normal)
Laser spot ellipticity show on front of tile 1:
with beam ellipticity settings for tile 0
Vacuum window
toroidal direction
poloidal direction

## Slide 16: First LID results at JET: toroidal/poloidal scan of divertor tile 0
A fuel retention map can be obtained by evaluating the partial pressure jump:
Tile: RH14W
Tile: RH14W
previously desorbed spot
area of const. D retention (green rectangle) identified

## Slide 17: First Measurements with LID-QMS before T operation
Before this measurement: poloidal and toroidal scan to identify area of const. D retention (green rectangle)
Laser power scan to determine minimum power for complete fuel desorption: 19 kW for 1 ms
19 kW
21 kW

## Slide 18: in situ Measurements with LID-QMS in DT campaign
Measurements during Deuterium-Tritium campaign at JET in September/October 2023:
  4 x 3 cm2 rectangles “cleaned” from fuel by overlapping laser spots before tritium operation
  one rectangle measured every week in “Raster mode”: 99 laser spots every 3 mm every 20 ms to increase the desorbed area
  Additional weekly measurement of rectangle 1
Observations:
  Large signal on mass 4 (D2) in all QMS
  Large signal on mass 5 (DT) only in QMS close to laser spots, but small signal in sub-divertor RGAs (probably in remote ducts/tubes walls saturated with D but not with T)
  Most constant signal with low pumping (cryo pump at liquid N2 and only 1 of 4 turbo molecular pumps pumping) → QMS repetition time (~5 s) << pump-out time
  4 x 3 cm2 “cleaned” rectangle
  99 laser spots

## Slide 19: Tritium Measurements
D2 , (TH) DT, (HD2) HD
Measurement with 99 spots inside an area cleaned 1 week before by overlapping laser spots
TH and HD2 can only have negligible contribution to mass 4 and 5 as there is little H2 (mass 2)
D2
DT
HD

## Slide 20: in situ Measurements with LID-QMS at JET
Measurements during Tritium Clean-up campaign at JET in October/November 2023:
  Monitor the tritium content during different clean-up techniques:
    Backing to 320° C
    ICWC plasmas
    Raised Inner Strike Point plasmas (RISP)
    Glow discharge plasmas
  Measurement by repetition of a poloidal scan of the inner divertor with LID-QMS shifted by few mm after each cleaning method

## Slide 21: in situ Measurements with LID-QMS at JET
LID-QMS on top of tile 1 before and after RISP plasmas for mass 5 (DT)
Final Measurements at JET after last plasma in December 2023: comparison of ex situ to in situ LID-QMS in 70 positions in the laser accessible area on tiles to be retrieved from the torus

## Slide 22: Overview of FULL LID-QMS work
14IWG1A
2019-23
14ING1C
2019-23
LH14W
2011-23
LH14N
2019-23
RH14W
2011-23
14ING1D
2011-23
RH14N
2019-23
14IWG1B
2011-23

## Slide 23: Back-up Slides

## Slide 24: Motivation
Ref [1]: S. Brezinsek et al., Nucl. Fusion 55 (2015) 063021, doi:10.1088/0029-5515/55/6/063021
Problem: Hydrogen isotope retention at the wall
Risk of high tritium release in case of large leak (e.g. ITER limit < 1kg T in the vacuum chamber)
Tritium losses in the fuel cycle
Wall material issues
…
[1]
Ref [2]: K. Heinola et al., J. Nucl. Mater. 463 (2015) 961-965, doi:10.1016/j.jnucmat.2014.12.098
tile 0
tile 1
tile 3
[2]
JET (Joint European Torus)

## Slide 25: ANSYS Laser spot temperature calculation

## Slide 26: QMS Calibration
Quadrupole Mass Spectrometer calibration by short (~1 s) gas puff into the torus
Gas injection module volume V = 1.5 l
Pressure drop Δp in module after injection
N corresponds to the partial pressure jump in the mass spectrometer signal in the torus
Very low partial pressure jump is used, which is similar to the jump during the laser pulse (~1018 D atoms)
repeated on each measurement day to account for different wall loading
injected gas molecules N
QMS5 calibration gas puff
QMS5 with laser pulse
Mass 4 (D2)
Ncalib
Time / s
Nsignal
Background of partial pressure on mass 4 subtracted from both

## Slide 27
Beam Path Overview – Torus Hall
N° | mirror type | focal length / mm | size / mm
8 | flat mirror | infinity | diameter = 140
9 | off-axis parabolic mirror | 5149 | diameter = 140
10 | flat mirror | infinity | diameter = 140
11 | flat mirror | infinity | diameter = 140
12 | flat mirror (motor controlled 2-axis movement) | infinity | diameter = 140
beam path: only mirror-based, no lenses, no fibres
to prevent transparent optic degradation by radiation and to test ITER-like optical components
Focussing
by 2 mirrors at 45° to each other connected rigidly moving together to shorten/extend the beam path
5
4
3
2
1
2
1
4
3
mirror 5
4
mirror 5
3
2
1

## Slide 28: Laser Parameter Scan
The effect of pulse duration is within a factor of 1.3, but comparable to spatial signal scatter
 A pulse duration of 3 ms seems to be adequate
pulse duration | energy | intensity | energy density | heat flux factor
tp / ms | E / J | I / MW/m² | EA / MJ/m² | FHF / MWs1/2/m2
0.5 | 4.5 | 1254 | 0.63 | 28
1 | 6.3 | 884 | 0.88 | 28
2 | 9 | 627 | 1.25 | 28
3 | 11 | 514 | 1.54 | 28
5 | 14 | 397 | 1.98 | 28
10 | 20 | 280 | 2.80 | 28
Complete D desorption requires ca. 1 MJ/m2 incident energy density
corresponding to a heat flux factor of 32 MW√s/m2 on CFC
_
1 ms pulses