## Slide 1
K. Schmid
and SP-C taskholders:
    E. Bernard, T. Morgan, A. Houben , A. Manhard, S. Markelj, T. Schwarz-Selinger, L. Ciupinski, M. Fellinger, D. Primezhofer, Y. Ferro, M. Lavrentiev, R. Bisson, J. Zavaznik, A. Kärcher, M. Vadrucci, V. Nemanic, L. Gao
SP C Updates and Plan
Notes: Please Indicate your subproject

## Slide 2
SP C.1 Transport of Hydrogen through the first wall of fusion devices

## Slide 3: SP C.1 Transport of Hydrogen through the first wall of fusion devices: CEA
Permeation (D,T) through Liquid/Solid interfaces with interface characterization
  Task 1: Characterisation of the oxide grown during the loading phase -> “blank” Wapiti cell
  Task 2 : Tritium permeation at RT through Pd-coated Eurofer samples
Task 1: The blank Wapiti cell was built and tested in the glovebox environment but still sample is contaminated
  we have a relevant sample with low T activity (only background contamination) : possibly below T exemption limit which broadens potential analysis setups at reach
Task 2: Samples were coated with Pd by the team of M. Cekada (JSI) on both sides, then loaded with 250 mbar of pure T2 at 150°C to study permeation with/without water downstream
  Factor 100 increase in the permeated activity in the presence of water downstream
  Activity in downstream air is the same order of magnitude, whether we have water downstream or not
  Different behavior when Eurofer surface is protected: permeation flux establishes at 1,5·103 Bq/day in Eurofer vs 7,7·103 Bq/day in Eurofer coated with Pd corrosion/oxidation play a role
Chart: Activity in water
| 0 | 5.1215277777737356 | 15.881944444437977 | 36.086805555554747 | 40.055555555554747 | 57.055555555554747 | 77.097222222218988
 | 24.12 | 121876.6 | 261137.345 | 619925.52 | 827807 | 1235082.375 | 1745066.65
Chart: Activity in air above water
| 7.8791666666656965 | 8.7020833333299379 | 9.7784722222204437 | 9.9777777777781012 | 12.977083333331393 | 16.747916666667152 | 21.729166666664241 | 21.756944444445253 | 23.738888888889051 | 33.946527777778101 | 43.935416666667152 | 47.915277777778101 | 64.956944444442343 | 84.698611111110949
 | 3803 | 6581 | 9692 | 13570 | 15396 | 21354 | 22185 | 24173 | 25324 | 28103 | 31498 | 36700 | 41553 | 56742
Notes: Task 1 hampered by T content in oxidised sample to be analyzed externally -> Try again
Task 2: Completed.
Most activity in Water
Activity in air is the same idependent on downstream interface
-> More permeation in presenc of water

## Slide 4: SP C.1 Transport of Hydrogen through the first wall of fusion devices: CEA
Permeation (D,T) through liquid/solid interfaces with interface characterization
Pressure variation: EUROFER + Pd
one pristine EUROFER with "wapiti oxide".
"wapiti oxide" characterization.
Autoradiography T surface measurement
Oxide characterization still open.
RAMAN , SIMS maybe Sacley.
Pressure variation in April
KOM Feb-2024
Notes: Task 1 hampered by T content in oxidised sample to be analyzed externally -> Try again
Task 2: Completed.
Most activity in Water
Activity in air is the same idependent on downstream interface
-> More permeation in presenc of water

## Slide 5: SP C.1 Modelling of Hydrogen Transport properties in the first wall: CEA
The solution of H was determined at the W/Cu interface
Deliverable: Diffusion properties of hydrogen at the W/Cu interface: activation barriers for MRE modeling
Grand-canonical ensemble is used
H reservoir is also considered as a real gas
H solubility is determined as function of temperature and chemical potential.
NEB calculations were performed at the W/Cu interface:
Phonon properties of H at the W/Cu interface
Vibrational frequencies of H at the W/Cu were computed.
Due to the distortion of the Cu network, two diffusion paths have been considered (pink & green).
The activation barriers were determined for each path.
An additional path connecting the two previous ones was also considered (blue)
 See presentation by Y. Ferro
Notes: • We previously built a DFT model of the W/Cu interface where a hexagonal. The Cu network reconstructs at the interface where it adopts a hexagonal close packed structure. This work was submitted to Nuclear Materials and Energy Journal – minor revisions are completed, and the paper is resubmitted.
• We also, previously, determined the most stable interstitial positions for H at the W/Cu interface. These positions are plotted in blue (octahedral) and red (tetrahedral) on the figure above.
• We determined the vibrational frequencies of H atoms at the most stable interstitial positions.
• Those vibrational frequencies were used in a thermodynamic model to determine the solubility as a function of the temperature and chemical potential.
• we considered the grand-canonical ensemble where H reservoir was treated as real and ideal gas. Our model was validated against experimental data of H solubility in W and Cu bulks.
• H solubility at the W/Cu interface is higher at the plane of the interface than in the W and Cu networks.
• A draft paper is completed.
• In the following, nudged elastic band (NEB) calculations were carried out to determined the activation barriers that determine the diffusion properties. Due to the Cu reconstruction, two diffusion paths were considered: the pink and the green.
• It was obtained that the pink path has lower values of activation energies than the green one, which means that it is most energetically favorable for hydrogen to diffuse through it (see graphs).

## Slide 6: SP C.1 Transport of Hydrogen through the first wall of fusion devices: CEA
Kinetic of hydrogen transport across the W/Cu interface and modeling distortions in Cu at the W/Cu interface
0D model of the interface.
Identification misfit defects by MD at the W/Cu interface with EAM potential
Many different interfaces between W/Cu due to different orientation
Build kinetic model (activation barriers etc.)
Different W/Cu orientation at the interface.
DFT & MD model of the interface. Build an MD potential.
Average model of H at interface over different interfaces.
KOM Feb-2024
Notes: • We previously built a DFT model of the W/Cu interface where a hexagonal. The Cu network reconstructs at the interface where it adopts a hexagonal close packed structure. This work was submitted to Nuclear Materials and Energy Journal – minor revisions are completed, and the paper is resubmitted.
• We also, previously, determined the most stable interstitial positions for H at the W/Cu interface. These positions are plotted in blue (octahedral) and red (tetrahedral) on the figure above.
• We determined the vibrational frequencies of H atoms at the most stable interstitial positions.
• Those vibrational frequencies were used in a thermodynamic model to determine the solubility as a function of the temperature and chemical potential.
• we considered the grand-canonical ensemble where H reservoir was treated as real and ideal gas. Our model was validated against experimental data of H solubility in W and Cu bulks.
• H solubility at the W/Cu interface is higher at the plane of the interface than in the W and Cu networks.
• A draft paper is completed.
• In the following, nudged elastic band (NEB) calculations were carried out to determined the activation barriers that determine the diffusion properties. Due to the Cu reconstruction, two diffusion paths were considered: the pink and the green.
• It was obtained that the pink path has lower values of activation energies than the green one, which means that it is most energetically favorable for hydrogen to diffuse through it (see graphs).

## Slide 7: SP C.1 Transport of Hydrogen through the first wall of fusion devices: MPG
Permeation of H isotopes through W heavy alloys (W/Fe-Ni)
Question: Transition of D between W and Fe-Ni phases
Investigate by ion-driven permeation (IDP)
  Produced layered model systems of Fe-Ni matrix on recrystallized W foil
  Measured IDP starting from matrix and W sides
W  matrix: practically identical to only W
  Issue: oxidation of downstream Fe-Ni
Matrix  W: strongly suppressed
  Issue: Fe-Ni sputtering, W island segregation
  Gas permeation not negligible!
Previous hypothesis qualitatively confirmed!
To Do: gas pressure calibration, modelling
Notes: Question how is D transported through W-heavy alloys: Transport in W grains vs Fe/Ni matrix

## Slide 8: SP C.1 Transport of Hydrogen through the first wall of fusion devices: MPG
Measurement and modelling of Ion Driven Permeation in "W-heavy alloys"
Measure permeation through HPM1850 and compare to modelling
Move from model system to real HPM
Modeling of 2D diffusion pathways
KOM Feb-2024

## Slide 9: SP C.1 Transport of Hydrogen through the first wall of fusion devices: JSI
Compare D permeation through W with D atoms and 300 eV/D ions
Task: Study of D permeation in H-prefilled W foil
Observations
Saturation of damaged layer by D after 28h – 3 times faster compared to no H-prefilled foil
Different saturation D concentration for recrystallized foil and stress-relieved foil ? (no explanation for that)
Experiment
Exposure of recrystalized or stress- relieved 50 µm W foils with protective layer
Exposure to H ions (flux ?x1018 H/m2s) at 600K for 24h
Exposure to D ions – flux 4x1018 D/m2s
Deliverable: PWIE-SP C.1.T-003-D004
Status: completed
Facilities: accelerator 8 days
Linked WP or TSVV: if required

## Slide 10
Study D-permeation on H-prefilled W foil at low temperatures
Permeated amount of D at low temperatures (400K, 500K)
Prefill @600K
D-iso ex at 400-500K
Start in June
KOM Feb-2024
SP C.1 Transport of Hydrogen through the first wall of fusion devices: JSI
Notes: Task 1 hampered by T content in oxidised sample to be analyzed externally -> Try again
Task 2: Completed.
Most activity in Water
Activity in air is the same idependent on downstream interface
-> More permeation in presenc of water

## Slide 11: SP C.1 Transport of Hydrogen through the first wall of fusion devices: CEA
Model D-permeation on H-prefilled W foil at low temperatures
Model permeation through H-pre-filled W
Use diffusion trapping code
Grain boundary diffusion?
Grain boundary diffusion
Swapping therm for iso-ex
First without pre-fill
600K iso-ex also works in classic desc.
KOM Feb-2024

## Slide 12: SP C.1 Transport of Hydrogen through the first wall of fusion devices: IPPLM
TEM observations of nanobubbles in tungsten subjected to He-irradiation and annealing
Determination of size and distribution of nanobubbles in defected zone
Density of nanobubbles depends on the distance from the surface
Size of the bubbles is not related directly with the density

## Slide 13
TEM analysis of annealed, He implanted W. In cooperation with MPG
Analysis of void formation
M. Zibrov (MPG) provides samples.
First samples ready.
Start in March
KOM Feb-2024
SP C.1 Transport of Hydrogen through the first wall of fusion devices: IPPLM

## Slide 14: SP C.1 Transport of Hydrogen through the first wall of fusion devices: OEAW/VR
Task: Studying the influence of (re-deposited) W on Eurofer on D retention (OEAW, VR)
Deliverable: Variation of TDS with W-layer thickness on Eurofer
Two comparable TDS experiments were performed in close collaboration with UU:
  It was found that the top W layer functions as outgassing barrier:
  → higher T needed to release D retained in Eurofer + W layer
  → overall amount of retained D is larger with additional W layer
exp. 1:
TDS on D loaded Eurofer layer
exp. 2:
TDS on D loaded Eurofer + W coating layer structure

## Slide 15
Studying the influence of (re-deposited) W/EUROFER layers on D retention
Influence of inverted layer system EUROFER layer on D-implanted W layer on D retention
Follow up Study
QCM & TDS & IBA
Start in May
KOM Feb-2024
SP C.1 Transport of Hydrogen through the first wall of fusion devices: OEAW/VR

## Slide 16
SP C.2 T retention Release from B layers
New in 2024

## Slide 17
Study the branching ratio of desorption products from B layers implanted with D ions
Branching ratio of deuterated desorption products from B-layers during TDS
Deuterium fluence effect on retention and desorption branching ratio from B-layers
Line of sight TDS
See molecules
Solid B-sample, sintered
Start end of March
Use D/H to create isotopolgues to detect cracking patterns
KOM Feb-2024
SP C.2 T retention Release from B layers: CEA

## Slide 18
Evaluation of D/B ratio in co-deposited boron
Sputter target upstream or
Di-borane injection or
Pulsed laser deposition in-situ
In-situ analysis of B/D layers. (NRA)
Student starts in April
KOM Feb-2024
SP C.2 T retention Release from B layers: DIFFER
Data on D/B ratio as function of B layer growth rate

## Slide 19
Influence of B layer on permeation
B layers with different amounts of D (HiPIMS)
TDS & Permeation
Substrates: EUROFER for permeation W for TDS
Start in Second half of 2024
KOM Feb-2024
SP C.2 T retention Release from B layers: JSI
Permeation with vs. without B layer on EUROFER on the inlet side

## Slide 20
Gas driven permeation and hydrogen retention in boron coated steel or W
B coated steel permeation
B coated steel and W w.r.t retention
Magnetron Sputtered layers
360L
Project already running
D-ion beam loading 250eV
B on both sides
KOM Feb-2024
SP C.2 T retention Release from B layers: FZJ
Influence of boron coatings on the hydrogen permeation and retention on W or Steel

## Slide 21
SP C.3 Influence of He, high-flux D and impurities on Hydrogen retention and transport

## Slide 22
TEM analysis W damaged at high temperatures. In cooperation with MPG IPP
Analysis of void formation
Samples from L. Hess (MPG)
Three samples ready
KOM Feb-2024
SP C.3 Influence of He, high-flux D and impurities on Hydrogen retention and transport: JSI

## Slide 23
Influence of surface He pre-implantation on D retention in W
SP C.3 Influence of He, high-flux D and impurities on Hydrogen retention and transport: JSI
Sabina Markelj / Thomas Schwarz-Selinger
 He implanted surface features increased recycling

## Slide 24
Influence of surface He pre-implantation on D retention in EUROFER
D uptake and retention in EUROFER as a function of He fluence
KOM Feb-2024
SP C.3 Influence of He, high-flux D and impurities on Hydrogen retention and transport: JSI

## Slide 25
SP C.4 Influence of n-damage on Hydrogen retention and transport

## Slide 26: SP C.4 Influence of n-damage on Hydrogen retention and transport: MPG
Task: Temperature needed to anneal trap sites in He containing displacement damaged EUROFER
Experiment:
20 MeV W ion irradiation at 290 K – 0.6 dpa
0.5 MeV He implantation at 290 K – 0.6 at. %
D plasma exposure (1e25 D/m2) at 370 K
Post-irradiation annealing followed by D loading and NRA
Results:
The presence of He atoms increases D retention by about 5 times compared with to the displacement damage case
D is released from He-containing displacement-damaged EUROFER at 520 K
He-related trap sites can survive up to 620 K
Annealing of trap sites in He containing EUROFER

## Slide 27
Trap site generation by displacement damage in EUROFER at high T
Compare trap concentration for annealed EUROFER and EUROFER damaged at same high-T.
Annealing of traps sites generated in EUROFER at high-T.
KOM Feb-2024
SP C.4 Influence of n-damage on Hydrogen retention and transport: MPG
Repeat with samples damaged at high temperature
Irradiation starts in March

## Slide 28
D plasma exposure of high-temperature self-ion irradiated W to study the dynamics of D trapping and release from cavities in W
D concentration profiles and TDS spectra from W samples damaged at high-T as a function of D fluence.
KOM Feb-2024
Experiments under way
Four samples ready
SP C.4 Influence of n-damage on Hydrogen retention and transport: MPG

## Slide 29
SP C.4 Influence of n-damage on Hydrogen retention and transport: MPG/FZJ
What we did and why: LIBS exhibit great potential in online determination of fuel retention after proper signal calibration. Reference D-containing W samples are required to further explore the LIBS technique.
Which experiments/calculations were performed 1. Recrystallization of 4x double-forged W samples 2. Self-damage (10.8 MeV W, 0.23 dpa) for 3x samples 3. D 1e25/m2 loading at PlaQ (5eV/D, 370K, 4x): D decoration 4. Partial degassing of 2-PlaQ-loaded samples (450 & 600 K) 5. NRA D depth profiling of 4-PlaQ-loaded samples 6. Dual-pulse LIBS measurements of the 4 PlaQ-loaded samples
Brilliant Results: NRA and LIBS yields “identical” depth profile
Things will be done in 2023 and early 2024:
1. D/W and He/W co-deposited layers preparation 2. LIBS and ERDA measurements for He/W layer 3. Summary
Notes: Task 1 hampered by T content in oxidised sample to be analyzed externally -> Try again
Task 2: Completed.
Most activity in Water
Activity in air is the same idependent on downstream interface
-> More permeation in presenc of water

## Slide 30
Quantification of LIBS
Sensitivity study to determine the detection limit (LIBS vs LIA-QMS).
KOM Feb-2024
Samples underway
Experiments in March and April
SP C.4 Influence of n-damage on Hydrogen retention and transport: MPG/FZJ