## Slide 1: Boronization in ITER: ITER requests and PWIE activities
K. Schmid

## Slide 2: Content
ITER’s open questions w.r.t boron
Hydrogen retention in boron co-deposits
Summary
Boronization layer lifetime

## Slide 3
Literature review of hydrogen retention in boron [S. Krat ISFN]
Reduce retention in W by 50%
by thermal desorption and isotopic exchange

## Slide 4: ITER’s open questions w.r.t boron taken from 34th ITPA DivSOL Uji Kyoto – T. Wauters
Need for boronization with high Z plasma facing components (PFCs)
Drawback of starting operation with W PFCs and no-boronization (e.g. plasma start-up/ramp-up)
Taken from ITPA DivSOL Kyoto by Andrei Pshenov
SolPS simulation of ramp on inner heat shield
Hampered by excessive W self-sputtering and resulting radiation (75% of PSOL)
Boronization could reduce W erosion :
Reduce low-Z impurity concentration (likely)
Cover W areas from erosion (unlikely/difficult)
Simulations rather preliminary, e.g. lacks prompt re-deposition

## Slide 5: ITER’s open questions w.r.t boron taken from 34th ITPA DivSOL Uji Kyoto – T. Wauters
Need for boronization with high Z plasma facing components (PFCs)
Drawback of starting operation with W PFCs and no-boronization (e.g. plasma start-up/ramp-up)
Duration of boronization effects for:
W PFC coverage
Impurity gettering for good vacuum conditions
Reason for deterioration of vacuum conditions between boronization
Optimum application of boronization
Required thickness
Frequency of boronization:
Only once for start up vs. repeatedly during campaign
Boronization scheme:
Glow discharge (requires field ramp down, but coats remote areas)
ICWD (works with field but only locally)
Dropper (works during diverted phase, deposition location?)
Boron migration/layer lifetime
Boron migration/layer lifetime

## Slide 6: ITER’s open questions w.r.t boron taken from 34th ITPA DivSOL Uji Kyoto – T. Wauters
Formation of boron deposits and fuel retention
Location of boron deposits following plasma operation
Boron migration/layer lifetime
Boron layer in-situ reactivation (oxygen removed from layers in-situ leaving boron) by GDC/ ICWC
Layers may survive for a long time in remote ares
 reactiveate their impurity gettering properties
 Reduce number of required boronizations
Content of hydrogen, oxygen, etc., in boronized layers
Depends on layer structure
 Layer growth rate dx/dt
 Temperature T
 Particle energy E
...
Problem is similar to C or B: what is the D/B ratio
D/B (E,T, dx/dt,..)
 Most input from PWI

## Slide 7
Hydrogen retention in boron co-deposits
D/B (E,T, dx/dt,..)
Mainly based on the work by A. Annen

## Slide 8: Hydrogen retention in boron co-deposits
Layer stability
A. Annen et Al, J. non cryst. Solids 209 (1997) p. 240
Only films grown at high bias are chemically stable under ambient atmosphere
Impurity getter layers should NOT be stable under ambient atmosphere
 ITER „relevant“ layers will be hard to analyse
Can‘t just carry them round exposed to ambient atmosphere

## Slide 9: Hydrogen retention in boron co-deposits
H-content
A. Annen et Al, J. non cryst. Solids 209 (1997) p. 240
At T < 375K
Depending on energy (bias) and pressure

## Slide 10: Hydrogen retention in boron co-deposits
H-content
A. Annen et Al, J. non cryst. Solids 209 (1997) p. 240
At T < 375K
Depending on energy (bias) and growth rate
Growth rate depends mainly on pressure
pressure dependence may actually be a growth rate depenence?

## Slide 11: Hydrogen retention in boron co-deposits
H-content
M. Saß et al, J. Appl. Phys. 82 (4) 1997 p. 1095
At T < 375K
At 600K drops by factor 2.3
 Depending on energy (bias), growth rate and temperature
H density drops from 3.5 at 300K to 1.5 at 600K  Factor 2.3

## Slide 12: Hydrogen retention in boron co-deposits
H-content
Compare to C:
R.P. Doerner at Al Nucl. Fusion 49 (2009) 035002
a-BH layers retains H similar or slightly lower than a-CH layers
At T < 375K
At 600K drops by factor 2.3
 Depending on energy (bias), growth rate and temperature

## Slide 13: Hydrogen retention in boron co-deposits
H-release
A.Annen PhD Thesis, IPP-Report: IPP 9/114 April 1997
Release starts at ~500K
Relase temperature increases with C content
These were „stable“ layers!
 May be different for „relevant layers“

## Slide 14
Boronization layer lifetime
Boron migration/layer lifetime

## Slide 15: Boronization layer lifetime
Sputter yield of boronization layers is not well known:
Comparison of sputter yields of amorphous (a-BH) B/H layers [1] with pure B [2] and SDTrimSP simulations of a-BH.
[1] PhD A. Annend unpublishd
[2] „Sputtering data“ IPP report 9/82 Feb. 1993
a-BH layers sputter ~1.5 x more than pure B
„Best“ match to experimental data using a surface binding energy fo 3.5 eV in SDTrumSP
Build a yield data base: D, Ne, B, W  B/W mixtures
Y(E, , CW, CB)
R(E, , CW, CB)

## Slide 16: Boronization layer lifetime
Sputter yield of boronization layers is not well known:
Chemical erosion is much lower than for a-CH layer
Neglect for now in WallDYN3D calculations
A. Annen and W. Jacob Appl. Phys. Lett. 71 (10), 8 September 1997

## Slide 17: Boronization layer lifetime
Sputter yield of boronization layers is not well known:
Computed B self sputtering using „validated“ SDTrim.SP settings
For expected oblique angles B yields exceed 1
WallDYN has „difficulties“ with run-away self-sputtering
 Limit impact angles to 40° for now

## Slide 18: Boronization layer lifetime
DIII-B benchmark experiment
EMC3-Eirene plasma case with grid only touching divertor targets
Quite high Te at targets ~30eV
Dominant charge states C+4, B3+
High impact energies:
  3 q Te + 2 Ti
Impact angle given sheath ExB and oblique B-field angle
 ~65° minus average surface angle ~20° = 45°
Self sputtering yield of C at 45° with 420eV ~0.8
 Very high!
Assume 1% C-chemical erosion for D, D-CX
Deposition of B/C on dimes head?
Neutral B source from “Dust Injection Simulator (DIS)”
(PPPL colaboration F. Effenberg)

## Slide 19: Boronization layer lifetime
DIII-B benchmark experiment
WallDYN3D matches surface analysis (...by chance)
(Experimental seeding strength = 2.8E20 B/s)

## Slide 20: Boronization layer lifetime
Use ITER plasma background with Ne impurities a hot, stagnant () far SOL
Put a thin B layer on top of W in main chamber and „measure“ the erosion rate
Migration matrix not perfectly normalized
B is lost at edge of calculation grid: PFR
In reality B probably ends up as dust down there
B is eventually lost from „Plasma“
At t=0
  B eroded from main chamber
  and
  deposits in divertor
B re-deposition slows down B erosion
[1020 B/(m2 s)]

## Slide 21: Boronization layer lifetime
Use plasma background 2481-00g with Ne impurities a hot, stagnant () far SOL
Put a thin B layer on top of W in main chamber and „measure“ the erosion rate
Use „measured“ erosion rate to estimate life time of a 100 nm layer
B remains in plasma shadowed regions, only eroded by CX
Lifetime of 100 nm B
(erosion only)
Lifetime of 100 nm B
(NET-erosion only)
Lower limit
Upper limit
Significant fractions of the first wall have lifetime > 1000 s.
[s]

## Slide 22: Boronization layer lifetime
Use plasma background 2481-00g with Ne impurities a hot, stagnant () far SOL
Put a thin 1nm B layer on top of W in main chamber and „measure“ the erosion rate
Re-plenish B layer with a B dropper during diverted discharge?
t=1 s
t=10 s
t=100 s
B-conc.
B dropper re-plenishes B at heavily loaded areas
t=100 s
B quickly erodes
B deposits on inner target and baffles...
...as long as source lasts
1021 B/s dropped in each 20° sector
Depends on local erosion vs. dropper rate
Not very efficient at coating weakly loaded areas
Very pre-liminary!
B dropper modelled as B atom point source in SOL
Collaboration with PPPL for more realistic dust modelling

## Slide 23: Summary
ITER wants/needs boronization to getter impurities and hopes B to maybe even cover W to reduce W ingress
From a lab/PWI perspective this requires:
a-BH erosion yields (chemical erosion?)
H/B ratios as function of deposition rate, particle energy and temperature
Look for weakly sticking BxHy species that might migrate to remote areas in ITER
Lab experiments will be hampered by the fact that relevant layers are unstable under ambient atmosphere
Deposit a-BH layer in e.g. a magnetron (varying dx/dt, E and T)
Cover them by e.g. Cu
Analyse H/B ration in accelerator
Once H/B(dx/dt, E, T) is known: WallDYN3D needed to predict B migration, layer formation and H-retention
Depending on „boronization scheme“ coupling to dust transport code needed