## Slide 1: Sputtering of pristine and D decorated W surfaces by various ions (MD)
Fredric Granberg
Faith Kporha, Alexandre Bergero, Kai Nordlund

## Slide 2: Introduction Sputtering of W
Yamamura & Tawara, Atomic Data and Nuclear Data Tables 62 (2) 1996 149-253
Exp. sputtering yields
  Effect of ion and energy
  Usually polycrystalline
  For self-ion, only the net
    ”reflection” = ”sputtering”

## Slide 3: METHODS Molecular Dynamics simulations
Classical MD simulations with different interatomic potentials
  The Mason et al. EAM and the Li et al. Tersoff-type potential for W-W, W-H and H-H
  Purely repulsive ZBL potential between Ne-W, Ne-H, Ar-W and Ar-H
Single impact simulations
  Good for understanding the base phenomena
  Caveat, might not be the most representative of experiments
    Studies can be “easily” extended to multiple impact scenario
      Main limitation is the CPU time, and the sequential workflow which is needed for these
      Can not as easily be done for other than low-index surfaces

## Slide 4: METHODS Simulation setups
Low index surface
Arbitrary surface
Schlueter et al. Phys. Rev. Lett. 125:225502 (2020)
BCA/RIA + MD

## Slide 5: METHODS Simulation example (Note: not linear time)

## Slide 6: METHODS Setup
Sample:
  100, 110, 111 and 112 surface orientations, periodic cell
  0%, 2.5%, 5% and 10% D (average concentration in topmost layers)
Ion: Ar, Ne and W
Energy: 100eV and 200eV, single impact
Incoming angle: 0, 15, 30, 45, 60 and 75 degrees
For random and amorphous surfaces, the non-periodic half-sphere setup
  50 – 1000eV single impact Ar irradiation

## Slide 7: METHODS D-decorated cells
Side-view and top-view of the cells at different D concentrations
Pristine 2.5% 5% 10%

## Slide 8: METHODS Analysis
Sputtering yield
Reflection yield
Outgoing angles
Outgoing particle energy
In MD all are inherently recorded
For tungsten self-irradiation, sputtering can be split into reflection and sputtering
Detected experimentally
Detected experimentally, self-ion problematic
Can be detected experimentally
Can be detected experimentally

## Slide 9: RESULTS
Ar -> W and D-decorated surfaces
  Surface orientation effect for Ar -> W
  D-decoration effect for Ar -> W
  Mechanisms present
Ne/Ar/W -> W
  Ion-type effect on W surfaces
  Ion-type effect on D-decorated surfaces
Parameter study of Ar -> W
D -> W surfaces

## Slide 10: RESULTS Surface orientation effect for Ar -> W (pristine)
Tungsten sputtering a function of incoming angle
Mason et al. Li et al.
100 eV 200 eV 100eV 200eV
Both potentials agree well in both yields and trends, agrees with previous results

## Slide 11: RESULTS D-decoration effect for Ar -> W
Deuterium sputtering from 10% D-decorated surfaces
Mason et al. Li et al.
100 eV 111 surface 200eV 100 surface
Both potentials agree well in both yields and trends
Increased D concentration linearly increase the D sputtering

## Slide 12: RESULTS D-decoration effect for Ar -> W
Tungsten sputtering for 10% D-decorated surfaces
Mason et al. 100eV Li et al. 200 eV
Pristine 10% D Pristine 10% D
Potentials give opposite trend, D-decoration increase sputtering in Mason et al. and decrese sputtering in Li et al.

## Slide 13: RESULTS Mechanisms present
Stable D position on W surfaces (100)
Energy required for sputtering
Mason et al. Li et al
Mason et al. shows correct according to DFT
Mason et al. Li et al

## Slide 14: RESULTS Ion-type effect on pristine W surfaces
Tungsten sputtering for different ion species
Mason et al. 100 eV
100 surface 110 surface 111 surface 112 surface
Ar and Ne quite similar, except the close packed 110 surface
  Smaller atom, can penetrate easier and transfer energy in correct direction? (Educated guess!)
W different, due to sticking to surface at small angles, and reflection at large angles

## Slide 15: RESULTS Ion-type effect on pristine W surfaces
Total sputtering (sputtering + reflection) of tungsten by tungsten-ions
Mason et al. 100 eV Li et al. 200eV

## Slide 16: RESULTS Ion-type effect on D-decorated surfaces
Tungsten sputtering for some surfaces and energies for pristine and 10% decorated surfaces
Mason et al.
(100) 100 eV (100) 100 eV 10% D (111) 200 eV (111) 200eV 10%
Again, in the Mason et al. potential the sputtering is increased due to the deuterium present

## Slide 17: RESULTS Ion-type effect on D-decorated surfaces
Deuterium sputtering from 10% D-decorated surfaces by different ion species
Mason et al.
(100) 100 eV 10% (100) 200 eV 10% (110) 100 eV 10% (110) 200eV 10%
Ar and Ne similar, except at low energy when maximum energy transfer is different
W different from the others, due to attraction to D and the surfaces themselves

## Slide 18: RESULTS Parameter study of Ar -> W
Still running
  500eV and 1000eV
  Other incoming angles
0deg | 100 | 110 | 111 | amo | rand | rand_min | rand_max
50 | 0 | 0 | 0 | 0 | 0 | 0 | 0
75 | 0.004 | 0 | 0.0028 | 0.0032 | 0.00294 | 0 | 0.0092
100 | 0.128 | 0.042 | 0.0892 | 0.067 | 0.06184 | 0.019 | 0.1258
200 | 0.4338 | 0.4532 | 0.4034 | 0.4062 | 0.415 | 0.379 | 0.4584
300 | 0.7428 | 0.7278 | 0.5532 | 0.6166 | 0.64055 | 0.5536 | 0.7088
60deg | 100 | 110 | 111 | amo | rand | rand_min | rand_max
50 | 0 | 0 | 0 | 0.0002 | 1.33E-05 | 0 | 0.0004
75 | 0 | 0 | 0 | 0.0056 | 0.00554 | 0 | 0.0218
100 | 0 | 0 | 0.0106 | 0.028 | 0.03014 | 0 | 0.0628
200 | 0.1446 | 0.001 | 0.2328 | 0.276 | 0.27487 | 0.1314 | 0.3392
300 | 0.643 | 0.1302 | 0.5464 | 0.5868 | 0.62169 | 0.3312 | 0.713
Chart: 
| 50 | 75 | 100 | 200 | 300
100 | 0 | 0.004 | 0.128 | 0.4338 | 0.7428
110 | 0 | 0 | 0.042 | 0.4532 | 0.7278
111 | 0 | 0.0028 | 0.0892 | 0.4034 | 0.5532
amo | 0 | 0.0032 | 0.067 | 0.4062 | 0.6166
rand | 0 | 0.00294 | 0.06184 | 0.415 | 0.64055
rand_min | 0 | 0 | 0.019 | 0.379 | 0.5536
rand_max | 0 | 0.0092 | 0.1258 | 0.4584 | 0.7088
Chart: 
| 50 | 75 | 100 | 200 | 300
100 | 0 | 0 | 0 | 0.1446 | 0.643
110 | 0 | 0 | 0 | 0.001 | 0.1302
111 | 0 | 0 | 0.0106 | 0.2328 | 0.5464
amo | 0.0002 | 0.0056 | 0.028 | 0.276 | 0.5868
rand | 1.3333e-05 | 0.00554 | 0.03014 | 0.27487 | 0.62169
rand_min | 0 | 0 | 0 | 0.1314 | 0.3312
rand_max | 0.0004 | 0.0218 | 0.0628 | 0.3392 | 0.713

## Slide 19: RESULTS D -> W surfaces
W sputtering
D sputtering
D ion reflection
W ”incorrect ”sputtering
1 keV D -> (100) W surface and 10% D decorated surface
Statistics still low, but there is an effect (unfortunately)
  This is the case for channeling directions, probably not others
  The higher the energy / lower the ion mass, the worse it is

## Slide 20: OUTLOOK Current status
Ar -> W and D-decorated surfaces
  Sputtering/reflection as a function of D decoration and surface orientation
  Submitted to JNM (available on the pinboard)
Ne, Ar and W -> W and D-decorated surfaces
  Sputtering/reflection as a function of D decoration, ion type and surface orientation
  Outgoing angle and energy distributions
  Simulations are completed, analysis ongoing and article under writing
Ar -> W low-index, amorphous and random surfaces
  Ongoing simulations as input for ERO2.0 simulations / comparison to SD TRIM SP

## Slide 21: OUTLOOK Current status
The irradiation of W by D ions is ongoing
  Due to low sputtering yields, 100k + impacts are needed for statistics per data point
  The cells needed are large compared to heavier ions
    Extremely CPU heavy and a lot of CPU time is needed
    We aim to obtain a “correction factor” that can be used, to use small cells and then add a correction to these results
Development of W-O-H & W-B interatomic potential ongoing
  Also part of TSVV-7 project
We can obtain many parameters for different setups, but we need to know what!

## Slide 22: THANK YOU FOR YOUR ATTENTION
F. Kporha, K. Nordlund and F. Granberg, Sputtering of deuterium decorated tungsten surfaces by argon: A molecular dynamics study, Submitted for publication in Journal of Nuclear Materials
F. Kporha, K. Nordlund and F. Granberg, Effect of ion type on the sputtering of pristine tungsten and deuterium decorated tungsten surfaces, Under writing