## Slide 1: WP PWIE: Plasma-Wall Interactions and Exhaust
2025 Planning Meeting
Forschungszentrum Jülich (lead lab)
Heinrich-Heine-Universität Düsseldorf
Sebastijan Brezinsek (PL)

## Slide 2: Scope: Work Package Plasma-Wall Interactions and Exhaust
MAGNUM
3D erosion & deposition modelling
Tungsten, (Beryllium), Boron
AUG
Radiative divertor
Tungsten +
seed gas (Ne, Ar, Kr)
Particle and heat flux
Tungsten + Deuterium
Fuel (Tritium) retention
Tungsten + Deuterium/Helium
[J. Romazanov]
[T. Morgan]
[S. Markelj]
[M. Bernert]
Focus on ITER and DEMO materials, H and isotopes, He, seeding gases, and impurities
Goal: steady-state operation
Support in WPW7X exploitation
operating with Graphite
towards Tungsten PFCs
Material qualification and synergistic effects of W and advanced W materials
[K. Schmid]
Recombining plasmas in PSI-2 and MAGNUM-PSI
Support in WPTE exploitation
In AUG, WEST and JET in PWIE
area with metallic PFCs
PWI diagnostic development
ITER

## Slide 3: Overview 2025
Original structure WBS and large fraction of activities prevail intact
PSO: Michael Reinhart
AI: LIBS spectra
AI: SOL simulation
Budget in July

## Slide 4: Overview 2025
Original structure WBS and large fraction of activities prevail intact (evolution)
In view of the ITER re-baselining and abandon of Be and usage of W and W + B instead
  General activities related to Be (LIBS, fuel recovery assessment, ITER simulations etc.) were closed in 2023
  Remaining activity is the JET-DT tile analysis (LIBS and ex-situ) with Be and W tiles to assess retention, migration, dust formation. Data feeds into benchmark of PWIE codes to validate physics models (low Z can be exchanged)
  Number of new activities to high priority ITER items related to clean W first wall operation (e.g. W sputtering and screening in limiter configuration, CXN fluxes etc.) and usage of boronisation (e.g. gettering, homogeneity) added
Moderate change in facility portfolio in 2025
  No JULE-PSI / reduced JUDITH-3 in operation in 2025 => transfer into HML in 2025
  Risk mitigation: use more PSI-2 (all B aspects new) and MAGNUM (mainly W aspects)
  Risk mitigation: use GyM for B studies => linear machine budget will be reorganised
  Use HADES as JUDITH replacement if needed

## Slide 5: Focused Topic 2025: Layer formation/properties in full-W machines
SP B: Understanding the formation of WEST-like deposits with W
  Final analysis of WEST-like deposits from long-pulse operation: stability and dust conversion factor
  Mimic WEST-like divertor plasma conditions and pulses in MAGNUM-PSI (and PSI-2)
    Thermal cycling of actively cooled W PFCs in NAGNUM-PSI and secondary upstream W source
    Role of surface temperature, thermal stresses, impurities, oxide formation, duty cycle etc. as parameters
    Pre- and post-characterisation and spectroscopy
  ERO simulations for linear plasma experiments (same A&M data for WEST)
SP D: Simulation of WEST long-pulse plasmas in full 3D geometry (incl. ripple)
  Plasma boundary simulation with SOLEDGE3X-EIRENE
  ERO2.0 simulation of WEST long-pulse devices including W local redeposition and MB shaping
SP A: HHF exposure of W MB exposed in WEST
  Damage evolution under e-beam loading
  Deposit stability assessment
Linked to WP TE and WP DIV

## Slide 6: Focused Topic 2025: Composition of first wall fluxes and far-SOL PWI
SP D: Simulation of fluxes to the first wall and W sputtering
  CXN and ion flux composition in simulations for COMPASS-U, AUG, (JET), ITER and DEMO
  SOLPS-ITER H-mode plasma simulations (ELM-averaged)
  Poloidal distribution of CXN with energy and angular distribution
  Role of inner and outer wall W source variation with change of CXN, D+, impurity ionisation level
  ERO2.0 simulations / WallDYN-3D simulations for AUG, JET (with W PFC,) ITER
  Comparison of cases with extended grid to the wall and normal grid to assed far-SOL profiles
SP B: Gross and net W erosion at the first wall (manipulators)
  Experiments with RIG/ROG variation and light impurity seeding
  Pre- and post-characterisation of materials with different sputtering threshold and FIB cuts
  Comparison with PSI-2 plasma experiments
  Assessment of first wall W sources in view of ITER rebaselining
Linked to WP TE, W7X and DES

## Slide 7: Focused Topic 2025: JET post-mortem analysis and simulation
SP E: Erosion and deposition in JET / LIBS on RH demonstration
  LIBS data analysis and interpretation
  Application of AI with new project (learning )
  Interpretation of erosion and deposition at limiters, inner divertor apron, and bulk-W divertor
  Collection of JET samples (if we manage to get them) =>Cutting => likely no analysis in 2025
  Interpretation of H, D, T in W and Be => Retention information
SP D: Simulation of material migration and fuel retention in JET
  Simulation of global transport with ERO2.0 combined with EDGE2D-EIRENE or SOLPS-ITER
  Simulation of retention in samples (co-deposits and implantation)
  Simulation of Ni CXN sources (already started) and migration
  Analysis of migration paths in different configurations
Linked to WP TE

## Slide 8: Focused Topic 2025: Consequences of B application in ITER
SP B: Samples for boronization (lab) and in manipulators
  B co-deposits and mixed B+O deposits
  Exposure in linear plasmas (PSI-2 / GyM) / lab plasmas / magnetron / (boronization)
  Impact of B on mirror properties
SP C: Fuel retention and removal in B layers
  Retention in those layers as function of flux, temperature, composition (new scaling for T with B)
  Fuel removal assessment (microscopic)
SP D: Simulation of material migration and fuel retention
  A&M data and MD simulation of boron chemistry
  Simulation of B migration in full-W devices in view of ITER needs
  Simulation of B lifetime and distribution (WallDYN-3D and ERO2.0) => Schmid already NF in 2024
SP F: Boronisation properties and wall conditioning
  Boronisation homogeneity and improved understanding of function / lifetime
  Wall conditioning techniques for fuel removal and B removal from B layers (ICWC, GDC, ECWC) on tiles
  Laser-based techniques application on very thin B layers and retention assessment
Linked to IO and WP TE and W7X

## Slide 9: Focused Topic 2025: T in damaged W and steel / sensitivity increase
SP X: Laser-based techniques as tool to interpret T retention mechanisms
  T retention in W by laser techniques has been demonstrated in damaged and undamaged material
  Increase of sensitivity required at no/low damage needed to provide input on physics of retention mechanisms with high spatial and depth resolution (advanced approaches)
SP C: Damage mechanism in DEMO-relevant materials
  Retention of T in materials DEMO-like material temperatures (W, steel, EUROFER)
  Permeation of T through the materials into water (overlap with FTD?)
  Explore gentle D loading of n-damaged materials from fission reactors
Linked to WP SAE, BB, MAT

## Slide 10: Deliverables
PWIE D5.19 PWIE.D.19 Characterization and predictive modelling of plasma-wall interactions in He und He/H mixed plasmas for ITER in Pre-Fusion Power phase. 31/12/2025
PWIE D5.20 PWIE.D.20 High fluence exposition of mono blocks made of references W and advanced W materials for DEMO, JT-60SA, DTT in MAGNUM-PSI and UPP including pre- and post-characterisation. 31/12/2025
PWIE D5.21 PWIE.D.21 Fuel retention studies in self-damaged and neutron damaged materials exposed in JULE-PSI. 31/12/2025
PWIE D5.22 PWIE.D.22 Comparison of in-situ (LID-QMS in JET) and ex-situ examination (FREDIS, TDS) of the laser-irradiated components regarding fuel/tritium content. 31/12/2025
PWIE D5.23 PWIE.D.23 PSI modelling of DEMO main chamber erosion, deposition and fuel retention. PIC modelling of the sheath in the DEMO divertor (with TSVV-07). 31/12/2025
PWIE D5.24 PWIE.D.24 Neutral gas kinetics modular code upgraded and final verification/validation report (with TSVV-05). 31/12/2025
FPWIE D5.25 PWIE.D.25 Initial PSI modelling of W sources, screening, transport and core concentration in full W-devices (with TSVV-06). 31/12/2025