## Slide 1: SP B – production, exposure, and analysis of W layers in 2024
Antti Hakola
On behalf of the SP B team and task holders
Discussion on next steps and priorities

## Slide 2: Goals for discussions today
What kind of W samples should be produced in 2024?
  W samples for plasma experiments in the linear devices (MAGNUM-PSI, PSI-2, GyM)
    Different surface morphologies? Different impurities?
    Different H and D depth profiles? Multilayer structures?
    Layers mimicking re-deposited W layers?
  W samples for dust impact studies
    What are the specific needs here? Continuing comparing the erosion of bulk W vs. deposited layers?
  W samples for tokamak experiments (AUG) – late 2024, depends on the details of the experimental programme
  W samples for LIBS studies
    What are the actual needs? Layers for in situ studies, e.g., in MAGNUM-PSI?
What plasma exposures are to be carried out in 2024?
  Finishing the flux dependence exercise initiated in 2023 – need for additional samples?
  Differences in erosion yields of bulk vs. fuzzy W
  Production and further erosion of re-deposited W layers
What is the foreseen analysis programme in 2024?
  Availability of the different labs for analysis – boundary conditions

## Slide 3: Material from the midterm meeting I
MAGNUM-PSI (DIFFER):
  Study 2: comparing W erosion rates by Ar to data available from PSI-2 and GyM
  Study 3: exposing re-deposited W layers to determine their erosion characteristics
GyM (ENEA):
  Study 1: exposing nanocolumnar W samples to Ar plasma (leftover samples from 2023)
    Ion flux 1.41020 m-2s-1, fluence up to 1.01025 m-2, bias voltage to be decided
    Characterization using AFM and SEM-EDX
PSI-2 (FZJ):
  Study 3: exposing bulk W and fuzzy W to Ar plasma in PSI-2
    Combined with post-mortem FIB/SEM investigations – also erosion FIB markers on the agenda
Erosion investigations in laboratory conditions (ÖAW)
  determine sputter yields for W and W+B model systems under bombardment of 2 keV D2+ ions using the QCM measurement technique
  measure the angular dependence of sputter yield values
Influence of dust impacts on erosion and other properties of the co-deposits (ENEA):
  Investigate the vanishing bounding regime vs W-O co-deposit thickness
  Investigate the vanishing bounding regime vs different co-deposited type or O concentration in W-O co-deposit
  Investigate the W-O co-deposit delamination vs samples temperature (from RT to 400°C) to be closer to the actual environment in tokamaks
Already agreed: evaluate the amount of W-O co-deposit removed upon dust impacts  thickness of the co-deposits should be up to 4-5 mm and different dust speeds to be applied (e.g., 600, 1000, and 1500 m/s)

## Slide 4: Priorities for surface analyses (ion-beam analyses)
FZJ:
  Analyses of samples from SP B.1 and SP B.2 experiments
IST:
  Implantation of huge D amounts in W-based coatings, followed by NRA/TOF-ERDA and SIMS (VTT) and LIBS (SP X)
  Analysis of D, C, B contents by NRA, erosion studies by RBS/EBS
  Analysis of main heavier contaminants by PIXE
JSI:
  Broad-beam analyses (NRA, RBS, PIXE) for selected samples
  Micro-beam analyses (RBS, PIXE) for selected samples
MPG:
  Analyses of samples from SP B.1 and SP B.2 experiments
NCSRD:
  Characterization of plasma-exposed samples using ion beam analysis (RBS/NRA, PIXE/PIGE, TOF-ERDA)
RBI:
  Broad-beam (RBS, NRA, TOF ERDA, PIXE) and micro-beam (RBS, NRA, PIXE) analysis of samples
VR:
  Surface composition and depth profiles using ion beam analysis, with focus on TOF-ERDA and RBS
  Resonant-NRA at low energies combined with RBS will be performed in selected samples to obtain high-sensitivity and high-resolution boron depth profile (E. Pitthan et al. Surf. Coat. Tech. 417 (2021) 127188)
  Setups at Tandem Laboratory at Uppsala University (P. Ström and D. Primetzhofer, J. Instrum. 17 (2022) P04011)
VTT:
  Analyses of samples from SP B.1 and SP B.2 experiments
WEST, MAGNUM-PSI
WEST, GyM, PSI-2
WEST, GyM, MAGNUM-PSI, PSI-2
WEST, W7-X, PSI-2
W7-X, WEST, MAGNUM-PSI
W7-X, PSI-2, WEST
WEST, GyM, MAGNUM-PSI
WEST, GyM

## Slide 5: Priorities for surface analyses (other techniques)
CIEMAT:
  SIMS and SEM analyses for samples coming from SP B.1 experiments and SP B.4
ENEA:
  SIMS, XPS, TDS (950 °C), LEIS devices available
FZJ:
  Microscopy analyses of samples from SP B.1 and SP B.2 experiments
IAP:
  GDOES and XPS for WEST samples (similarly to C3-C5 marker tiles)
IPPLM:
  Microscopy analyses of samples from SP B.1 and SP B.2 experiments
MPG:
  SEM and FIB analyses of samples from SP B.1 and SP B.2 experiments
NCSRD:
  Determination of surface state and crystalline structure of plasma-exposed samples (SEM/EDS, XRD)
VTT:
  SIMS analyses of samples from SP B.1 and SP B.2 experiments
TBD
W7-X, WEST, PSI-2
WEST, W7-X, MAGNUM-PSI
WEST
GyM, MAGNUM-PSI, PSI-2
WEST, GyM, MAGNUM-PSI
WEST, GyM, MAGNUM-PSI, PSI-2
WEST, GyM, MAGNUM-PSI, PSI-2, dust gun

## Slide 6: Material from the midterm meeting II
W-based layers and their characterization using PLD and HiPIMS/magnetron sputtering (ENEA):
  Production of reference coatings with different morphologies and crystallinity - from compact to porous, from crystalline to “amorphous”
    Use both metallic and patterned Si substrates (flat vs. pyramidal)
  Varying the impurity content of the layers (O, N, Ne)
  Production of multilayer structures of W
  Characterization by SEM, EDX, and AFM
Production of W layers (IAP):
  Production of W coatings with varying H and D depth profiles simultaneously
  Analysis of the produced coatings:
    GDOES for depth profiling, XPS for chemical composition, XRD for phase composition
SP X collaboration and LIBS development
  In any case, depth resolution of ~15 nm (=shallow ablation depths) required for LIBS studies to efficiently determine the impurities and their concentrations as a function of depth
  LIBS can be applied for studying the composition and fuel retention in such layers
    Can also be combined with LID-QMS
  LIBS can be combined with linear-machine experiments in PSI-2, UPP and MAGNUM-PSI  in situ investigations