## Slide 1: LID Rastering
11.3.2020 I Miroslaw Zlobinski et al.
Thermal simulation (ANSYS) #1

## Slide 2
Laser Parameters
earlier:
minimal requirements to reach Be melting at 1550 K from room temperature: e.g. with 1 ms pulse and 4.5 J absorbed energy on 3 mm diameter spot
This simulation:
1 ms pulse and 3.7 J absorbed energy on 3 mm diameter spot (i.e. 530 MW/m2) (for comparison: 1D-analytical calculation with temperature-independent material parameters: temperature increase from 300 K to 1350 K maximum temperature)

## Slide 3
Geometry
1 ITER castellation block
28 mm
12 mm
4 mm
8 circular laser spots with 3.0 mm diameter 3.0 mm centre-to-centre distance here max.: 24 spots (with margin)
[without margin: max. full coverage: 36 spots (4 x 9)]
2 mm margin
2
1.5

## Slide 4
Material parameters
W substrate (temperature dependent heat properties) no layer
Heat capacity Thermal conductivity
Density

## Slide 5
Temporal pulse shape
8 laser pulses, each 1 ms duration, every 7.0 ms (143 Hz)
Each laser pulses nearly rectangular with 0.1 ms for rising and 0.1 ms for falling edge
0.1 ms 1.0 ms
Laser intensity / MW/m2
time/s
0

## Slide 6
Result Video

## Slide 7
Result: Maximum Temperature vs. time
maximum temperature ca. 1280 K, material cools between pulses, no strong accumulative heating effect
to improve: smaller time step during laser pulse to better calculate maximum temperature

## Slide 8
Result MaximumTemperatur vs. time
Spatial temperature distribution at the end of 8th laser pulse (49.9 ms)

## Slide 9: End