## Slide 1: Impurities in long-pulse operation of W7-X
Monika Kubkowska
M. Jakubowski2, M. Krychowiak2, A. Dinklage2, M. Gruca1, S. Jablonski1, L. Syrocki1, B. Buttenschoen2, F.Reimold2, Yu Gao2, G. Fuchert2, S. Lazerson2, D. Naujoks2, U. Neuner2, O. Grulke2, V. Winters2, D. Zhang2 and the W7-X team 1Institute of Plasma Physics and Laser Microfusion, Warsaw, Poland 2Max-Planck-Institut für Plasmaphysik, Greifswald, Germany
Institute of Plasma Physics and Laser Microfusion, Warsaw, Poland
This scientific paper has been published as part of the international project co-financed by the Polish Ministry of Science and Higher Education within the programme called 'PMW'.
50th EPS Conference on Plasma Physics
Work done under EUROfusion WPW7X

## Slide 2: Outline
Motivation
Wendelstein 7-X
Impurities in W7-X’s long pulses in dettached and attached divertor configuration
Summary

## Slide 3: Outline
Motivation
Wendelstein 7-X
Impurities in W7-X’s long pulses in dettached and attached divertor configuration - ECRH heated plasma
Summary

## Slide 4: Long pulse operation
Extending plasma pulse length is essential for an economically viable fusion reactor.
The goal of the W7-X is to demonstrate the high performance with high power and quasi-continuous operation.
In W7-X OP1.2b experiments despite a high influx of C into the SOL during discharges with dedicated overloading of the leading edges, the plasmas remained stable. Zeff stayed below 1.5 throughout the discharge, and radiation increased at the plasma edge only.
Long-time scale processes could play a role, like wall recycling or erosion.

## Slide 5: Long pulse operation in fusion devices
Plasma heating power normalized to the plasma surface (P/S in MW m2) vs the high-performance duration.
X. Litaudon et al., Nucl. Fusion 64 (2024) 015001
The highest values of P/S have been obtained on the ASDEX Upgrade with a tungsten wall, but it is limited in duration by the machine’s technical capability (no active cooling and normal conducting magnet).
For ITER, the expected ratio of P/S is in the range of 0.2 MW m−2, to be sustained from 100 s up to 3000 s (when adding the externally injected power to the self-alpha heating power produced by the D-T fusion reactions, P is in the range of 150 MW).

## Slide 6: Long pulse operation in fusion devices
Plasma heating power normalized to the plasma surface (P/S in MW m2) vs the high-performance duration.
The highest values of P/S have been obtained on the ASDEX Upgrade with a tungsten wall, but it is limited in duration by the machine’s technical capability (no active cooling and normal conducting magnet).
For ITER, the expected ratio of P/S is in the range of 0.2 MW m−2, to be sustained from 100 s up to 3000 s (when adding the externally injected power to the self-alpha heating power produced by the D-T fusion reactions, P is in the range of 150 MW).
For W7-X P/S values are in the range 0.03-0.05 for a typical long pulse scenario
X. Litaudon et al., Nucl. Fusion 64 (2024) 015001
detached
attached
W7-X: 0.05MW/m2

## Slide 7: Introduction to Wendelstein 7-X
Major radius R = 5.5 m
Minor radius r = 0.5 m
Plasma volume V = 30 m3
Long pulse operation (30 min)
Water cooled island divertor
PECRH = 8.5 MW
PNBI = 6.6 MW
PICRH = up to 1.5 MW
R
r
A. Langenberg, PLASMA-2023 conference
©IPP

## Slide 8: Introduction to Wendelstein 7-X
W7-X Status / Achievements:
4 experiment campaigns (2015-2022): OP1.1, OP1.2a/b, OP2.1
~15 months of plasma operation
Main plasma parameters close to NC[1] expectations:
        Ti = 3.0 keV[2], ne = 1.4 x 1020 m-3[3]
        Wdia = 1.1 MJ[2], tE = 0.3 s[2]
Long pulse operation 480 s[4], stable detachment[5]
No impurity accumulation issues[6]
[1] C. Beidler, H. Smith, A. Alonso et al. Nature 596 (2021)
[2] S. Bozhenkov, Y. Kazakov, O. Ford et al. Nuclear Fusion 60 (2020)
[3] G. Fuchert, K. Brunner, K. Rahbarnia et al. Nuclear Fusion 60 (2020)
[4] H.-S. Bosch, P. van Eeten, O. Grulke et al. Fusion Engineering and Design 193 (2023)
[5] M.W. Jakubowski, et al. Nucl. Fusion 61 (2021)
[6] Th. Wegner, J.-P. Bähner, B. Buttenschön et al. Journal of Plasma Physics 89 (2023)
A. Langenberg, PLASMA-2023 conference
©IPP

## Slide 9: Introduction to Wendelstein 7-X

## Slide 10: W7-X timeline
10
2015 / 2016
5 MW
4 MJ
6 sec
2017 / 2018
8 MW
200 MJ
100 sec
Inertial cooling
Inertial cooling
graphite divertor in OP1.2, 10 MW/m2
2022 - 2026
10 MW
1GJ, 18 GJ
30 minutes
…
Water-cooling of PFCs
OP1.1
OP1.2
OP2
202x …
Heating upgrades
18 GJ
30 minutes
OP3
carbon-free device

## Slide 11: W 7-X: Island divertor: exhaust for helical plasma
Open field lines guide ions lost from the confined plasma to the divertor targets. Islands form SOL.
Large magnetic islands (standard: 5/5 ) form so-called island divertor.
W7-X wants to demonstrate high power, high performance at steady-state 10 separate divertor units, adapted to the shape of the flux surfaces
There are two notable difference between island SOL and tokamak SOL:
Long connection length: W7-X:

## Slide 12: W 7-X: Island divertor
Island divertor at W7-X in standard configuration forms two strike-lines on horizontal and vertical target
Thermography shows strike lines of island divertor

## Slide 13: Long pulse development at Wendelstein 7-X
Detached plasma
High Low
Reactor relevant divertor downstream paratemeters (e.g. Te,downstream ~ 5 eV and
Attached plasma
Low High
Reactor relevant power fluxes in attached plasmas
heat flux [MW/m2]
Future reactor will operate with power fluxes of up to 5 MW/m2.  In stellarator-based 500 MW reactor about 80-85% of total heating power needs to be radiated away  In Wendelstein 7-X with PECRH = 7 MW we cannot have both requirements simultaneously.
Research conducted at the W7-X allows the study of certain aspects of fusion reactors.
D. Zhang, et al , PRL, 2019

## Slide 14: W7-X detached long pulse scenarios
Plasma radiation proportional to C2+ intensity and plasma density
Obtaining detachment with help of intrinsic impurities (carbon) is rather straightforward at W7-X.
Carbon is released from the plasma facing components (mostly due to oxygen sputtering)
In order to reach certain level of radiated power we need to increase carbon concentration at the plasma edge (via plasma density).
V. Perseo et al 2021 Nucl. Fusion 61 116039

## Slide 15: W7-X detached long pulse scenarios in OP1.2b
M. Jakubowski et al 2021 Nucl. Fusion 61 106003
O. Schmitz et al 2021 Nucl. Fusion 61 016026
Detached discharge in OP1.2b – W7-X with inertially cooled divertor
line integrated density is raised to a level above 1e20 m-2, in that case the plasma radiated power fraction was at level exceeding 0.8 (frad ≥ 0.8) and peak heat flux below 0.5 MW/m2.
What is important that the average effective ion charge Zeff, obtained from the spectroscopic bremsstrahlung measurements, was constant at the level around 1.5

## Slide 16: W7-X detached long pulse scenarios
No significant increase of impurity during the discharge,
The main contribution to Zeff comes from carbon as the divertor’s material

## Slide 17: W7-X detached long pulse scenarios
prolonged in OP2.1 to 100 s
with actively water cooled divertor configuration
The oscillations seen in the transition period are artefacts due to the feed-back controller settings, which results in changes in Prad and automatically divertor power loads.

## Slide 18: W7-X detached long pulse scenarios in OP2.1
prolonged in OP2.1 to 100 s
CVI line intensity looks rather stable
O lines intesity little increase but it doesn’t affect the Zeff value which are below 2 over the discharge

## Slide 19
Lower carbon contents at the plasma boundary due to boronizations
Boronization produces boron dominated layer on a PFC, which has a strong ability to getter oxygen.
  In OP1.2: Oxygen reduced by a factor of 10 (or a lot more, in some cases)
  Carbon reduced by about a factor of 7, to large degree due to much lower oxygen content at the plasma edge.
Inefficient absorption O2 ECRH
After 3 boronizations
T. Wauters et al. Nuclear Materials and Energy 17 (2018) 235

## Slide 20: Choice of seeding impurities for heat load control
The choice of impurities or the mix of several impurities will depend on the expected temperature range, the achievable impurity density nZ and ne.
As the SOL at W7-X is supposed to operate at plasma electron temperatures of few to 10 eV the choice of impurities is limited to low- or medium-Z species, e.g. N2 or Ne.
Especially nitrogen seems to be attractive impurity as it LZ characteristics is similar to carbon
SOL of island divertor at Wendelstein 7-X
Lz calculated for coronal equilibrium [1]
M. Wischmeier, et al., IAEA-FEC TH/P7-5 (2018)
Cooling factor for a set of intrinsic and seeded impurities

## Slide 21: Detachment with neon seeding long lived due to high recycling of Ne
C
C
C + Ne
C + Ne
C + remaining Ne
C + remaining Ne
Prad  1.5 MW
OP1.2b
M.W. Jakubowski, et al., PSI 2022
F. Effenberg, et al. Nuc. Fus. 59, 106020 (2019).

## Slide 22: Neon seeding lead to detachment very similar as the intrinsic detachment
To increase ne Ne every 2.5 s was puffed which kept Prad baseline constant at frad = 0.8 in the first 18 s of discharge (gyrotrons dropped after 18 s).
Ne was almost constant at the level of 1.3×1020 m-2 during the entire discharge.
averaged heat flux distribution on the divertor plate in the t=8-15 s shown, the peak heat flux during the detached phase for Ne seeding stay at the very low level, remaining almost everywhere below 0.5MW/m2.
Ne line intensities of the higher ionization levels oscillate with each puff after an initial increase, but the baseline remains constant -> no Ne accumulation in the plasma core
No significant C and O changes
Seeded impurity does not affect the core plasma
Radiation fraction in the confined plasma region is higher – max radiation is at higher temperatures
OP2.1

## Slide 23: The longest OP1.2b discharge with attached divertor
The radiation fraction frad during the entire programme was about 30%, which resulted in a fully attached divertor plasma.
ne was stable till t = 80s. As in the previous campaign the divertor units were not water-cooled their surface temperature was increasing throughout the experiments.
During this program it reached the surface temperatures above 1000C. This resulted in the stronger emission of impurities, e.g. oxygen or water molecules from the divertor target plates, which increased plasma radiation and plasma density in the last phase of the discharge.

## Slide 24: Record heating energy of 1.3GJ w/ attached divertor in OP2.1
O. Grulke, 29th FEC IAEA conference

## Slide 25: Attached divertor configuration – similar to the record pulse
Results from PHA spectra simulations

## Slide 26: Summary
First campaign with water-cooled plasma facing components (incl. HHF divertor) allowed to gain first experience with long pulse scenarios:
    8 minute attached plasma
    >100 s detached plasma
    W7-X ECRH plasma is resilient to impurity accumulation in spite of long pulse scenarios with high plasma radiation.
    Both Ne and C are suitable for power dissipation in the long pulse discharges.
112 s
480 s

## Slide 27: Thank you for your attention!
Work done under EUROfusion WPW7X

## Slide 28: W7-X: attached and detached divertor configuration
Attached (touching):
Hot plasma (20 eV – 100 eV) in direct contact with divertor plates  higher heat loads.
Stronger particle flux  particles arrive at higher rate.
Detached (not touching)
Colder plasma (< 5 eV) in direct contact with divertor plates  Power radiated away, low heat loads.
Higher recycling of particles