## Slide 1: Boronisation studies : current status of knowledge and plans for 2024-2025 within WP TE
E. Tsitrone
Many thanks to the RT-06 RTC : Y. Corre, K. Krieger, A. Widdowson and the AUG and WEST team (V. Rohde, A. Gallo, E. Geulin, M. Diez, C. Martin …)
Acknowlegments to the ITPA DivSOL « Report on the new ITER baseline with a W wall, issues and open R&D questions” (V. Rohde, S. Masuzaki, T. Wauters for the Boronisation section)
TE-PWIE workshop, September 17, 2024

## Slide 2: Outline
EU has a good portfolio of metallic machines to study boronisation in support of the new ITER baseline : AUG and WEST
Current status of knowledge on boronisation from WP TE devices
Impact of boronisation on plasma operation
Distribution of boron layers in the vessel
Plans for AUG/WEST in 2024-2025
Summary

## Slide 3: Outline
EU has a good portfolio of metallic machines to study boronisation in support of the new ITER baseline : AUG and WEST
Current status of knowledge on boronisation from WP TE devices
Impact of boronisation on plasma operation
Distribution of boron layers in the vessel
Plans for AUG/WEST in 2024-2025
Summary

## Slide 4: Boronisation opens up the operational domain
[J. Bucalossi et al., NucFus 2022]
  AUG : boronization required for low density operation
  Usual reduction of oxygen contamination / radiated power
  Widens H mode operation space w/o W accumulation
  Low density / high Te operation achievable after fresh boronisation (AT, RMP ELM suppression, fast ion scenarios ...)
  WEST : 1st boronization was key in early days of operation
  Usual reduction of oxygen contamination / radiated power
  Improved breakdown conditions
    Avoidance of Runaway Electrons (high level of impurities  narrow operational window for burn-through)
  Higher density operation achievable
[A. Kallenbach et al., Nuc Fus 2009]
Both devices use boronisation for initial conditioning after venting

## Slide 5: Operation without boronisation is possible but requires specific tuning
  AUG : successful restart w/o GDB in full W configuration performed
  Plasma restart possible, ~ 1500 pulses before GDB
  Operational limit : W core accumulation / core radiative losses compared to core heating (ELM frequency)
  Recipe : use ECRH for central heating / operate at large gas puff
  WEST : successful long pulse operation w/o boronisation
  Operation w/o boronisation for dedicated PWI campaigns where no modification of wall conditions required
  High D fluence campaign (> 400 long pulses, ~ 30 GJ of coupled energy, ~3h of plasma) : no evolution of the radiated fraction in the ohmic phase
[A. Kallenbach et al., NF 2009]
[A. Gallo et al., submitted to NME ]
AUG
WEST

## Slide 6: Boronisation “lifetime” : several time constants involved
  WEST : impact on radiated power:
    Plasma breakdown :
      strong reduction in radiated power, recovery 40-60 pulses
    Limiter phase
      Less pronounced reduction in radiated power, faster recovery (~10 pulses)
    Diverted phase (LSN) :
      Reduction in radiated power vanishes rapidly (~ few pulses)
[J. Bucalossi et al., IAEA 2023, submitted to Nuc Fus]
[A. Gallo et al., APS 2022]
Learning curve
      Caveat : comparison difficult as boronisation conditions (nb of anodes, B consumption, Twall…) + recipe for plasma breakdown / ramp up / flat top scenario evolves
  AUG :
    Short term (recycling, B coverage in strike point area) vs long term (O level) effects also evidenced

## Slide 7: Boronisation transiently reduces recycling, but has little long term impact on fuel retention
[V. Rohde et al., JNM 2007, A. Kallenbach et al., Nuc Fus 2009 ]
  AUG : boronisation transiently reduces recycling
    B layers from boronization increase D wall pumping during 1 or 2 days of operation (Reduced D recycling at boronized W surfaces, stronger D gas puff needed to reach given density)
    Hard to quantify impact of B layers on overall D retention as B layers get eroded from PFCs ==> requires repetitive GDB and fixed scenario
  WEST : modest/short term impact of boronisation on fuel retention for long pulse operation
    Particle balance repeated before / after boronisation on long pulse (~1 minute)
    Strong impact on 1st short ohmic pulse : strong increase in gas puff needed to reach equivalent density (x2)
    Modest (inverse) impact after ~100s of plasma on fuel retention during long pulse
[E. Tsitrone et al., ITPA DivSOL meeting, Kyoto, Feb 2024]
AUG

## Slide 8: Impurity powder dropper : risk mitigation for ITER
  Wall conditioning evidenced on both machines
    Beneficial effects on wall pumping, reduction of oxygen content and radiated fraction in both devices
    Improved confinement observed in both devices
    Large B rate can have adverse effect (up to disruptions)
    During the drop in WEST : increased W sputtering, but reduced W core transport , beneficial impact above threshold
    Main chamber in AUG : local limiter B coverage much larger than for conventional GDB : margin for drop rate
[K. Krieger, NME 2023]
[K. Afonin, NME 2024]
WEST
[R. Lunsford, NME 2024]
WEST and AUG equipped with IPD : deposition channels / local distribution of B different from GDB
 Can extend the lifetime of deposited boron layers on areas prone to rapid erosion
[R. Lunsford, NucFus 2019]
AUG

## Slide 9: Complex structure of B layers found in tokamaks
  WEST : non uniform B layers evidenced
    Divertor : B rich layer found in HFS deposits (far SOL)
    First wall : non uniform poloidal / toroidal deposited layer thickness, B rich layers interleaved with W oxide layers
  AUG :
    Whitish unstable B layers found when venting : cleaned after each campaign with wet wiping
WEST divertor deposits after the C7 campaign
WEST first wall deposits after C3
W
O
B
  In both machines :
    Difficult to disentangle impact of C and B
    Wide D/(B+C) range : from 0.1 to 0.4
[C. Martin, submitted to PSI 2024]
[E. Bernard, PSI 2022, R. Sakamoto, private com.]
[Courtesy V. Rohde]

## Slide 10: Outline
EU has a good portfolio of metallic machines to study boronisation in support of the new ITER baseline : AUG and WEST
Current status of knowledge on boronisation from WP TE devices
Impact of boronisation on plasma operation
Distribution of boron layers in the vessel
Plans for AUG/WEST in 2024-2025
Summary

## Slide 11: Specific features of WEST / AUG for the 2024 / 2025 campaigns
  AUG :
    Restart after long shutdown with new upper divertor
    Manipulators available for sample exposure during boronisation (LTS available)
    New diagnostics for material migration (QMB)
  WEST :
    Change of inner / outer bumper tiles from BN back to W
    Boronisation collector probe available in 2025 (LTS available)
    Longer term : LIBS (LID QMS) for in situ measurements
WEST ready for phase 2 – summer 2021
September 2024
New upper divertor for AUG – September 2024
[Courtesy V. Rohde]

## Slide 12: Plans for 2024 : focus on B layer uniformity
  Test (briefly ) start up without boronisation :
    WEST : restart w/o GDB for a few days
    AUG : restart w/o GDB for 1 day or until required data (spectroscopy …) available
    NB : restart presently planned on both machines by ~mid October (stay tuned to WP TE news)
Similar restart plan for both AUG/WEST
  Perform “half” boronisation :
    WEST : 3 of 6 anodes, ITER ref temperature (70°C), no collector probe available in 2024 (will be repeated in 2025 with collector probe, exposing W and SS samples), LTS
    AUG : 2 of 4 anodes, room temperature, samples exposed in manipulators + LTS + new QMB
  Perform “full” boronisation :
    WEST : 6 anodes at 70°C, no collector probe available in 2024 (will be repeated in 2025 with collector probe, exposing W and SS samples), LTS
    AUG : 4 anodes, room temperature, samples exposed in manipulators + LTS + new QMB
Reference shots required to be repeated for comparison of no boro / half boro / full boro
    On both machines : perform start up limiter studies on W inner bumpers for each phase (tbc)

## Slide 13: Longer term plans on AUG/WEST
Call for 2025 experimental proposals now open !
https://wiki.euro-fusion.org/wiki/WPTE_wikipages:_Call_for_proposals_2025
  Scientific objectives of RT06 (Preparation of efficient Plasma Facing Components (PFC) operation for ITER, DEMO and HELIAS) : increased focus on boronisation
    Quantify local power load distributions on castellated and shaped PFCs for ITER and DEMO…
    Assess the impact of sustained high power / high particle fluence plasma …
    Quantify material erosion sources from metallic walls under ITER relevant plasma conditions …
    Quantify fuel retention in devices with metallic walls, with a focus on long pulse operation (using recent fuel retention diagnostic upgrades such as laser-based diagnostics where available) and including impact of boronisations
    Determine fuel-removal in metallic devices in conditions relevant for ITER (including the impact of boronisation) and extrapolate to DEMO
    Assess efficiency and lifetime of conditioning methods in metallic devices, with a focus on boronisation
  Deadline October 11
    All details on WP TE wiki :

## Slide 14: Outline
EU has a good portfolio of metallic machines to study boronisation in support of the new ITER baseline : AUG and WEST
Current status of knowledge on boronisation from WP TE devices
Impact of boronisation on plasma operation
Distribution of boron layers in the vessel
Plans for AUG/WEST in 2024-2025
Summary

## Slide 15: Summary
  Boronisation routinely used in AUG / WEST :
  After a vent and/or to access specific plasma conditions
      High Z material coverage by B in plasma exposed area (transient)
      Reduction of D recycling / enhanced wall pumping (transient)
      O gettering ( decrease of W sputtering by impurities) (longer term)
    Used to gain experimental time (“kitchen physics” based on TEXTOR recipe)
    B chemistry complex (and largely unknown in tokamak conditions)
  New focus as required for full W ITER configuration :
      Optimize boronisation parameters for ITER (electrodes, injection points, wall temperature etc  design) and assess frequency required (conservative IO estimate : up to once every 2 weeks)
      Impact of B on fuel retention / removal (D/B, disentangling B vs C)
      Increased modelling capabilities needed (B deposition from GDB, subsequent B migration during plasma operation, fuel uptake / removal and O gettering)
  Synergies between PWIE / TE : well controlled experiments in linear devices (parametric dependencies) vs integrated tokamak experiments + post mortem analysis of tokamak exposed samples